Dynamic Charge Characteristics of High Carbon Lead Acid Batteries in Electric Vehicle Traction Applications

By

Katharine May Fewings

A thesis submitted in partial fulfilment of the requirements for the degree of

Master of Philosophy

The University of Sheffield

Department of Electrical and Electronic Engineering

Electrical Machines and Drives Group

Supervised by Prof David Andrew Stone and Dr Martin Paul Foster

September 2015

## Acknowledgements

I am deeply grateful to my supervisors Prof David Stone and Dr Martin Foster for allowing me the opportunity to complete this work and for providing me with support, encouragement and advice throughout my M.Phil.

I would especially like to thank Dr James Green for the support he provided in the first months of my M.Phil, for his continual advice and for encouraging me to deepen my knowledge.  Additionally I would like to thank Dr Dan Gladwin for his thesis writing advice as well as the conversations we shared about my project.

I would also like to thank my work colleagues for their thought provoking conversations on a wide range of interesting topics.

Finally I would like to give my thanks to my amazing family for the support that they have all given me over the years.  To my dad for knowing the answer to every “how does this work” question that I have asked since childhood, to my mum for always, always having faith in me and my brother for his ability to make me laugh no matter what.

## Abstract

The work presented in this thesis was completed with the aim of providing a complete picture of the dynamic charge acceptance (DCA) behaviour of lead-acid (PbA) batteries of different carbon additive technologies.  It was inspired by the growth in the electric vehicle (EVs) market due to the increasing need for clean energy and the fact that, despite advancements in their technology, EVs still remain expensive due to the cost of the battery.  Considering their inexpensive manufacturing costs, as well as material cost, the advancement of automotive PbA batteries for EV use is an area of high interest.  The recent development of PbA batteries with carbon additives makes them a reasonable battery choice in the future for EVs, due to their continuous improvements in charge acceptance and battery life.

To help the reader to understand the challenges of using PbA batteries in EVs the high-rate, partial-state-of-charge operation mode required of them is reported on, as well as the detrimental effects this can have on the PbA battery technology.  The benefits of carbon additives to PbA are then presented as well as the different high carbon PbA battery technologies used within this work.  DCA measurements are defined and their applicability to determine a battery’s suitability for use in EVs is outlined.  This thesis will then describe the test rig designed to complete the DCA tests as well as the LabVIEW (Laboratory Virtual Instrument Engineering Workbench) control software.   The results of the (DCA) testing are then reported on and discussed before the scope for further study is examined.

## Glossary

ADC 	Analogue to digital converter

AGM 	Absorbent Glass Mat

BEV		Battery electric vehicle

Cexp		Experimentally measured capacitance of the battery

CHA		A charging period within the testing sequence

Char		Test results for charging state of charge steps

Cnom		Nominal capacitance of the battery

DCA		Dynamic charge acceptance

DCH 	A discharging period within the testing sequence

Dis 		Test results for discharging state of charge steps

e-  		Electron

EV		Electric vehicle

H+ 		Hydrogen ion

H2O		Water

H2SO4	Sulfuric acid

HEV		Hybrid electric vehicle

HRPSoC	High rate partial state of charge

ICE		Internal combustion engine

ICEV		Internal combustion engine vehicle

k 		An integer value

LabVIEW	Laboratory Virtual Instrument Engineering Workbench

LIB 		Lithium ion battery

NI		National Instruments

NiMH 	Nickle metal hydride

OCV 	Open circuit voltage

Pb		Lead

PbA		Lead-acid

PbO2	Lead dioxide

PbSO4 	Lead Sulfate

PUA 	A pause period within the testing sequence

Q		Charge added or removed to or from the test battery

SLI		Starting lighting ignition

SoC		State of charge

TDMS	Technical Data Management Streaming

VI		Virtual instruments

VRLA	Valve regulated lead acid

x 		The charging current factor that the capacity of the battery is multiplied by during microcycles

μCycle	A complete microcycle within the testing sequence

- Contents

Acknowledgements	i

Abstract	ii

Glossary	iii

Chapter 1	Introduction	1

1.1.	The history of the automotive lead-acid battery	1

1.2.	New demand for electric vehicles	5

1.3.	Modern electric vehicle technology	5

1.4.	Automotive battery technology within electric vehicles	7

1.4.1.	Nickel Metal Hydride	7

1.4.2.	Lithium ion	7

1.4.3.	Lead–acid	8

1.5.	The role of the PbA battery in the future of EVs	9

1.5.1.	The “UltraBattery”	10

1.6.	Dynamic charge acceptance	12

1.7.	Test procedure	13

1.8.	Conclusion	16

1.9.	References	17

Chapter 2	Design of test rig setup hardware	21

2.1.	Test facility design requirements	21

2.2.	Test facility implementation.	23

2.3.	Test Rig	23

2.3.1.	Power Supply (DC Link)	24

2.3.2.	Push-Pull power stage	25

2.3.3.	Control board	27

2.3.4.	Programmable voltage limiter board	28

2.3.5.	Temperature controlled chamber.	29

2.4.	Control Interface System	30

2.5.	References	31

Chapter 3	Test procedure software	32

3.1.	Overview of LabVIEW software	32

3.2.	Master VI	33

3.3.	Checking SoC VI	36

3.4.	Charger VI	37

3.5.	Rest VI	41

3.6.	Microcycle VI	41

3.7.	DAQmx Interface	43

3.8	Recording Data	45

3.9	Conclusion	47

3.10	References	47

Chapter 4	DCA test results	48

4.1.	Test Batteries	48

4.2.	DCA Results	50

4.2.1.	1.67C Microcycle Charging Current	51

4.2.2.	4C Microcycle Charging Current	58

4.3.	Conclusion	68

4.4.	References	69

Chapter 5	Discussion	71

5.1.	Results discussion	72

5.2.	Future study	74

5.3.	References	75

Appendix 1 – Test procedure flow diagram	76

Appendix 2 – Software State Diagram	81

# Introduction

The work in this thesis aims to investigate the dynamic charge acceptance (DCA) properties of carbon enhanced lead-acid (PbA) batteries, using a made for use test rig.  The test rig is verified by comparative measurements of DCA in a number of different carbon enhanced PbA batteries together with a standard motorcycle starter battery, used as the control.  This chapter aims to define DCA in terms of battery performance  and show how it is measured.  It will outline the rise of electric vehicles (EVs) as well as what benefits batteries with a high DCA have in the EV market.  This will be done by presenting previous research in the area as well as outlining the need to investigate the future potential of advancements in PbA technology.  The test procedure used throughout testing will be presented and finally this chapter will outline the thesis structure.

## The history of the automotive lead-acid battery

While commercial EVs may seem to some to be a relatively new technology, born out of the recognition of the damage caused by fossil fuels, EVs have been in use since the 19th century.  The first examples, created in the 1830s, relied on non-rechargeable batteries, before the invention of the mass-produced rechargeable battery which led to a wider use of the technology [1.1].  Due to the unreliable nature of early internal combustion engine vehicles (ICEV), and the need for a manual crank start, most private cars of the time would have been electric [1.1].  During this time EV technology was complemented by the PbA battery, the first rechargeable battery technology.

First established in 1859, a creation of Gaston Planté [1.2], the PbA battery rapidly found its place in the automotive world as well as stationary storage applications.  The battery, in its infancy, consisted of two lead (Pb) plates, separated by rubber strips, which were immersed in a sulfuric acid (H2SO4) electrolyte solution.  After a current was passed from one plate to the other and then removed from the solution a potential voltage appeared across the plates, allowing for a reverse current to be generated from the battery cell [1.2].

Despite further developments, the PbA battery was initially restricted by its limited capacity and low specific energy, the measure of energy stored per kg, as well as the slow manufacturing process.

It had previously been established, by Kӓstner, Nobili, Schönbien and Wheatstone in 1810, 1828, 1838 and 1843 respectively, that passing a current through lead electrodes that are submerged in an H2SO4 solution will result in a formation of lead dioxide (PbO2) on one of the electrodes [1.2].  However, it wasn’t until 1881 that the major breakthrough in PbA battery technology was developed by Camille Fauré: a process of coating the lead plates in a red lead oxide, sulfuric acid and water paste [1.2].  When this paste was applied the plates, which were then charged, active masses of Pb and PbO2 were formed on the separate plates.  This process not only allowed for the industrial production of PbA batteries, but also the specific energy of the battery was greatly improved to 8 Wh kg-1 at 10 hours discharge rate. This allowed for one of the first practical EVs, powered by rechargeable PbA batteries, to be invented by Gustave Trouvé in 1881 [1.2].  Within 20 years this technology was fitted in submarines, dirigible balloons and, by 1899, a PbA battery powered EV broke a speed record of 109 km h-1 [1.2].

However, despite their initial popularity, as technology moved on and the self-starter for the ICEV was invented in 1911, production of EVs fell into decline.  With an increased access to cheap fuel, a substance with a specific energy of 9000 Wh kg-1 compared to even the modern day PbA battery’s specific energy of 30-40 Wh kg-1 [1.2] the ICEVs popularity grew and the rechargeable PbA battery was left with the secondary automotive functions of starting, lighting and ignition (SLI) [1.1].

Despite changes to the battery design the chemical reaction within the system was established in 1882 by Gladstone and Tribe [1.4] and has remained unchanged.  It is known as the double sulfate theory and is as follows:

PbO2 + Pb + 2H2SO4  ↔ 2PbSO4 + 2H2O

This can be further broken down for the negative electrode:

Pb + HSO4  ↔  PbSO4 + H+ + 2e-

and for the positive electrode:

PbO2 + HSO4 + 3H+ + 2e-  ↔  PbSO4 + 2H2O

For all above reactions a discharge period reads from left to right and in reverse for a charging period.

Despite all of the advancements there were still a number of fundamental problems with the PbA battery, including water loss and over gassing during use.  It was found that charging both of the electrodes would result in an electrode potential of –0.358 V on the negative electrode and 1.690 V on the positive electrode causing a total cell voltage of 2.048 V [1.4].  As this voltage is higher than the standard voltage used for water decomposition, charging the battery will result in a loss of water in the electrolyte during operation [1.4].  This was especially true in the early 20th century when the lead sheets that had previously made up the electrode plates had been replaced with lead alloy grids, consisting of lead and high levels of antimony, while sintered PVC was used for the separators [1.2].  While, the antimony in the positive electrode helped to improve the drive cycle of the battery, as the electrode naturally corroded it was found that the antimony was deposited on the negative plate via the acidic electrolyte [1.2].  This was prone to triggering a hydrogen evolution during low overpotentials, resulting in an acceleration of water decomposition in the electrolyte [1.2].  Therefore the battery water levels would need to be systematically topped up.  To combat this the antimony-lead plate grids were replaced with calcium-lead and the problem of water loss and the maintenance connected to it were reduced [1.2].

This, however, was not enough to allow for the battery to be sealed as, during charging and overcharging periods, hydrogen is produced on the negative electrode due to the reaction:

2H+ + 2e-  →  H2

While oxygen is produced on the positive plate during these periods due to:

H2O  →  12O2 + 2H+ + 2e-

Both of these gas evolutions will result in an increase of pressure in a closed system [1.4].  Therefore, the focus turned to facilitating an oxygen recombination cycle where the separator material and electrolyte would allow for the oxygen to reach the negative plate where it could be reduced.  Two separator types, both consisting of silica, were developed.  The first, in 1935, was created by Otto Jache from Sonnenschein and consisted of a porous silica gel. The second  was made in 1967 by D.  McClelland and J.  Devitt of Gates Corporation and consisted of silica glass fibres. The latter was known as absorbent glass mat (AGM) [1.2].  These both create small gas channels allowing the oxygen to dissipate through the material to the negative electrode where the following reaction can occur to create an oxygen recombination cycle:

12O2 + 2H+ + 2e-  →  H2O

However, despite the silica separators, it is still possible that the production of oxygen at the positive plate can become too high for the oxygen reduction at the negative plate.  Therefore a valve was built into the cell lid to allow for a release of excess pressure creating a valve regulated lead acid (VRLA) battery [1.4].  The valve is kept closed during normal operation to prevent gases entering the battery, only opening to vent the oxygen when the pressure within the battery reaches a predetermined value.  Before the battery reaches atmospheric pressure the valve is closed again [1.5].  An example of the current conventional construction of a SLI type VRLA battery is shown in figure 1.1

Figure 1.1: A deconstructed diagram of a convention SLI type VRLA battery. Reproduced by permission of Elsevier Ltd [1.3]

Layers of the positive plates, separators and negative plates seen in figure 1.1 create cells of 2.048 V which are connected with the battery pack to create batteries of various sizes

PbA batteries can generally be classified as:

- Flooded batteries: Require regular maintenance due to water loss.  A higher level of electrolyte is used to flood the cells in order to reduce the need for water top up [1.5]

- Gel VRLA: VLRA battery where the acid electrolyte is greatly reduced and immobilised by hardening it into a gel.  As water is initially lost during charging the gel dries and cracks, allowing for the oxygen recombination cycle to complete. [1.5]

- AGM VRLA: VLRA battery where the reduced acid electrolyte is absorbed into a highly porous separator where the oxygen recombination cycle occurs through the interstices [1.5]

Currently SLI batteries are usually flooded or AGM batteries with a nominal voltage of 12 V for passenger cars and 24 V for heavy duty commercial vehicles in Europe [1.4].

## New demand for electric vehicles

With the current growing interest of governments in reducing CO2 emissions [1.6] EVs have once again become a research subject of high significance.  As transport has major environmental effects, with figures for 2014 showing that it was responsible for 14% of the total anthropogenic greenhouse gases produced [1.7], EU targets for 2021 have been set for a reduction in CO2 emissions of 40% for all new cars [1.8].

Whilst there have been large incentives to encourage people to turn to EVs, such as providing consumer grants of £5,000 for private EV payments [1.9], 69% of driving licence holders in the UK would still not consider buying an EV [1.10].  The main reasons for this lack of interest are the perceived problems surrounding recharging and the distance of travel the capacity of the battery would allow for, as well as high costs [1.10].  A large part of the additional cost to buying an EV over a conventional ICEV is the battery [1.11].  Therefore, if the public opinion of EVs is to improve, it is important to work towards finding a low cost battery technology which is able to meet the needs and expectations of the driver.

## Modern electric vehicle technology

Modern EVs can be split into two main types: those that use only a rechargeable battery known as battery electric vehicles (BEVs) and those, known as hybrid electric vehicles (HEV), which work in conjunction with an internal combustion engine.  The former consists of an electric motor driven by a rechargeable battery, which is usually recharged using mains electricity while the vehicle is stationary.  Ultimately the benefits of this technology depend on the process of electricity generation, with renewable energy resulting in the highest CO2 emission reduction.  The second configuration, the HEV, also consists of an electric motor and rechargeable battery. However, the system is also assisted by an ICEV either to drive or accelerate the vehicle directly or to act as a generator to recharge the battery during use.

To deal with the batteries’ energy depletion during use, all EVs utilise regenerative braking. This is where the electric motor is operated as a generator while the vehicle is decelerating to recharge the battery [1.11].  Here an electric brake is used in conjunction with the conventional mechanical brake (friction braking), both of which are controlled by the usual foot pedal.  The total braking torque is decided by the driver pressing the brake pedal whilst the load to each type of brake is decided by a control strategy.  The electric brakes work by running the electric motor attached to the driving wheels in reverse and using the inertia of the vehicle to turn the motor into a generator [1.12].  The back EMF created by this generator is boosted and acts as a voltage source, redirecting the current to recharge the battery during braking.  The initial braking is completed by the electric brake to recover the maximum energy, with the mechanical brakes initiating if the braking force required is greater than that created by the electric brake.  If the battery is full, and therefore not able to accept the charging current, the electric brake will not be capable of producing a sufficient braking force. This will result in all or most of the braking being completed by the mechanical brakes, therefore limiting the amount of energy regeneration [1.12].   It has been shown that the use of regenerative braking can result in an increase of up to 15% in the driving range of the EV [1.12]. Therefore it is important that the automotive battery is capable of accepting high charging currents during braking periods

Additionally all HEVs employ an automatic stop start function.  This allows the internal combustion engine (ICE) to cut out as soon as the vehicle is stationary, thus relying on the rechargeable battery to maintain the SLI functions until the vehicle moves and the ICE is restarted.  The level of electrification in HEVs can also vary, resulting in a scaled level of cost to the user as well as reduction in local CO2 emissions.

The levels of hybridisation are:

- Micro-hybrid electric vehicles: Uses only stop start function and regenerative braking which is common to all HEVs.  This has the lowest effect on CO2 emissions at 4-7% but also has the lowest cost per % CO2 reduction at €35-100.  Cars using this technology include the Land Rover Freelander 2TD4 and the BMW 320d

- Mild-hybrid electric vehicles: In addition to the minimum HEV functions the electric motor is used for propulsion assist during an initial acceleration from a stop before the ICE takes over.   The CO2 benefit of this vehicle technology is 8-12% with a cost of €200-250 per % CO2 reduction.  Models include the Mercedes Benz S400 BlueHybrid and the Honda Civic.

- Full hybrid electric vehicles: As well as using the electric motor for propulsion assist this HEV type can also rely on the motor for drive power for a limited amount of time.  The CO2 benefit of this vehicle is 15-20% with a cost €200-250 per % CO2 reduction.  Models include the Toyota Prius and the Ford C-Max

- Plug-in hybrid electric vehicles: This vehicle is the most similar to the BEV as the battery is recharged from mains and can therefore utilise the electric motor during driving for extended periods of time.  It is still classed as a hybrid, however, as it relies on the ICE to assist when the battery energy has been depleted.  This system has the best CO2 emission reduction of 20+% but has a higher cost of €300-500 per  % CO2 reduction.  [1.4] Models include the Toyota Prius Plug in Hybrid, the Cevrolet Volt and the Ford C-Max Energi

With the varying levels of electric drivetrain required it follows that the demands of the batteries also varies, however, the battery in all types of EV must be able to cope with high rates of discharge if only for maintaining the SLI functions of the car while the ICE is not in use.

## Automotive battery technology within electric vehicles

### Nickel Metal Hydride

Most of the current best-selling passenger EVs use nickel metal hydride (NiMH) for the rechargeable battery as it has a specific energy nearly double that of lead acid batteries at        30-80 Wh kg-1.  However they also typically cost at least three times more than lead acid batteries, 1.4-2.8 Wh $-1 compared to 5-8 Wh $-1.[1.1].

One of the concerns of NiMH batteries is their high rare earth metal content, with estimates between 2.17-3.5 kg per EV battery pack.  The mining of rare earth metals has potentially similar political and environmental issues to the extraction of petrol, with Europe importing 90% of its supply due to its own limited resources.  Price increases have led to the total cost of rare earth materials in NiMH batteries increasing by 3000% from the end of 2005 to June 2011 [1.14].  This has resulted in most technologies that are thought of as environmentally friendly trying to move away from their dependence on rare earth materials [1.14].

### Lithium ion

Previously it was believed that lithium ion batteries (LIB) would be unobtainable for commercial electric vehicles in the immediate future due to their high costs [1.1].  However with their price falling more rapidly than previously predicted it is likely they could eventually surpass NiMH usage with a number of the best-selling passenger EVs having already adapted the technology [1.15].

The exceedingly higher specific energy of LIBs, 160 Wh kg-1 [1.1] compared to NiMH and PbA, certainly makes the former an attractive option, however with such a rapidly growing technology it is important to consider its waste management and disposal.  With the high likelihood of all EVs using LIBs by 2025 [1.15] predicted estimates of the number of LIBs entering the waste stream annually by 2020 in the US alone range between 30-500 million cells [1.15].  Without appropriate recycling and waste management regulations LIBs pose an environmental risk due to their content of copper, nickel, lithium and carbonaceous materials such as graphite and carbon black.  It is estimated that 42% of the materials, such as aluminium, copper and nickel, which make up the LIBs waste stream are currently recyclable while 48% are made of non-recyclable materials.  The remaining 10% includes lithium and manganese, two high value components that are not currently recovered from redundant batteries [1.15].

With the high predicted projection of EVs containing LIBs and their limited recycling facilities, access to, and the availability of, lithium resources becomes highly important.  While the planetary levels of lithium can easily cope with the increasing demand, when considering current production levels, the amount of available lithium is deemed inadequate for EV growth.  Regardless of production rates, as with rare earth metals, Europe’s own lithium resources are limited with their ownership only accounting for 3% [1.16].

### Lead–acid

As mentioned in section 1.1 all automobiles, regardless of their powertrain technology, still use a PbA battery for their SLI function, despite the high atomic weight of lead resulting in a low specific energy of 30-40 Wh kg-1 [1.13].  Its extensive history has led to a cost-optimised manufacturing technology which, coupled with the low cost of raw materials, makes the PbA battery the most economically attractive option [1.1].  In terms of performance within SLI functions, PbA batteries have a sufficient power density of 180 W kg-1 while their low self-discharge rate of 2-5% per month means they are capable of storing obtained energy for extended periods [1.2].

Unlike NiMH and Li-ion, their well-established recycling systems means that more than 95% of automotive PbA batteries used in the majority of industrial countries are currently recycled.  This leads to 80% of the lead needed for new batteries coming from recycled lead.  This high recycling rate, as well as the low temperatures needed for the metal production, means that PbA batteries have the lowest levels for carbon dioxide emissions, criteria pollutant emissions and has the lowest production energy compared to other battery types [1.17].

## The role of the PbA battery in the future of EVs

Currently the immediate future of PbA batteries is with the micro HEV, where the function of the battery does not deviate significantly from the SLI battery.  It does, however, increase the demand on the battery.  Due to the stop start function the vehicle will likely perform around ten times as many engine cranks during its life time than was previously designed for, making the capture of energy during regenerative braking imperative [1.18].  To maximise this energy recuperation method it is necessary to run the battery in a constant partial state of charge, to ensure it is always able to receive charge, while subjecting it to high rate shallow charge and discharge events.  For HEV applications the optimal range of state of charge is above 30%, to provide enough energy for cold cranking, and below 70%, for efficient energy recuperation.

This mode of operation, known as high rate partial state of charge (HRPSoC), has been found to cause the battery to prematurely fail, consequently raising the running costs for HEVs.  When a PbA battery is discharged at a low rate the normal electrochemical reaction, outlined in section 1.1, will cause lead sulfate crystals of various sizes to be deposited both on the surface and interior of the negative plate [1.19].  Charging the battery at a low rate then dissolves these crystals.  However, as the battery is discharged with high currents, such as those needed for cranking, a progressively concentrated layer of tiny sulfate crystals develops on the surface of the plate, reducing the viable surface area for electron transfer [1.19].  This therefore limits the discharging chemical reaction, that of converting lead and lead dioxide to lead sulfate, to the surface of the plates instead of into the interior.  When the battery is subsequently charged, after a high rate discharge, this sulfate layer limits the utilisation of the active negative material [1.19]; therefore impeding the charging electrochemical reaction outlined in section 1.1. This causes an increase of the lead sulfate, as well as a hydrogen evolution, thus limiting the batteries’ charge acceptance.  This will eventually limit the batteries power to an extent that will reduce the batteries ability to perform engine cranks [1.19].

Various methods for improving the performance of the negative plate during this mode of operation were identified, such as: increasing the electronically conducting surface area, introducing an element to improve charge efficiency, and diminishing the growth of sulfate crystals [1.18].  Carbon quickly became a candidate to help provide these improvements.

Early investigations provided encouraging results with increasing rates of carbon additives resulting in a decrease in sulfate crystal growth rate therefore garnering improvements in cycle life.  This was attributed to the carbon enhancing the overall conductivity of the negative plate by creating new conductive networks of carbon in between sulfate crystals [1.20].  As research expanded into different types and quantities of carbon additives the definitive function of the carbon remained unknown.   However theories have centred around the previously mentioned improved conduction network on the negative plate [1.21], reduction in sulfate crystal growth [1.20], reduction in hydrogen evolution [1.22], increase in acid diffusion within the negative plate interior [1.23] and the supercapacitive effects of carbon black.  Regardless of the precise reason, test results on batteries were encouraging.

## The “UltraBattery”

One of the proposed methods of utilising carbon additives was to provide an effective peak power buffer for the battery cell, in the form of an electric double layer supercapacitor.  This is an electrochemical energy storage device, where the high capacitance of the device allows for a large accumulation of electrostatic charge on the electrode at the electrolyte interface.  As they are characterised by their high power density but limited energy density [1.24] they have emerged as an obvious complement to PbA batteries, effectively acting as a secondary battery.

An early setup consisted of a parallel connection of a supercapacitor and a VRLA cell.  The performance of this combination was tested by subjecting it to 2400 test cycles of a typical mild HEV drive cycle, taken from the Honda Insight, scaled down to represent the demands on a single cell within a pack [1.25].  While the VRLA cell, when unassisted, failed to manage to complete half the cycles, due to currents exceeding 100 A, the addition of a single supercapacitor improved the performance.  This test was completed with three capacitors with values ranging from 100 F to 2500 F where the highest capacitance resulted in the most improvement, allowing this combination to complete all 2400 test cycles [1.25].  It was observed that during high rate events the capacitor protects the battery by accepting and providing the majority of transient current for charging and discharging respectively.  As the peak rate of the current reduces, the battery is effectively charged by the supercapacitor to then act as the bulk long term energy storage device.  Once the current is removed this charging continues until their potentials reach equilibrium [1.25].  However, due to the operational voltages of the two devices differing, an electronic control system is necessary to regulate their individual current flow.  Due to this extra complexity the total cost of this system can be pushed to levels exceeding that even of LIBs [1.25], whilst the combined weight and volume of the PbA cell and supercapacitor would increase to approximately 2.5 and 3.4 times that of the NiMH system.  [1.25]

The Furukawa UltraBattery is an evolution of this technology whereby an asymmetric super capacitor, consisting of a lead dioxide positive plate and a carbon based negative plate, is embedded in the same pack as lead-acid cell, consisting of a lead dioxide positive plate and a sponge lead negative plate [1.27].  This is illustrated in figure 1.2.

Figure 1.1 – The red positive lead oxide electrode is shared by both the lead-acid battery and the supercapacitor while their negative lead and carbon electrodes, shown in gold and silver respectively, are connected in parallel. Reproduced by permission of ECS – The Electrochemical Society [1.28]

As these two devices have the same positive plate composition their negative plates can internally be connected in parallel.  While this connection removes the need for a control system, the difference in operating potential of the devices can result in the battery cell reaching its end cell terminal voltage while the capacitor still holds energy on its plate [1.27].

Regardless of this, tests conducted on the ultra-battery report a significant improvement in performance.  The charge and discharge power improvements were found to be ~50% and ~60% respectively when compared to the control cell without supercapacitor support.  The cycle life also experiences improvements with the UltraBattery completing ~17,000 cycles, consisting of charge and discharge pulses, compared to the ~1,400 cycles completed by the control cell.  This cycle life increased to remaining in a healthy state after 370,000 cycles if the pulse times were shortened and the battery was fully charged after every 25,000 cycles.  [1.26]

## Dynamic charge acceptance

As regenerative braking is standard in all EV and HEV technologies it was identified that a useful characterisation of a battery’s ability to respond to the increasingly demanding electrical systems within modern automobiles is its ability to dynamically accept charge [1.13].  This is important, both for recovery of energy when the EV is braking – to reduce losses in the overall braking system – and also in the charging of the battery, as an increased ability will lead to a faster recharge.  It has been noted that this ability is highly dependent on the battery’s immediate history, meaning that merely cycling a battery through charge / discharge cycles during measurements will not present a true picture of the batteries behaviour.  Due to the nature of automotive use, the battery may have to accept a high current pulse after a rest period, a partial discharge or a partial charge. All of these all have an effect on the amount of charge the battery can accept [1.18].

Figure 1. 3: An example of the battery voltage and current during a drive cycle taken from a Volkswagan Passat 2.0l fitted with a CPT SpeedStart and an Exide 12 V battery pack.  The battery is being charged when the current is negative

This is demonstrated in figure 1.3, which shows the battery voltage and current behaviour during a drive cycle taken. This was taken from a Volkswagen Passat 2.0L fitted with a CPT SpeedStart Integrated Starter Generator and an Exide 12 V battery pack.  The car was driven by a professional driver at the Millbrook proving ground at Bedford and the raw data was provided by ProVector Ltd. When the current is positive the battery is being discharged. It shows a mixture of rest periods lasting ~100 seconds followed by high discharging pulses of ~250 A and relatively smaller recharging pulses of ~50 A.

However it is also difficult to obtain a true picture of the DCA characteristics of the PbA battery in operation as it is inconsistent and hard to predict [1.27].  To combat false charge acceptance rates the idea of DCA was incorporated into automotive battery testing.  In real world terms DCA has been defined as “the amount of charge that is actually charged to the battery during regenerative braking phases of a driving cycle divided by the amount of charge that could be provided by the generator” [1.29].  There is currently no standard test method for producing DCA performance measurements, with car manufacturers incorporating varying tests into their micro-hybrid battery specifications.  To harmonise DCA testing a standardised method is being developed by the European industry.  Therefore efforts have been made in [1.27] to identify a quick testing method that presents a stable DCA result that is representative of real world conditions.  Testing in this thesis is based on methods analysed in this paper as well as those produced by Karden in [1.31].  This work investigates the DCA results of PbA batteries and explores a comparison between normal PbA batteries, carbon loaded PbA batteries, and a novel ‘UltraBattery’ configuration.  This thesis therefore presents the method used within this work for measuring the DCA of PbA batteries, and gives a comparison of DCA for different PbA battery technologies, whilst presenting an insight into the most appropriate PbA battery technology for HEV use.

## Test procedure

Attempts have been made to standardise DCA testing for all battery chemistries to allow comparisons between battery type and size.  An initial testing procedure to be used in this work was devised at the start of the work, and while certain parameters were adjusted and tuned as testing progressed, the general structure, as seen in figure 1.4, remained constant throughout. An outline of this procedure, based on a testing procedure produced by Karden [1.31],   is given below while a flow chart representation is provided in appendix A1.

The test procedure is broken down into five sections, as outlined below:

- The Pre Test Conditioning, where the experimentally verified capacity Cexp (A/Ah) of the battery is measured.

- Discharging micro-cycles, completed when the battery is in one of five different states of charge (SoC).  The battery is discharged to each SoC prior to the micro-cycling.

- Mid-test rest, where the battery is discharged to 0% SoC and rested for a period.

- Charging micro-cycles, completed at five different states of charge.  The battery is charged to each SoC prior to the micro-cycling.

- Post Test, where the battery is discharged as a post-test capacity measurement and then charged back to 100% SoC either for storage of for commencement of the next test.

Pre Test Conditioning

Discharging Microcycles

Charging Microcycles

Post Test

Mid-test Rest Microcycles

Figure 1.4 – Battery current demand, seen in the lower graph, and the battery voltage response, top graph, over a full test cycle where the sections correspond to those outlined above.  Charging currents are negative

The Pre-test Conditioning

This test is used to initially estimate the current SoC of the battery.  It cannot be assumed that the battery is fully charged at the start of the test, so conditioning puts the battery into a known state.

- The battery is initially fully discharged at 25A to its pre-test lower voltage limit, usually 10.5V for a 12V (nominal) battery.  These voltage limits were taken from [1.31]

- The battery is fully charged at a fifth of its nominal capacity, Cnom/5 (A/Ah) for 10 hours to its pre-test higher voltage limit, usually 14.8V for a 12V (nominal) battery.

- The battery is then fully discharged at 25A to its pre-test lower voltage limit again

- The battery is fully charged at Cnom/5 for 10 hours to its pre-test higher voltage limit again, this cycling allows the battery to be exercised before the capacity measurement.

- The battery is fully discharged at Cnom/5 to its pre-test lower voltage limit.  This data is used to find the experimentally measured capacity, Cexp, this capacity is then used for the tests to determine the SoC levels during the tests.

Discharging Microcycles

- The battery is charged at Cexp/5 to first test SoC level.

- The battery is then rested, where a zero current demand is applied to the battery for one hour to establish the “open circuit” voltage (OCV) prior to the tests.

- Micro-cycles, a single micro-cycle being shown in figure 1.5, are then completed 20 times.  The number of micro-cycle as well as the charging rate and time limits were used in accordance with [1.31].  The structure of the individual micro-cycle is:

  - The battery is charged with a high charging current for 10 s. If the battery reaches the upper voltage limit during this time the magnitude of the charging current is reduced to maintain constant voltage charging. The amount of current accepted by the battery is monitored

  - The battery is then rested for 300 seconds

  - The battery is discharged at 1C until the integrated charge delivered during the charging pulse is removed from the battery

  - The battery is rested again for 300 seconds.

Figure 1.5: Current accepted by the battery, seen in the lower graph, and the battery voltage response, seen above, for one microcycle.  Charging currents are negative

- The battery is discharged at Cexp/5 to the next test SoC level.

These three last steps are repeated at each test SoC.

During the microcycles the battery voltage is initially limited at 16 V, however, this level is programmable in the software.  The level of the high charging current applied during the micro-cycle is also modifiable for different sets of tests, if required.  When presented the results are scaled to the capacity of the battery under test, making the tests comparable between batteries of different sizes.

Mid-test rest

In-between the sets of micro-cycle tests carried out whilst discharging the battery, and those carried out whilst charging the battery, a mid-term rest is introduced as part of the test specification.

- After the 20 micro-cycles are completed at the final SoC level, the battery is discharged at Cexp/5 until the battery voltage reaches its lower voltage limit.

- The battery is then rested for 30 minutes before the charging micro-cycle tests are carried out.

Charging MicroCycles

These are the same as the discharging micro-cycle tests, with the battery charging, instead of discharging, to the next SoC level between sets of micro-cycles.

Post Test

- The battery is fully discharged at Cexp/5 to its lower voltage limit.

- The battery is then fully charged at Cexp/5 for 24 hours to its higher voltage limit, to bring it up to 100% SoC and place it in a known condition at the end of the test, either for storage, or subsequent testing.

## Conclusion

This chapter has provided information on lead-acid battery technology and its potential within the electric vehicle industry.  Dynamic charge acceptance was presented as a way of gauging the ability of the battery to operate in high-rate partial-state-of-charge conditions.  The test procedure used for obtaining DCA data for this thesis was then outlined.

The results of the tests on the battery types will be explained in chapter 4.  Having outlined the test procedure for the battery comparisons, the remainder of the thesis will explain the hardware requirements for the tests (Chapter 2), the software written to implement the tests (Chapter 3), and the results of the tests (Chapter 4).  A flow chart representation of the testing sequence as well as a state diagram of the software is included in appendix 1 and appendix 2 respectively.

## References

[1.1]	J.  Larminie and J.  Lowry, Electric Vehicle Technology Explained.  London: Wiley Editorial, 2003. ISBN: 0-470-85163-5

[1.2] 	D.  Pavlov, “Invention and Development of the Lead-Acid Battery” in Lead-Acid Batteries: Science and Technology.  Oxford: Elsevier B.V.  2011. ISBN: 978-0-444-52882-7

[1.3]	D.  Pavlov, “Fundamentals of Lead-Acid Batteries” in Lead-Acid Batteries: Science and Technology.  Oxford: Elsevier B.V.  2011. ISBN:  978-0-444-52882-7

[1.4] 	J.  Garche, P.  T.  Moseley and E.  Karden, “Lead-acid batteries for hybrid electric vehicles and battery electric vehicles” in Advances in Battery Technologies for Electric Vehicles, B.  Scrosati, J.  Garche, W.  Tillmetz, Eds, London: Elsevier Ltd, 2015, pp.  75-101. ISBN: 978-1-78242-377-5

[1.5] 	D.  Linden, T.  B.  Reddy, Handbook of Batteries, 3rd ed. New York: McGraw-Hill, 2002. ISBN 0-07-135978-8

[1.6]	Climate Change Act, 2008, c.27, London, UK: HMSO. Available: http://www.legislation.gov.uk/ukpga/2008/27/contents [Accessed: 28 April 2016]

[1.7]	R.  K.  Pachauri and L.  A.  Meyer, Eds,  Climate Change 2014: Synthesis Report.  Contribution of Working Groups I, II and III to the Fifth Assessment Report of the Intergovernmental Panel on Climate Change, Geneva, Switzerland, IPCC, 2014, pp.  151. Available: http://www.ipcc.ch/report/ar5/syr/ [Accessed 28 April 2016]

[1.8] 	Eur-lex.europa.eu, Regulation (EU) No 333/2014 Of The European Parliament And Of The Council Of 11 March 2014 Amending Regulation (EC) No 443/2009 To Define The Modalities For Reaching The 2020 Target To Reduce CO 2 Emissions From New Passenger Cars.  2014.  Available: http://eur-lex.europa.eu/legal-content/EN/TXT/PDF/?uri=CELEX:32014R0333&from=EN [Accessed: 28 April 2016]

[1.9] 	Office for Low Emission Vehicles, Investing in ultra low emission vehicles in the UK, 2015 to 2020, London, Crown.  Available: https://www.gov.uk/government/uploads/system/uploads/attachment_data/file/307019/ulev-2015-2020.pdf [Accessed: 28 April 2016]

[1.10]	Department for transport, 'Public attitudes towards electric vehicles', London, 2015.  Available: https://www.gov.uk/government/uploads/system/uploads/attachment_data/file/435980/public-attitudes-evehicles.pdf.pdf [Accessed: 28 April 2016]

[1.11] 	O.  van Vliet, A.S.  Brouwer, T.  Kuramochi, M.  van den Broek and A.  Faaij, “Energy use, cost and CO2”, J.  Power Sources, 196, pp.  2298-2310, 2011. Available: doi:10.1016/j.jpowsour.2010.09.119

[1.12] 	X. Nian, F. Peng, H. Zhang, “Regenerative braking system of electric vehicle driven by brushless DC motor”, IEEE Trans. Ind. Electron,  vol. 61, pp. 5798-5808, 2014. Available: doi:10.1109/TIE.2014.2300059

[1.13]	E.  Karden, P.  Shinn, P.  Bostock, J.  Cunningham, E.  Schoultz and D.  Kok, “Requirements for future automotive batteries – a snapshot”, J.  Power Sources, 144, pp.  505-512, 2005. Available: doi:10.1016/j.jpowsour.2004.11.007

[1.14] 	E.  Alonso, A.M.  Sherman, T.J.  Wallington, M.P.Everson, F.R.  Field, R.  Roth and R.E.  Kirchain, “Evaluating Rare Earth Element Availability: A Case with Revolutionary Demand from Clean Technologies”, Environ.  Sci.  Technol, 46 (6), pp.  3406–3414, 2012. Available: http://pubs.acs.org/doi/abs/10.1021/es203518d

[1.15] 	K.  Richa, C.W.  Babbitt, G.  Gaustad and X.  Wang, “A future perspective on lithium-ion battery waste flows from electric vehicles”, Resources, Conservation and Recycling, 83, pp.  63-76, 2014. Available: doi:10.1016/j.resconrec.2013.11.008

[1.16] 	C.  Grosjean, P.H.  Miranda, M.  Perrin and P.  Poggi, “Assessment of world lithium resources and consequences of their geographic distribution on the expected development of the electric vehicle industry”, Renewable and Sustainable Energy Reviews, 16, pp.  1735-1744, 2012. Available: doi:10.1016/j.rser.2011.11.023

[1.17]	 J.L.  Sullivan and L.  Gaines, “A review of battery life cycle analysis: state of knowledge and critical needs” 2010 Available: https://anl.app.box.com/s/mcw0rl7a55gok9imea1hexde3wgo9fjk [Accessed 28 April 2016]

[1.18] 	P.T.  Moseley, D.A.J.  Rand and B.  Monahoy, “Designing lead acid batteries to meet energy and power requirements of future automobiles”, J.  Power Sources, 219 pp.  75-79, 2012. doi:10.1016/j.jpowsour.2012.07.040

[1.19] 	L.T.  Lam, N.P.  Haigh, C.G.  Phyland and A.J.  Urban, “Failure mode of valve-regulated lead-acid batteries under high-rate partial-state-of-charge operation”, J.  Power Sources, 133, pp.  126–134, 2004. Available: doi:10.1016/j.jpowsour.2003.11.048

[1.20] 	M.  Shiomi, T.  Funato, K.  Nakamura, K.  Takahashi and M.  Tsubota, “Effects of carbon in negative plates on cycle-life performance of valve-regulated lead/acid batteries”, J.  Power Sources, 64, pp.  147-152, 1997. Available: doi:10.1016/S0378-7753(96)02515-3

[1.21]	K.  Nakamura, M.  Shiomi, K.  Takahashi and M.  Tsubota, “Failure modes of valve-regulated lead/acid batteries”, J.  Power Sources, 59, pp.  153, 1996. Available: doi:10.1016/j.jpowsour.2008.08.059

[1.22] 	P.T.  Moseley, “Consequences of including carbon in the negative plates of valve-regulated-Lead-Acid batteries exposed to high-rate partial-state-of-charge operation”, J.  Power Sources, 191, pp.  134-138, 2009. Available: doi:10.1016/j.jpowsour.2008.08.084

[1.23] 	P.T.  Moseley, R.F.  Nelson and A.F.  Hollenkamp, “The role of carbon in valve-regulated lead–acid battery technology”, J.  Power Sources, 157, pp.  3-10, 2006. Available: doi:10.1016/j.jpowsour.2006.02.031

[1.24] 	Li Li Zhang and X.  S.  Zhao, “Carbon-based materials as supercapacitor electrodes”,  Chem.  Soc.  Rev., 38, pp.  2520-2531, 2009. doi:10.1039/B813846J

[1.25] 	P.  Bentley, D.A.  Stone and N.  Schofield, “The parallel combination of a VRLA cell and supercapacitor for use as a hybrid vehicle peak power buffer”, J.  Power Sources, 147, pp.  288-294, 2005. Available: doi:10.1016/j.jpowsour.2005.01.016

[1.26] 	L. T.  Lam, R.  Louey, “Development of ultra-battery for hybrid-electric vehicle applications”, J.  Power Sources, 158, pp.  1140-1148, 2006. Available: doi:10.1016/j.jpowsour.2006.03.022

[1.27]	H.  Budde-Meiwes, D.  Schulte, J.  Kowal, D.U.  Sauer, R.  Hecke, E.  Karden, “Dynamic charge acceptance of lead–acid batteries: Comparison of methods for conditioning and testing”,  J.  Power Sources, 207, pp.  30-36, 2007. Available: doi:10.1016/j.jpowsour.2011.12.045

[1.28] 	J.  Furukawa, T.  Takada, T.Mangahara, L.  T.  Lam, “Development of flooded-type UltraBattery for Micro-HEV applications” in Large Scale Energy Storage Systems.  C.  Wei, W.  Cai, A.  Negishi, K.  Ota, Eds. Pennington NJ: The Elctrochemical Society.  2009. ISBN: 978-1-60768-065-9

[1.29]	J.  Kowel, D.  Schulte, D.U.  Sauer and E.  Karden, “Simulation of the current distribution in lead-acid batteries to investigate the dynamic charge acceptance in flooded SLI batteries”, J.  Power Sources, 191, pp.  42-50, 200. Available: doi:10.1016/j.jpowsour.2008.12.016

[1.30] 	A.J.  Fairweather, D.A.  Stone, M.  Foster, “Evaluation of UltraBattery performance in comparison with a battery – supercapacitor parallel network”, J.  Power Sources, 226, pp.  191-201, 2013. Available: doi:10.1016/j.jpowsour.2012.10.095

[1.31]	E.  Karden, F.  Jöris, H.  Budde-Meiwes and D.U.  Sauer, “Test methods for dynamic charge acceptance (DCA) of microhybrid starter batteries” presented at 13ELBC European Lead Battery Conference, Paris, 2012

# Design of test rig setup hardware

Having discussed the testing of batteries in chapter 1, this chapter will detail the development of a hardware test rig capable of implementing  charge / discharge cycles, as well as carrying out tests to determine the dynamic charge acceptance of the test batteries.  It will also present the utilisation of a temperature controlled chamber to house the batteries whilst under test.  The control software designed for the test rig will then be described in chapter 3.  Initially this chapter will outline the requirements of the test rig set up needed to complete the tests before explaining the components of the setup.

## Test facility design requirements

To ensure the hardware is flexible, the test rig needed to be capable of applying (and accepting) high currents to (and from) the battery, whilst monitoring the battery voltage and current.  The value of the applied current needed to be adjustable during the testing, as the current applied during any test cycle varies, depending on the individual test battery capacities at each test temperature.

It was decided that the test facility was to be capable of supplying a current of at least 5 times the ampere-hour capacity of batteries under test (5C).  As the initial batteries proposed for this study, a Furukawa FTZ12–HEV and a Yuasa YTX9–BS, have nominal capacities (Cnom) of 8.5 Ah and 8.4 Ah respectively, the test rig was to have a current rating in excess of ±45 A.  However, to ensure significant overhead on the facility, and to ensure larger batteries such as the 6V 24Ah Exide batteries, could be tested a rating of ±100 A was chosen.

As the current applied to the battery during the testing was related to the experimentally measured capacity of the battery, Cexp, and as this is a function of the battery temperature [2.1], it also was important to keep the battery at a constant and known temperature for the duration of the tests.  The two approaches commonly taken are to use a water bath for the battery, which is excellent at controlling the test temperatures but is difficult to construct, and a temperature controlled chamber where only the ambient temperature is controlled around the test battery.  A very tight temperature control, as may be achieved with a water bath, may not be indicative of a typical battery operating environment within a vehicle. As the battery is usually operated ‘air-cooled’, the simpler temperature controlled chamber was chosen as a compromise, to remove variations in battery performance caused by changes in laboratory temperature without necessitating a fluid filled cooling system.

It was also important that the battery was not damaged during testing.  The upper and lower voltage limits were set to 14.8 V and 10.5 V respectively and used for all low rate charging and discharging cycles to ensure that either overcharge or overdischarge could not lead to damage through extensive gassing or sulfation of the electrodes.  These were taken from limits used by Karden for AGM PbA batteries in previous tests [2.2].  However, during short periods of less than 10 seconds it was thought that the battery could withstand a short-term overvoltage without leading to significant damage.  This decision was made based on the fact that AGM VRLA batteries have an inherent ability to re-combine any gases produced in such a time. Therefore the transient upper voltage limit was raised to 16 V, as it is in [2.2], for short term charging spikes during testing.  This meant that it was necessary to be able to apply adjustable upper and lower voltage limits in the test rig.

It is assumed at this stage that the test periods will be of the order of several hours, possibly days, and therefore long term stable testing and data recording will be required from the rig.

The requirements of the test rig are listed below and shown, with values, in table 2.1:

- Apply high currents of various values throughout the tests, both positive (discharging) and negative (charging).

- Maintain a constant and known temperature for the battery.

- Record battery voltage and current.  The sample frequency of 10Hz was chosen as a compromise between sampling speed of the system and the large amount of data which will be generated when the test is run continuously for days.

- Apply adjustable upper and lower voltage limits to the battery during the testing.

| Rig requirement | Value |
| --- | --- |
| Max battery voltage under test | 16 V |
| Minimum battery voltage under test | 10.5 V |
| Maximum test current magnitude | 100 A |
| Sample frequency | 10 Hz |

Table 2.  1 – The main specific parameter requirements of the test rig are given as well as the required values

## Test facility implementation.

The list of requirements above led to the final design of the test facility, shown in figure 2.1, composed of a temperature controlled chamber, based around a commercially available freezer with an inbuilt heater and temperature controller, as well as a custom built test rig which is controlled by a PC.  Throughout testing, the battery under test is kept within the chamber to keep it at a constant temperature.  The custom built test rig is capable of controlling currents up to around 100 A whilst monitoring the battery voltage and the current accepted by the battery, based on a previous design by Prof Stone.  The current demand and the upper and lower voltage limits is set using National Instruments (NI) DAQmx interfaces, and controlled using a PC.

Figure 2.1 – Test rig, seen on the right and temperature controlled chamber, to the left.  The battery is contained within the controller throughout testing and connected to the rig via the cables seen on the front panel.

## Test Rig

A system diagram of the test rig is shown in figure 2.2.  The main power supply for the system is the dc link voltage, provided by two 12 V batteries, to allow for charging and discharging the test battery. A secondary power supply provides power for the control board and the current limiter within the rig.  It also contains two NI DAQmx interfaces, the USB6212 and the USB6009.  The first device outputs the current demand to the hardware whilst inputting the battery current and voltage for data acquisition. The second device provides the upper and lower voltage limits for the test battery and allows them to be set dynamically during the test.  To achieve the latter the limiter circuit uses the values from the USB6009, compares them with the feedback of the battery voltage, and limits the battery current demand accordingly if the voltage limits are being exceeded at that current demand level.  This is explained in more detail in section 2.3.4.  If the battery voltage is within the desired limits, the current demand is unmodified and passed to the control board.  To apply the desired current to the battery the control board is used to compare the instantaneous current demand with the feedback of the battery current, which is given by the current transformer.  The control board then controls the battery current via the push-pull power stage.  This is explained in more detail in section 2.3.2

Figure 2.2 – Schematic diagram of the test rig showing the main components of the rig and how they interact with each other.  Both PSUs are powered by mains electricity and the DAQmx devices are used to interface with the control PC

### Power Supply (DC Link)

The power supply to the system dc link is external to the design of the rig, and is shown in figure 2.2 as DC Link Batteries, above the push-pull power stage.  This power supply needs to be able to supply the full current for the test rig (>100 A), therefore two 12 V batteries in series are used for the dc link, giving a nominal dc link voltage of 24 V.  With a maximum voltage on the test battery of 16 V, and the fully discharged dc link batteries’ lower voltage limit of 10.5 V each (21 V total), the worst case is 4 V dropped across the push-pull power stage in the test rig at maximum current.  Under these conditions, the limiting maximum impedance of the switching devices is 4/100 = 40 mΩ.  The dc link batteries need to be capable of supplying the full current, and are kept float charged by a 30 A, variable voltage laboratory power supply which is connected whilst the test rig is operational, and is set to float charge the dc link batteries at 2 x 13.8 = 27.6 V.  The dc link voltage can drop when full current is delivered however this is only applied during microcycles and will therefore only last 10 s.  The dc link batteries used in the rig are 2 x 100 Ah, 12 V, NorthStar stationary storage batteries connected in series, which were available in the laboratory.

### Push-Pull power stage

The push pull power stage, shown as Pushpull Stage in figure 2.2 and shown in detail as part of figure 2.4, is required to control the current flow into and out of the battery under test.  This power stage is based on n-channel MOSFETS, and is controlled by the control board described in section 2.3.3.  The MOSFETS, seen as Q3 and Q4 in figure 2.4, effectively form a bridge leg configuration, but are operated in a linear mode.  The control board converts the n-channel ‘top-leg’ devices to behave as pseudo p-channel devices giving a topology which is a standard class B linear amplifier, given that there is zero bias current flowing in the quiescent condition, and the linearity of the output is not a design criterion.  Feedback of the current to the battery under test is done via a LEM 125 A closed loop Hall Effect current transducer.  The output of the current transducer is fed into the control board to provide closed loop control of the output current as described below.

As the MOSFETs in the power stage are to carry 100 A maximum, and have a link voltage of <30 V, low voltage MOSFET devices would seem ideal.  However, as the system is effectively a linear amplifier, there is a high power dissipation within the devices.  The maximum power dissipated in the top MOSFET (Q3) would be when the dc link voltage is a maximum, and the battery voltage is a minimum, giving 27.6-10.5 V across the MOSFET = 17.1 V.  In this condition, at maximum current, the MOSFET would be expected to dissipate 100*17.1 = 1710 W in the device.  The device package with the highest power dissipation ability is the ISOTOP package, and a power limit is usually 300 W for this package, therefore ~1800/300 = 6 devices are required in parallel for Q3, assuming perfect sharing.  For the lower MOSFET (Q4), the maximum expected power dissipation would occur at full battery voltage (~16 V) and full current.  This is 16*100 = 1.6 kW, therefore around 6 devices in parallel are required in the bottom switch position (Q4).

These are worst case scenarios for the test rig, as the maximum current expected to be seen in the tests is 45 A, but to ensure the rig is flexible and able to cope with future tests, the higher ratings are assumed.  Due to the high power dissipation of the switching devices, the cooling of the parallel branches requires a forced air cooled heatsink. To allow the device case to reach 80oC, to allow for higher temperature at the silicon, with a 20oC ambient temperature there is 60oC temperature rise allowed on the heatsink.  This allows headroom for the silicon temperature to rise above the device case temperature.  Usually the silicon die should be kept below 150°C, hence there is a headroom of 70oC for the die temperature rise.  This gives a maximum thermal resistance of 60/1800 = 0.033oC / W for the heatsink under worst case conditions.  This is quite a low thermal resistance, hence the requirement for forced air cooling.  The heatsink chosen was a 0.48oC / W device, where 2 could be mounted together to form a cooling channel, with a fan at each end and the MOSFET devices split between the two heatsinks.  A thermal switch was also mounted on the heatsinks, and used to shut down the system if the heatsink gets too hot.

A close-up of some of the devices mounted on the heatsink arrangement can be seen in figure 2.3.  The resistors R15 and R7 in figure 2.4 are specific to each device, and therefore are made up from 6 resistors, one in series with each parallel MOSFET device.  These resistors provide feedback of the current in each device to the drive by lowering the effective gate-source voltage of the device as the drain current increases.  This gives rise to current sharing between the MOSFET devices if one has an increase in current relative to the others, the gate-source voltage of that device is lowered relative to the others, hence the current is reduced in that device.

Figure 2.3 – The interior of the test rig including a fan-cooled heatsink and ISOTOP power devices.

The MOSFETs used in the test rig are IXYS 60V 100A devices, the main criterion for operation is the power dissipation capability of the package, and not the device silicon ratings as it is operated exclusively in a linear (high dissipation) mode.

### Control board

The purpose of the control board, as mentioned in the previous section, is to control the current flow to and from the test battery.  The dc link voltage, shown as DC Link Batteries in figure 2.2, is provided by the two 12 V batteries to deliver current to the output stage to charge the test battery when a negative (charging) current is demanded.  A positive current demand leads to no current being taken from the dc link batteries, and the test battery being discharged through the push-pull power stage.

The operation of the power stage, shown in figure 2.4, can be illustrated by considering the differential amplifier on the control board (U1 in figure 2.4) which compares the instantaneous current demand with the current feedback from the test battery, provided by a 1:1000 current transformer.  A more negative value on the current demand input will cause the output of the differential amplifier, U1, to fall, therefore reducing the amount that the transistor, Q1, is turned on.  This, in turn, will turn on MOSFET Q3 proportionally and the battery will charge from the link voltage.  A positive current demand will lead to Q4 turning on proportionally with current demand causing the battery to discharge.

Figure 2.4 – Circuit diagram of the control board

To allow for the high currents needed to charge and discharge the test battery, the push pull stage of Q3 and Q4 as well as the resistor bank, R15 and R7, is repeated in parallel giving six parallel branches.  The resistors R15 and R7 give some direct negative feedback of the current in the output power device to the gate drive of each device, and ensure the branches operate in parallel, sharing the battery current.

The parallel push-pull output stages are mounted on a large heat sink with a cooling fan to ensure good heat dissipation and close thermal coupling of the devices.  The rest of the control circuit is contained within the control board, where low currents and low dissipation do not present a problem.  The control board is powered by the secondary power supply, as lower voltages are required by the control electronics, and this provides power supply decoupling between the control and power circuits.

### Programmable voltage limiter board

As the upper and lower voltage limits were required to change at various points during a test cycle, a variable voltage limiter circuit was needed. This ensured that the battery was protected from overvoltage during longer low rate charge cycles whilst allowing higher voltages during high rate microcycles.  A linear current limiter was designed by Dr James Green so that the current would limit if the voltage moved out of the acceptable range of the batteries’ safe operation.

Figure 2.5 – Circuit diagram of the programmable voltage limiter board

This circuit, shown in figure 2.5, was based around a series of operational amplifiers, and compares the instantaneous battery voltage with the reference voltage values set as the upper and lower voltage limits. This is set by the software and via the DAQmx routine in the LabVIEW (Laboratory Virtual Instrument Engineering Workbench) control software and a ‘USB6009’ USB coupled ADC / DAC hardware module.

The inputs to this circuit are the battery current demand, actual battery voltage, and the current upper and lower voltage limit values outputted from the software via the USB6009.  The circuit shown in figure 2.5 compares the battery voltage limit with the upper and lower voltage limits and controls the current demand, Id, applied to the power stage and hence to the battery.

As the output range of the USB6009 is 0 to 5 V, the battery voltage input is dropped across potential dividers consisting of R1/R2 and R5/R6 for upper and lower voltage limits respectively.  For the upper voltage limit, this scaled battery voltage is then compared, using the differential amplifier, U1, with the upper voltage limit value set by the USB6009 and the LabVIEW control software.  If the battery voltage is found to be greater than the upper voltage limit, transistor Q2 is turned on and the current demand is reduced.  The same process occurs for the lower voltage limit. When the battery voltage potential divided by R5 and R6, is less than the limit, transistor Q1 opens and the current is limited.  If the battery voltage is within the voltage range of the limiter, neither Q1 or Q2 opens and the current demand is applied to the battery unmodified.

### Temperature controlled chamber.

As the performance of the battery changes with the operating temperature of the battery, the temperature was kept constant throughout each of the tests.  This was achieved using a commercially available freezer which was used as the basis of a temperature controlled chamber, an example of which is shown in figure 2.6.

A commercial PID controller was used, shown in the box on top of the freezer in figure 2.6, to control both the freezer on/off and an internal heater and fan, shown in the bottom of the open freezer, figure 2.6.  If the temperature of the freezer rises above a set point (25oC shown in figure 2.6 on the display), an alarm condition is triggered within the controller and the freezer is turned on to lower the temperature.

Figure 2.6 – Temperature controlled chamber consisting of a commercially available freezer and an internal heater and fan.  These are controlled by a PID controller to set the temperature with a 1 oC margin

The heater control is more analogue and not on/off, as with the freezer, therefore the temperature can be controlled to within 1oC of the actual temperature set-point, and maintained when in use by this arrangement.  This gives a controlled ambient temperature for the battery, and therefore allows a more consistent test temperature than could be achieved in the laboratory alone, giving repeatability between tests.  The temperature within the chamber can be controlled from -10oC to 50oC, allowing a reasonable range of practical temperatures for battery operation to be obtained.

## Control Interface System

The USB6009 and USB6212 devices are USB data acquisition systems, capable of interfacing to the LabVIEW system.  The USB6009 gives a 14-bit (differential) ADC input at up to 48kS/s, and 12-bit DAC capability for the hardware interfacing while the USB6212 gives a 14-bit (differential) ADC input at up to 400kS/s, and 16-bit DAC capability for the hardware interfacing.

The control of the test rig is carried out using a LabVIEW based graphical control interface.  The NI DAQ systems were designed to be interfaced to LabVIEW, and therefore this was the most easily implemented approach to the testing / test rig control.  The LabVIEW system is running on a host PC, with the DAQ devices providing the software / hardware interface.

This chapter has described the hardware for the test rig setup giving details of the main rig components as well as cooling chamber and the interface system with the control PC.  The following chapter will describe the LabVIEW software written to control the system, and facilitate testing of the sample batteries.

## References

[2.1]	R.  Hutchinson, “Temperature effects on sealed lead acid batteries and charging techniques to prolong cycle life”, U.S.A, U.S Department of Commerce, 2004. Available: http://prod.sandia.gov/techlib/access-control.cgi/2004/043149.pdf Last visisted: [28 April 2016]

[2.2] 	E.  Karden, F.  Jöris, H.  Budde-Meiwes and D.U.  Sauer, “Test methods for dynamic charge acceptance (DCA) of microhybrid starter batteries” presented at 13ELBC European Lead Battery Conference, Paris, 2012

# Test procedure software

In the previous chapter the full test rig setup requirements were outlined and details were given as to how the design of the rig met these requirements.  This chapter will focus on the software designed to manage the testing sequence.  An overview is given of how LabVIEW programming was used to create the control software with details of its main functions and how it was designed to interface with the hardware.  Presented initially is a description of how the test procedure, outlined in chapter 1, was divided in terms of software tasks.

## Overview of LabVIEW software

In order for the hardware described in the previous chapter to complete the test outlined in chapter 1 a control program was written in LabVIEW (Laboratory Virtual Instrument Engineering Workbench), a programming environment which allows the user to create programs using a graphical language referred to as “G”.  The software was based on some previously available software for test rig control developed by Dr James Green, with modifications carried out by myself to include rig-specific issues.  Each program created using LabVIEW is called a virtual instrument, VI, and consists of a front panel, used to interface with the user, and a block diagram which contains all of the code [3.1].

The software communicates with the hardware using two NI DAQmx devices, the USB6009 and the USB6212, which allows the program to control the relay system and the current demand, as described in chapter 2, as well as enabling it to record the battery’s voltage and current.

To create the test program, the requirements for the software were broken down into four main tasks, or ‘slave’ VIs:

- Checking the state of charge (SoC) of the battery.  (Checking SoC VI)

- Charging or discharging the battery, either to a new SoC or fully.  (Charger VI)

- Allowing the battery to rest by opening the relays connecting the battery to the rig, and allowing the battery to drift to its open circuit voltage (OCV).  (Rest VI)

- Micro-cycling the battery as described in chapter 1 (Microcycler VI)

These slaves can be run independently, however during testing they are run in conjunction with, and are controlled by, a “master” VI.  The master VI does not complete any of the data acquisition, but instead monitors which part of the overall test the program is in at a given time, and therefore which slave VI needs to be opened and what tasks need to be completed.  Once the relevant slave VI is opened the master establishes a message queue connection with the slave, as a means of communication, and sends it the parameters needed for its specific tasks.

This data can be obtained by the master VI in one of three ways.  If the parameter is variable for different tests, such as current charging rates, it is uploaded to the master at the beginning of each test, using a configuration file, and stored in a subVI called the shifter.  However, if the parameter is constant for all tests, such as the sampling rate, then this is written into the master VI.  Finally, some parameters depend on data obtained during testing which the master updates to the shifter throughout the test.

Once it has received the relevant parameters from the master VI, the slave VI establishes communication with the DAQmx devices.  As the devices are only capable of outputting and inputting ±10 V an individual scale is applied to each port of the device, using the program ‘Measurement and Automation Explorer’ within LabVIEW.  The slave VI is then able to apply a proportional voltage to the appropriate port of the DAQmx devices which can control the current applied to the test batteries, as well as switch the relays, as explained in chapter 2.  The battery current and voltage are then read from the appropriate input port of the device and are sent back to the master using the queue previously established.  All slave VIs interact with the DAQmx devices using the same code, which is explained in section 3.7, while the master VI has no direct communication with the devices.

An outline of the Master and the four slave VIs is given below, while the full state diagrams are included in appendix A2.

## Master VI

The master VI does not complete any of the actual testing routines but acts rather as a manager, overseeing the running of the slave VIs as and when required.  The main tasks of the manager are opening, running and closing slave VIs as well as dealing with the data that they have acquired.  Before the test is run the user is required to enter three parameters that are essential for test completion.  For the software to be able to save the data coherently a root path to an assigned folder must be entered including a root name.  Throughout the testing sequence separate files are created for all stages using the same root name with an individual number. These are stored in the NI technical data management streaming (TDMS) file format.  As well as this, the user must enter the root path to the configuration file which contains all the data for variable parameters needed for running the tests.  Finally a data path to a log folder is required, in which to save any logging data files; again, with a text file name that will be common to all log files saved.

The configuration file shown in figure 3.1 (a) is a text file consisting of all of the variable parameters of a test, for example upper and lower voltage limits, lengths of tasks, current demands etc.  During start up the values are taken from this file and stored in the shifter subVI seen in figure 3.1 (b).  This allows the master to access the data needed to be sent to the slave VIs as well as store data retrieved from the slaves, often setting them as new parameters for future tasks.  This means that the test parameters can be changed, by changing values in the config file without having to change any of the program’s code.

| a. | b. |
| --- | --- |

Figure 3.1 – (a) A section of an example of the configuration file used by the user to determine the parameters of the test.  (b) A section of the shifter used by the master used throughout the test.  The data from the config file is entered into the shifter at the beginning of the test while other data is updated during the test

This allows the master to access the data needed to be sent to the slave VIs as well as store data retrieved from the slaves; often setting them as new parameters for future tasks.  This means that the test parameters can be altered, by changing values in the config file without having to change any of the program’s code.

Each time a slave VI is opened the master VI determines what specific task it needs to complete based on the current position of the test, an example of which is seen in figure 3.2.  The parameters for that task are then pulled from the shifter and sent to the Slave VI, as seen in figure 3.3.  This data is stored in the shifter of the slave VI for the VI to access when needed

Figure 3.2 – The master VI determines the parameters to send to the Charger VI.  The Test Charger Discharger Pre-Amble array, seen in pink, stores the names of the pre-test stages and the Test Charger Discharger Pre-Amble Counter, seen in blue, is used to shift through the stages.  The SubVI, seen in figure 3.3, containing the parameters for that stage is then opened.

Figure 3.3 – The subVI holds the parameters to send to the Charger VI.  The shifter is accessed to retrieve the parameters, seen in orange, which are sent with a corresponding string message, seen in pink, to the Charger VI.  The bottom six orange values are constants for the tests and cannot be changed using the configuration file.

Each time a slave VI is opened the master VI determines what specific task it needs to complete based on the current position of the test, an example of which is seen in figure 3.2.

The parameters for that task are then pulled from the shifter and sent to the Slave VI, as seen in figure 3.3.  This data is stored in the shifter of the slave VI for the VI to access when needed

During the running of the slave VI, data is constantly being sent back to the master VI partly to be displayed on the front panel, as seen in figure 3.4, and also to provide the master with data needed for the rest of the test.

Figure 3.4 – The front panel of the master VI.  The TDMS data path root, test config file and log file name are entered by the user while all other values are updated during the test

Once the slave VI has finished running a “Finished” message is sent back to the master VI which will cause the master VI retrieve any last data before closing the slave VI.

Having explained the master VI a description of what each slave VI does is given below.

## Checking SoC VI

The Checking SoC VI is only run once, at the beginning of the test, to establish the initial SoC of the battery.  After the master VI has opened the slave VI, and communication between the two has been established, the master VI sends the general data it has stored about the battery to the slave VI.  This includes the nominal capacity of the battery as well as the voltage when it is at 0% SoC and 100% SoC.  The slave VI also ensures that the relays are closed and reads the OCV of the battery, as explained in section 3.7.  These values are then entered into equation (3.1), in the way shown in figure 3.5, in order to find the SoC of the battery as both a percentage and in Ah.  These values are entered into a TDMS file as well as being sent back to the master VI.

| SoC%=OCV-SoC(V0%SoC0%)V100%SoCSoC100%-V0%SoCSoC(0%) ×100 | (3.1) |
| --- | --- |

If the battery has been over or under charged the SoC is recorded as its 100% or 0% respectively, again as both a percentage and in Ah.

Figure 3.5 – The “Calculate SoC” action of the Checking SoC VI.  This action uses a sub VI to calculate the SoC of the battery.

## Charger VI

This VI is called at various points during testing, either fully charging and discharging during the preamble and post–test or partially charging to move between test SoCs.  Each time the charger VI is opened it will apply the required current demand, as explained in section 3.7, to the battery to partially or fully charge or discharge it.  As explained in section 3.2 the parameters, such as current demand and how much charge to add to or remove from the battery, are sent from the master VI to the slave VI.  Once the parameters have been set, the slave VI opens the relays and applies the desired current to the battery until its present task is finished.

Early on during testing this slave VI is used to determine the experimentally verified capacity, Cexp, of the battery, which is then used throughout the test.  This is done during the preamble where the battery is subjected to 3 charge/discharge cycles, as explained in chapter 1, while the current accepted by the battery is monitored.  Whilst the Charger VI is running, integrated charge is repeatedly calculated, as seen in figures 3.6 (a) and (b), by accessing the instantaneous current and integrating it with the current of the battery the previous time this calculation was made.   This value of integrated charge is added to a running total and is sent back to the master VI, to be stored in the master’s shifter, and used to update the front panel of the master VI.

Figure 3.6 –  (a)  The battery data, which includes the current accepted by the battery, is fed into the subVI seen in figure 3.6 (b) This is used, with prior battery data as well as a counter for integrated charge, to calculate the total integrated charge

Figure 3.6 – (b) This subVI accesses the current from the battery data as well as the current value from the last time this action was completed.  It then calculates the integrated charge for that period of time and adds it to a running total of integrated charge

While the Charger VI is running, integrated charge is repeatedly calculated, as seen in figures 3.6 (a) and (b), by accessing the instantaneous current and integrating it with the current of the battery the previous time this calculation was made.  This value of integrated charge is added to a running total and is sent back to the master VI, to be stored in the master’s shifter, and used to update the front panel of the master VI.

The final value of the final discharge is used as the Cexp for that test and is later accessed by the master to calculate the amount of charge needed to move to the required SoC, as well as the amount of current demand to be applied to the battery during the microcycles

There are four ways for the charger VI to come to a finish, depending on which task it is completing, all of which are seen in figures 3.7 and 3.8.  All four methods will trigger the same reaction: the slave VI is told to stop and the master VI is sent a message informing it that the slave has finished.

Figure 3.7 –  The amount of charge that has been added to or removed from the battery, the amount of charge required to integrate and the lower cut off current and voltage values, seen in orange, are used with the battery data, seen in brown, to determine if the charger VI has finished its task.

These finish triggers are:

- The VI has been running for at least 60 seconds and amount of charge added to or removed from the battery is equal to the amount that the master has requested.

- The VI has been running for 60 seconds and the amount of current accepted by the battery falls below the lower current limit that has been set by the master

- A lower voltage limit has been set by the master VI and the battery voltage falls below this value

- The VI has been running for the amount of time set by the master.

The current task that the VI is completing will determine the finish condition as follows:

- When the slave VI is moving between SoCs then no current cutoff limits are set, voltage limits are set as those for 0% SoC and 100%, to ensure no overcharge or overdischarge.  The time limit set by the master is sufficiently large enough to allow for the required charge to be added or removed. The VI will stop once the required charge has been  added or removed from the battery.

- If the battery is being fully charged then no current or voltage limits are set and the amount of charge to integrate is set above that which the battery is capable of.  This will allow the battery to be fully charged for the required time, while the limiter reduces the current once the battery reaches its upper voltage limit to allow for constant voltage charging, as explained in chapter 2. The VI will stop once the time limit set by the master has been met or the current applied to the battery falls below the level set by the master.

- If the battery is being fully discharged then a lower voltage limit is set by the master whilst time and integrated charge limits are set high enough to allow the battery to reach this lower voltage, where the slave VI will then stop.

Figure 3.7 –  The amount of charge that has been added to or removed from the battery, the amount of charge required to integrate and the lower cut off current and voltage values, seen in orange, are used with the battery data, seen in brown, to determine if the charger VI has finished its task.

Figure 3.8 – The last possible end time is set at the beginning of charge or discharge using the current time and time limit sent from the master.  To check the end time this value is compared with the current time to determine if the VI’s task is finished.  The green sub VI subtracts the current time from the last possible end time to generate the time remaining which is then sent back to the master VI

## Rest VI

The Rest VI is used, before a set of microcycles, to establish the OCV of the battery at each test SoC as well as allowing the battery to rest at the mid-point of the test.  During the running of this VI the relays are opened, by the method described in section 3.7, and the battery voltage is allowed to drift for a desired rest time.  This duration is set by the configuration file and is sent to the slave VI from the master.  The VI finishes once it has identified that this time has elapsed, as seen in figure 3.9

Figure 3.9 – The VI uses a subV to determine if the current time is equal to the end time.  If not the time remaining is calculated, stored in the shifter of the slave VI, and then sent back to the master where it will be displayed on the front panel.  Once the time has elapsed the slave VI is told to stop and a message to say that the slave is finished is sent back to the master

## Microcycle VI

The microcycler VI is called once the battery has moved to a set SoC, and the OCV has been established.  It runs once at each set SoC where it iterates through the desired number of microcycles.  As explained in Chapter 1, one microcycle involves applying a high charging current for a short period of time and then allowing the battery to rest for a short amount of time.  The battery is then discharged to remove the charge added to the battery during the charging period and the battery is rested for the same amount of time again.  Unlike the resting period before each set of microcycles, where the relays are opened to achieve zero current, the relays remain closed throughout the microcycles and a current demand of zero is applied to the battery during rest periods.  The method for this is explained in section 3.7

The method for this is explained in section 3.7

The number of microcycles, as well as the current demand and the charging, discharging, and rest times, are set using the configuration file and sent to the slave by the master during the slave VIs start up.  For the charging pulse the current demand is a multiple of the experimentally verified battery capacity found at the beginning of the test.  The amount of charge applied to the battery during each charging pulse is monitored and this value is then removed from the battery during the discharging pulse, as seen in figure 3.10.  This is done to ensure that the current SoC of the battery does not drift during each set of microcycles.

Figure 3.10 – During the charging pulse of the microcycle the total charge added to the battery is recorded and stored in the shifter and is set as Charge to Integrate.  The discharging integrated charge is then monitored during the discharging pulse.  Once the Discharging Integrated Charge has reached the Charge to Integrate the discharge pulse will finish

Figure 3.11 – At the end of each microcycle any net difference between integrated charge is calculated.  As discharging integrated charge is negative this is done by adding the two values together.  This is then added to the running total for each microcycle in this set while the values in charging and discharging intgrated charge are reset to zero.  At the beginning of each set of microcycles the value of integrated charge is reset to zero.

To ensure that any potential drift is kept to a minimum, any difference between the charge added to the battery and that removed from it is recorded at the end of each microcycle and added to a running total, as seen in figure 3.11.  At the end of each set of microcycles this value is sent back to the master so that it can be taken into account when calculating how much charge to add to or remove from the battery to move it to the next SoC, as seen in figure 3.12.

Figure 3.12 –  The master calculates the amount of charge to integrate to move the battery to the next test SoC for each set of microcycles.

## DAQmx Interface

Every time a slave VI is run it will interact with the DAQmx devices to set limits, currents, relay states etc, and to obtain the data from the tests.  For each slave VI this is done in the same way.  As seen in chapter 2 the devices are used to apply current demand to the control board as well as applying the upper and lower voltage limits to the limiter.  They are also used to control the relay system as well as reading the data back from the battery.  All slave VIs complete these tasks using the same code.

Each of these functions; ‘reading from the battery’, ‘writing to the battery’, ‘switching relays’ and ‘setting limits’, is established as an individual task.  Within these tasks are separate activities. For example within ‘reading from the battery’ there is: reading the voltage, reading the current and reading the current readback.  Each of these activities is assigned an input/output port in the USB6009 device and a linear scale.

As the DAQmx devices are only capable of inputting and outputting ±10 V is it necessary to scale the appropriate inputs and outputs to the real-world values.  These data points for these scales were obtained using a voltmeter measuring battery voltage, an ammeter measuring current into the battery and a program written in LabVIEW to measure the voltage and current readback on the USB6009.

Figure 3.13 – Battery current scaling for USB6009 where the current demand applied to the battery is on the     y-axis and the corresponding voltage outputted from the device is on the x-axis

Figure 3.14 – The battery current is applied to the battery current (activity) of the battery read task to increase the limits of the input range of the battery current port

These scales, an example of which is given in figures 3.13, were then produced and assigned to the battery voltage, battery current and current demand, as seen in figure 3.14.  This calibration was completed after every third test.

When a slave VI is opened one of the first things it does is establish which tasks will be used within the program and create a reference to each task as seen in figure 3.15.  This reference is stored in the shifter of the slave VI as a ‘refnum’ so that when the devices are asked to complete a task, as seen in figure 3.16, the appropriate port and scale are used.

Figure 3.15 – The tasks completed by the devices are initiated and a reference to each one is stored in the shifter

This reference is stored in the shifter of the slave VI as a ‘refnum’ so that when the devices are asked to complete a task the appropriate port and scale are used. This is seen in figure 3.16.

Figure 3.16 –  When the program requires the devices to complete a task the reference created for that task, by the method shown in figure 3.15, is used to apply the appropriate scales to the appropriate port

## Recording Data

The majority of the data is stored by the slave VIs, with the master VI only writing to one file in order to document the display data - the values which are shown on the master’s front panel during testing.  As with interfacing with the devices all VIs complete this task identically.  All data is saved in a TDMS file format as they produce relatively small files for a large amount of data and they can be written to at a high speed.  The TDMS format also allows data to be grouped together in a three tiered hierarchy.  The top level, being the file, can contain an unlimited number of groups which in turn can contain an unlimited number of channels.   Every time a slave VI is opened it generates a new TDMS file name, using the TDMS root name sent from the master, and adding a unique number to it, as explained in section 3.8.  All data generated is stored in this file until the slave VI Is finished and closed.  As LabVIEW stores the data in a temporary cache whilst it writes it to a data file, splitting up the files in this way means that LabVIEW regularly releases the memory it uses.

When a slave VI is opened the master VI sends the data path root to the slave VI.  This is entered by the user at the beginning of testing and consists of the location of the data folder for the current test as well as a root name for all data files.  This root name is then used to generate a file name by adding a number to the end of the filename, starting with 001.  The data folder containing the files is searched, and if there is already a file with this name the number is incremented until a unique file is found.  A new file is then created, as well as a reference to this file which is stored in the shifter of the VI.  The data is regularly written to this file, using this reference to locate the file, until the slave VI is closed.  Excluding the Microcycle VI, only one group is created for the duration of the slave VIs task with the current, the voltage and the current demand each being stored in a separate channel, as seen in figure 3.17.  In the case of the Microcycler VI, the data for each microcycle is stored in a different group incrementing a counter at the end of each microcycle to create a new group.   Once the task is finished the TDMS file is closed before the master VI closes the slave VI.

For all slave VIs the battery voltage, battery current and battery current demand waveforms are stored in separate channels

Figure 3.17 – The data file reference is used to locate the required file.  The battery data is then written to the file with the voltage, current and current demand split into separate channels.  The constant stored in Number of Run Presses is incremented at the end of each microcycle to use as a counter to create a new group for each microcycle.

In the case of the Microcycler VI, the data for each microcycle is stored in a different group incrementing a counter at the end of each microcycle to create a new group.  Once the task is finished the TDMS file is closed before the master VI closes the slave VI.

For all slave VIs the battery voltage, battery current and battery current demand waveforms are stored in separate channels

## Conclusion

The software used for testing within this work was developed from a previously existing battery testing system, created in LabVIEW using the programming language G, with rig specific changes made to allow for its use.  Four slave VIs were created with an overseeing master VI controlling the order of testing as well as interfacing with the user.  During testing all required tasks were completed with the data captured accurately

This chapter has given an overview of the software used to implement testing.  The reasoning for creating five VIs is described, as well as the relationship between the master VI and the slave VIs with an individual description of each VI.  The methods used for interfacing with the hardware described in chapter 2 and for storing the generated data, were also given.  A full state diagram of the VIs as well as the interactions between them is presented in appendix A2.

## The following chapter will present the data obtained during testing to show the DCA characteristics of the batteries under test.  The results will be split into two sections.  The first section will present the data obtained when a lower charging current of 1.67C was applied to the battery during the microcycles, as explained in chapter 1, while the second section will contain the data from a charging current of 4C.  An explanation of the results will be given as well as a discussion and comparison between datasets.

## References

[3.1]	J.  Travis, J.  Kring, “Labview for Everyone: Graphical Programming Made Easy and Fun”, Pearson Education, 2009. ISBN: 0-13-185672-3

# DCA test results

Having presented the hardware and software designed for the testing in the previous chapters, this chapter concentrates on the results of the tests, presented in sections 4.2.1 and 4.2.2.  The sets of results are split into two groups each defined by the value of current applied during the charging pulse of the microcycles.  Initially a relatively low charging current of 1.67C was used, in keeping with tests by Karden in [4.1].  After reviewing these results it was found that the test batteries easily accepted this low level of current, especially at lower SoCs, therefore leading to an incomplete set of results.  The charging current was then increased to 4C.

## Test Batteries

Testing was completed using three different PbA test battery technologies, a Furukawa FTZ12–HEV 12V UltraBattery [4.2], two high carbon 6V Exide AS 06 024 C spiral wound PbA batteries connected in series [4.3], and a Yuasa YTX9–BS 12V PbA motorcycle battery [4.4].  The high carbon batteries were available from ongoing projects at the University of Sheffield, and the Yuasa battery was sourced commercially as a similar size and capacity to the Furukawa UltraBattery, for comparison.  A table is given in table 4.1 detailing the parameters of the test batteries

| Battery | Nominal Voltage V | Nominal Capacity, C20 Ah | Dimensions (LxWxH) Mm | Weight Kg |
| --- | --- | --- | --- | --- |
| FTZ12–HEV | 12 | 8.4 | 150 x 87 x 110 | 3.8 |
| AS 06 024 C | 6 | 24 | 65 x 175 x 190 | 4.7 |
| YTX9–BS | 12 | 8.4 | 150 x 87 x 105 | 3.0 |

Table 4.1 – A table showing the parameters of the test batteries.  As two AS 06 024 C batteries were tested in series the nominal voltage, length and weight should be considered as double the values given here.

The FTZ12–HEV, shown in figure 4.1, is a combination of a PbA battery and an asymmetric super-capacitor embedded in the same cell.  The super capacitor consists of a lead dioxide positive electrode, the same as a PbA battery, and a porous carbon negative electrode.  As both positive electrodes are fabricated using the same material, the PbA and the supercapacitor can share their positive electrode while the negative electrodes are connected in parallel as outlined in chapter 1, section 1.5.1.  This enables the two technologies to share the load [4.5]

Figure 4.2 – The Furukawa FTZ12-HEV UltraBattery.  It consists of a lead-acid battery and an asymmetric super-capacitor with the negative electrodes connected in parallel

Capacitor negative electrode

Lead-acid negative electrode

Separator

Shared positive electrode

i

i

i1

i2

The AS 06 024 C, seen as a set of two in figure 4.3, is a PbA battery with a carbon loaded negative plate.  It has been established that the addition of carbon to the negative active material works to counteract the deterioration of performance found in PbA batteries used within HEVs [4.6].

Figure 4.3 – Two Exide AS 06 024 C carbon loaded lead-acid batteries connected in series

The YTX9-BS, seen in figure 4.4, is a commercial off the shelf VRLA PbA battery used as a comparison battery to give a benchmark for the other tests.

Figure 4.4 – Yuasa YTX9-BS lead-acid battery.  This battery was selected due to its similar dimensions to the FTZ12-HEV UltraBattery

The results of the test, and comparisons with the standard battery will now be described in the following section.

## DCA Results

As explained in chapter 1, DCA is a measure of the amount of current accepted by the battery during a specific period of time.  In the context of these tests, that period of time is each microcycle’s 10 s charging pulse, also explained in chapter 1. During this period an upper voltage limit of 16 V is applied to the battery.  When the battery voltage reaches this limit the current applied to the battery is reduced by the limiter, as explained in chapter 2, consequently reducing the charge accepted by the battery.  This behaviour is illustrated in figures 4.5 and 4.6 where each figure shows the current applied, as well the voltage response, during a set of 20 microcycles,

In figure 4.5 the microcycles have been completed whilst the battery is in a higher SoC and the upper voltage limit has been reached almost immediately, therefore causing the current to limit.  The set of microcycles shown in figure 4.6 have been completed at a lower SoC, allowing the voltage to rise without reaching 16 V and therefore the battery is able to accept all current applied to it for the full 10 s.  The DCA of the battery is consequently higher in the microcycles shown in figure 4.6, than in those shown in figure 4.5.

| Figure 4.5 – A set of 20 microcycles at 90% SoC where the current is reduced due to the battery hitting 16 V | Figure 4.6 – A set of 20 microcycles at 42% SoC where the current remains constant for the full 10 s |
| --- | --- |

### 1.67C Microcycle Charging Current

For the first series of testing the charging current applied during the microcycles was the experimentally measured capacity of the battery, Cexp , for that test temperature, multiplied by 1.67. This is referred to as 1.67C.

In figure 4.5 the microcycles have been completed while the battery is in a higher SoC and the upper voltage limit has been reached almost immediately, causing the current to limit.  The set of microcycles shown in figure 4.6 have been completed at a lower SoC, allowing the voltage to rise without reaching 16 V and therefore allowing the battery to accept all current applied to it for the full 10 s.  The DCA of the battery is therefore higher in the microcycles shown in figure 4.6, than in those shown in figure 4.5.

Looking at an overview of the results for this charging current, seen in figures 4.7 and 4.8, the general trend of a battery having a higher DCA when it is at a lower state of charge becomes more evident.  Here the 10th microcycle is taken from each set of microcycles and is plotted against the test SoC at which it was completed, for the FTZ-HEV and the YTX9–BS in figures 4.7 and 4.8 respectively.  In both figures the discharging SoC steps are shown in (a) while the charging SoC steps are shown in (b).  For all DCA graphs the charge accepted by the battery is normalised Cexp of the individual battery at each test temperature to allow for comparisons between different battery capacities.

| a | b |
| --- | --- |

Figure 4.7 – (a) The DCA of the FTZ12-HEV during the charging pulse of the 10th microcycle is shown for each discharging test SoC for all test temperatures.  (b) The DCA of the FTZ12-HEV during the charging pulse of the 10th microcycle is shown for each charging test SoC for all test temperatures

For both batteries, for the majority of test temperatures, when the battery is at a lowest SoC the full charging current is accepted over the 10 s period.  As the SoC increases the DCA falls. This fall is more prominent in the YTX9–BS, while the FTZ12–HEV achieves a higher DCA characteristic overall.

| a | b |
| --- | --- |

Figure 4.8 – (a) The DCA of the YTX9-BS during the charging pulse of the 10th microcycle is shown for each discharging test SoC for all test temperatures.  (b) The DCA of the YXT9-BS during the charging pulse of the 10th microcycle is shown for each charging test SoC for all test temperatures

In the case of the FTZ12–HEV, at the higher temperatures, the battery remains fairly consistent in accepting the full current during the discharging SoCs where the battery accepts all current in all but the two highest SoCs.  Regardless of the general trend of a lower DCA in the YTX9–BS, the trend of a higher DCA in the discharging SoCs sets is apparent in both batteries.

As outlined in [4.7] it is expected that the DCA characteristic is higher immediately after the battery has been discharged as the lead sulphate crystals which limit charge acceptance are more soluble after a discharge history.  This is especially true for PbA batteries containing carbon, such as the FTZ12–HEV, as it has been established that the addition of carbon delays the formation of sulphate crystals with varied successes depending on the type and amount of carbon [4.8].

The overview of results also highlight the effect temperature has on the batteries’ ability to accept charge, with an increase in temperature largely resulting in an increase in DCA.  The correlation with temperature is more obvious with the YTX9–BS while the FTZ12–HEV remains relatively consistent, especially for the discharging SoC steps. This is excluding 0°C where its DCA values fall for both discharging and charging SoCs.  For both batteries the optimal temperate of those tested was 40°C

The overview results of the FTZ12–HEV’s charging SoC steps, shown in figure 4.7(b), seem to indicate that for the top two temperatures during the charging tests the results for 70% SoC seem to have a higher DCA than those for 90%, which is unexpected. However, as these graphs show just one DCA results from each set of 20, it is important to view the full DCA results to gain a clearer picture.

The full DCA results for each test temperature are presented in figures 4.9b to 4.13b. During the test, as outlined in chapter 1, the battery is charged or discharged to the test SoC and allowed to rest before the set of 20 microcycles are completed.  Therefore the tests will generate an individual DCA value for every microcycle completed, in a set of 20, at each test SoC.  Each set of DCA results is plotted on the x-axis, with incrementing microcycles plotted consecutively against the estimated SoC that the set was tested at on the y-axis. Both charging and discharging SoC steps are plotted on the same graph

0°C

Discharging

Charging

a

b

Figure 4.9 – (a) The final OCV value of both test batteries during the rest periods before each set of microcycles is plotted on the y-axis with the estimated SoC for both charging and discharging plotted on the x-axis.  (b) For both batteries each DCA value from each set of 20 microcycles are plotted on  the y-axis, set against the estimated SoC of the battey on the x-axis.  For both graphs testing was completed at 0°C

10°C

Discharging

Charging

a

b

Figure 4.10 – (a) The final OCV value of both test batteries during the rest periods before each set of microcycles is plotted on the y-axis with the estimated SoC for both charging and discharging plotted on the x-axis.  (b) For both batteries each DCA value from each set of 20 microcycles are plotted on  the y-axis, set against the estimated SoC of the battey on the x-axis.  For both graphs testing was completed at 10°C

For the 1.67C series of results the discharges to each test SoC proved inconsistent with most discharges falling short by 4%. For all results, in this series of testing and the next, the amount of charge added or removed from the battery was calculated after the test and results are plotted against the calculated SoC.

While the calculation of the discharging and charging steps are fairly precise, what the battery does once the relays are closed cannot be controlled and the battery naturally floats to its OCV.  For this reason the test SoC values given in the DCA graphs can only be considered an estimate.  To account for this, the OCV values for each test SoC for each test temperature are presented in figures 4.9a to 4.13a.

20°C

Discharging

Charging

a

b

Figure 4.11 – (a) The final OCV value of both test batteries during the rest periods before each set of microcycles is plotted on the y-axis with the estimated SoC for both charging and discharging plotted on the x-axis.  (b) For both batteries each DCA value from each set of 20 microcycles are plotted on  the y-axis, set against the estimated SoC of the battey on the x-axis.  For both graphs testing was completed at 20°C

As with the general trend graphs the full DCA results show a more favourable DCA characteristic after the battery has been discharged.  However it becomes clear, when looking at the full set of results, that the initial high result immediately after a discharge history is prone to fall with each consecutive microcycle.  This conforms to the expectations provided by [4.9], as it was outlined in [4.10], that the solubility of the sulfate crystals that result from a discharge period is inversely proportional on the local H2SO4 concentration. During discharging the H2SO4 solution immediately adjacent to the plates is depleted due to the reaction outlined in      chapter 1.

30°C

Discharging

Charging

a

b

Figure 4.12 – (a) The final OCV value of both test batteries during the rest periods before each set of microcycles is plotted on the y-axis with the estimated SoC for both charging and discharging plotted on the x-axis.  (b) For both batteries each DCA value from each set of 20 microcycles are plotted on  the y-axis, set against the estimated SoC of the battey on the x-axis.  For both graphs testing was completed at 30°C

This reduction in H2SO4 results in sulfate crystals that are relatively soluble allowing for an efficient recharge. While the DCA of initial microcycles improves due to this solubility, subsequent charging increases the H2SO4 concentration, thereby decreasing the solubility of the crystals. Consequently the efficiency of the recharge is reduced leading to a reduced DCA [4.10].

This behaviour is a more prevalent characteristic of the YTX9–BS, with the FTZ12–HEV being more likely to maintain the higher DCA.  It is also evident that even in the cases where the FTZ12–HEV results do demonstrate this behaviour, it is mostly true that, for the same test SoC, the final DCA value remains higher in this test battery than the DCA value of the initial microcycle of the YTX9–BS.

40°C

Discharging

Charging

a

b

Figure 4.13 – (a) The final OCV value of both test batteries during the rest periods before each set of microcycles is plotted on the y-axis with the estimated SoC for both charging and discharging plotted on the x-axis.  (b) For both batteries each DCA value from each set of 20 microcycles are plotted on  the y-axis, set against the estimated SoC of the battey on the x-axis.  For both graphs testing was completed at 40°C

As previously mentioned in this section, the DCA result at 70% SoC during the charging SoC steps is, in the case of the top two temperatures, lower than that at 90% SoC. When looking at the full results, however, it appears that it is actually more prevalent; with at least one battery at each test temperature displaying this behaviour. These results show that when the batteries were at 90% SoC during the charging SoC steps their DCA behaviour is more akin to what would be expected in a discharging step e.g. a high initial DCA, which falls with each consecutive microcycle. As charging to 90% SoC causes the battery to reach its upper voltage limit, a reduced charging current is applied to the battery – albeit for a longer duration to reach the desired SoC. It may be that this reduction in applied current has an effect on the accumulation of sulfate crystals, however, the definitive reason for this is unknown and is an area for further research.

As it has been documented in [4.11] that, as well as the batteries’ SoC, its immediate charging history, and test temperature, the length of time the battery is given to rest before completing microcycles has an effect on the battery’s DCA. It has been found that, in general, a longer pause will result in a lower DCA. This is believed to be due to the “Hardening Crystals” effect, where the solubility of the sulfate crystals that form on the negative plate, and limit DCA, reduces with time leading to a lower dissolution rate for older crystals [4.11].

To allow for some comparison in rest time, without radically extending the test time, one test SoC was chosen to have two sets of microcycles completed after a charging period but with different durations of resting periods. This was only possible for 90% SoC, those to the far left and far right of the full DCA graphs. As the battery is fully discharged by the end of the pre test conditioning it can then be recharged to 90% SoC. As a result, in this series, the first 90% SoC test was completed after the battery had been allowed to rest for 1 h while for all other SoCs, including the second 90% SoC test, the battery is rested for just 10 minutes. As the first 90% SoC DCA results do not mirror the aforementioned atypical behaviour of the second as severely , it may be that a longer rest time after a charge to 90% SoC may reduce this behaviour. Again this is an area of ongoing research

In this initial series of testing there are two anomalous results, one in 4.10(b) and one in 4.12(b) where the current applied to the battery drops out. The reason for this is unknown, however the remainder of the test results have not been affected.

While it is a desirable behaviour for the battery to accept all current applied to it, the fact that the results for the FTZ12–HEV show that it accepts all charge even, in some cases, when the battery is above 70% SoC means that the true behaviour of the battery is incomplete.  To provide a clearer picture of the behaviour at the lower SoCs the charging pulse current was increased to 4C.  These results are presented in section 4.2.2

### 4C Microcycle Charging Current

In this series of tests a string of two high carbon 6V 24Ah Exide PbA batteries was added to the FTZ12–HEV and YTX9–BS test batteries.

As with section 4.2.1 an initial overview of the 10th microcycle for each set of 20 microcycles for all test batteries at each test temperature is presented in figures 4.14 to 4.16 for the FTZ12–HEV, YTX9–BS and Exide batteries respectively

| a | b |
| --- | --- |

Figure 4.14 – (a) The DCA of the FTZ12-HEV during the charging pulse of the 10th microcycle is shown for each discharging test SoC for all test temperatures.  (b) The DCA of the FTZ12-HEV during the charging pulse of the 10th microcycle is shown for each charging test SoC for all test temperatures

Again the overview graphs demonstrate a consistently superior DCA characteristic in the FTZ12–HEV when compared to the YTX9–BS, where the increased charging current has had less of an impact on the former.  The FTZ12–HEV is still able to accept the full charging current for the full charging period when in the lower SoCs during the discharging SoC steps.  During the charging SoC steps, however, the battery only maintains its ability to accept the full charging pulse when it is in the lowest SoC. While this is still fairly similar to the previous result it does provided a clearer picture of the battery behaviour.

The YTX9–BS, in comparison, only accepts the full 4C charging current when in the lowest SoC and this only occurs in the top two temperatures for the discharging steps and the top temperature for the charging.  The results for 10°C are omitted from these results as the battery failed before this test could be completed.

| a | B |
| --- | --- |

Figure 4.15 – (a) The DCA of the YTX9-BS during the charging pulse of the 10th microcycle is shown for each discharging test SoC for all test temperatures.  (b) The DCA of the YTX9-BS during the charging pulse of the 10th microcycle is shown for each charging test SoC for all test temperatures

| a | b |
| --- | --- |

Figure 4.16 – (a) The DCA of the Exide during the charging pulse of the 10th microcycle is shown for each discharging test SoC for all test temperatures.  (b) The DCA of the YTX9-BS during the charging pulse of the 10th microcycle is shown for each charging test SoC for all test temperatures

As the order of test for all the batteries was: 20°C, 30°C, 40°C, 0°C, 10°C the failure of the YTX9–BS occurred during the last test in this piece of work.  It should be noted that, while the falling state of health of the YTX9–BS may have had an effect on the DCA results in the tests immediately before failure, when these are compared to earlier tests there is no marked difference in the behaviour of the YTX9–BS

For the string of Exide batteries these DCA results show that it does not match the performance of the FTZ12–HEV despite the carbon additives.  For the discharging SoCs, only during three tests does the battery accept the full charging current, even in the lowest SoCs.  For the charging steps the majority of tests result in the battery only accepting the full charging current in the lowest SoC.  This is excluding the test completed 0°C where the performance of all batteries is reduced

Again, as in the previous section, figures 4.17.a to 4.21a show the final OCV values immediately before each set of microcycles set against the test SoCs for each temperature while figures 4.17b to 4.21b show the full DCA test results for all test SoCs for each test temperature.

0°C

Discharging

Charging

a

b

Figure 4.17 – (a) The final OCV value of all test batteries during the rest periods before each set of microcycles is plotted on the y-axis with the estimated SoC for both charging and discharging plotted on the x-axis.  (b) For all batteries each DCA value from each set of 20 microcycles are plotted on  the y-axis, set against the estimated SoC of the battey on the x-axis.  For both graphs testing was completed at 0°C

As with the overview graphs, the full DCA results show that the higher charging current results in the YTX9–BS rarely succeeding in accepting the full charging current.  This only occurs in the top two temperatures and only when the battery is lower than 30% SoC.  The string of Exide batteries, while appearing similar to the YTX9–BS for the higher SoCs, demonstrates a more appealing DCA characteristic when in the lower test SoCs than the YTX9–BS with this battery accepting the full charging pulse for more SoCs

10°C

Discharging

Charging

a

b

Figure 4.18 – (a) The final OCV value of both test batteries during the rest periods before each set of microcycles is plotted on the y-axis with the estimated SoC for both charging and discharging plotted on the x-axis.  (b) For both batteries each DCA value from each set of 20 microcycles are plotted on  the y-axis, set against the estimated SoC of the battey on the x-axis.  For both graphs testing was completed at 10°C

Unlike the previous series of tests, where after the pre test conditioning the battery is charged to the first test SoC, during these tests the battery is fully charged after the pre test conditioning. Therefore the initial 90% SoC test is completed after the battery is discharged to from 100% SoC.  It is still allowed to rest for 1 h instead of 10 minutes.  The DCA results after the 1 h rest have a marginally more consistent behaviour than the remainder of the discharging SoC results, however there is not a substantial difference. It may be that a rest time of 1 hour is not sufficient for the “Hardening Crystals” effect to take place as this is the lower limit of rest time given in [4.11].

20°C

Discharging

Charging

a

b

Figure 4.19 – (a) The final OCV value of all test batteries during the rest periods before each set of microcycles is plotted on the y-axis with the estimated SoC for both charging and discharging plotted on the x-axis.  (b) For all batteries each DCA value from each set of 20 microcycles are plotted on  the y-axis, set against the estimated SoC of the battey on the x-axis.  For both graphs testing was completed at 20°C

While the majority of the behaviour of the batteries during this series of tests matches that of the previous section the phenomenon of the set of DCA results at 90% SoC in the charging SoC steps displaying behaviour more suited to a set immediately after a discharge is not seen in this section. While this was consistently seen during the 1.67C tests the only exhibition of this behaviour at 4C is seen for the YTX9–BS where, for all test temperatures, the initial DCA results of the 90% SoC in the charging SoC steps are relatively higher than the subsequent DCA results. It may, therefore, be that the higher charging current has an effect on this behaviour

30°C

Discharging

Charging

a

b

Figure 4.20 – (a) The final OCV value of all test batteries during the rest periods before each set of microcycles is plotted on the y-axis with the estimated SoC for both charging and discharging plotted on the x-axis.  (b) For all batteries each DCA value from each set of 20 microcycles are plotted on  the y-axis, set against the estimated SoC of the battey on the x-axis.  For both graphs testing was completed at 30°C

Conversely, during these tests it is noted that for the FTZ12–HEV, when the battery is at 30% SoC immediately after a charging period, the DCA of the battery actually increases for consecutive microcycles. This behaviour is also seen slightly for the surrounding SoCs but is most predominant at 30%. The reason for this is unknown and is an intriguing area for further research

The OCV graphs show that, during the majority of tests in this series, the starting voltage for the initial microcycle for each test SoC were more consistent across the test batteries when compared to previous tests, especially for the discharging SoCs.  However, for the YTX9–BS the OCV for the charging steps is significantly higher than that for the discharging, despite the fact that for all these tests they had been set to the same SoC before being allowed to rest

40°C

Discharging

Charging

a

b

Figure 4.21 – (a) The final OCV value of all test batteries during the rest periods before each set of microcycles is plotted on the y-axis with the estimated SoC for both charging and discharging plotted on the x-axis.  (b) For all batteries each DCA value from each set of 20 microcycles are plotted on the y-axis, set against the estimated SoC of the battey on the x-axis.  For both graphs testing was completed at 40°C

It is also evident that the OCV for the YTX9–BS is consistantly higher than the other batteries for both charging and discharging tests.  It has been identified that a higher OCV after a set rest time is an indication of acid stratification which is an indication of an ageing battery [4.9].  This corresponds with the fact that the YTX9–BS  battery failed before all tests could be completed.

To provide a view of how DCA can be affected by the OCV immediately before testing, the results for the FTZ12–HEV, YTX9–BS and Exide at  20°C are presented again in figures 4.22, 4.23 and 4.24 respectively. In these graphs each set of micrcocycles is plotted against OCV instead of SoC whereby all those sets that fall within the same 0.1 range are plotted together under a number on the x-axis.  The ranges of OCV and their corresponding numbers can be found in table 4.2

| x-axis Value | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| OCV Range (V) | 13.40 -13.49 | 13.30 - 13.39 | 13.20 -13.29 | 13.10 -13.19 | 13.00 - 13.09 | 12.90 - 12.99 | 12.80 - 12.89 | 12.70 - 12.79 |
| x-axis Value | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 |
| OCV Range (V) | 12.60 -12.69 | 12.50 - 12.59 | 12.40 -12.49 | 12.30 -12.39 | 12.20 - 12.29 | 12.10 - 12.19 | 12.00 - 12.09 | 11.90 - 11.99 |
| x-Axis Value | 17 | 18 | 19 | 20 | 21 |
| OCV Range (V) | 11.80 -11.89 | 11.70 - 11.79 | 11.60 -11.69 | 11.50 - 11.59 | 11.40 -11.49 |

Table 4.2: A list of ranges that the test batteries fell into during testing and the number that they correspond to in figures 4.22, 4.23 and 4.24

In these graphs it remains apparent that, for this test temperature, the FTZ12–HEV is still superior compared to the other test batteries, in both charging and discharging steps. However, while these results clearly show a superior behaviour when the battery has a low OCV, where the FTZ12–HEV accepts the full charging current, when looking at the higher OCV results, the behaviour of all test batteries is relatively matched.

High OCV

Low OCV

Figure 4.22 – The DCA results of each set of 20 microcycles for all batteries.  Each set is plotted againt the range of OCV that the battey was in immediately before the 20 micrcycles were conducted.  These ranges and the x-axis number they correspond to can be found in table 4.2.  Testing was completed at 20°C

High OCV

Low OCV

Figure 4.23 – The DCA results of each set of 20 microcycles for all batteries.  Each set is plotted againt the range of OCV that the battey was in immediately before the 20 micrcycles were conducted.  These ranges and the x-axis number they correspond to can be found in table 4.2.  Testing was completed at 20°C

For example, in group 5 where all test batteries have an OCV between 13.00 V – 13.09 V after a charging step, the FTZ12–HEV only marginally outperforms the other batteries. In this group the FTZ12–HEV maintains a DCA of ~0.5 A/Ah with the others reaching ~0.4 A/Ah. This is improved in group 8 where all test batteries have an OCV between 12.70 V – 12.79 V after a discharging period. Here the DCA of the FTZ12–HEV falls between ~2 and 1.1 A/Ah, the YTX9–BS between ~1.2 and 0.9 A/Ah and the Exide string between 1.5 and 1 A/Ah.

High OCV

Low OCV

Figure 4.24 – The DCA results of each set of 20 microcycles for all batteries.  Each set is plotted againt the range of OCV that the battey was in immediately before the 20 micrcycles were conducted.  These ranges and the x-axis number they correspond to can be found in table 4.2.  Testing was completed at 20°C

For the higher OCVs the FTZ12–HEV starts accepting the full charging currents after a discharging period when the OCV is 12.10 – 12.19 V while the other batteries can only manage an initial DCA of ~3.4 Ah//A, when OCV is 12.20 – 12.29, before rapidly falling. The Exide shows minimal improvement on the YTX9 – BS for this test temperature when the results are presented this way.

The envelope of these results show that while the DCA of the FTZ12–HEV are still superior to, different levels depending on battery OCV, there is a marked difference between the charging and discharging results for this battery. For the Exide and YTX9 – BS, however, there is a more consistent result at this temperature with both charging SoCs and discharging SoCs having a more linear relationship between DCA and OCV.

## Conclusion

This chapter has presented the results of the test outlined in chapter 1, with test results separated into sections based on the charging current applied to the battery during microcycles. Initially two batteries were tested, the Furukawa FTZ12–HEV 12V UltraBattery and the Yuasa YTX9–BS 12V, a commercial PbA battery. For the first series of tests the charging current was limited to 1.67C. This provided a picture of the batteries behaviour when they were in a high SoC but, due to the batteries accepting the full charging current, information was missing for the lower SoCs. Even with an incomplete picture of the batteries’ behaviour the FTZ12–HEV presented a more appealing DCA characteristic with the YTX9–BS reaching its upper voltage limit for the majority of SoC, therefore creating a reduction in DCA.

To provide a more complete picture of the DCA characteristic of the batteries the charging current was increased to 4C and a third battery technology was added to the test batteries. This was a string of two high carbon 6V 24Ah Exide batteries. While increasing the charging current to the higher value provided a better picture for the YTX9–BS – the amount of charging current it accepted in the lower SoCs was further limited – the FTZ12–HEV continued to accept the full charging current for the same SoCs for the majority of test temperatures. The results for the string of Exides displays a behaviour marginally improved to that of the YXT9–BS and not to the extent of the FTZ12–HEV.

Finally the full set of DCA results completed at 20°C for each battery were plotted, instead of against the SoC, against the OCV of the battery immediately before each set of 20 microcycles were completed. These graphs confirmed the preferable behaviour of the FTZ12–HEV when the battery had a lower OCV but highlighted that when the batteries had a higher OCV they displayed relatively similar abilities.

## References

[4.1] 	E.  Karden, F.  Jöris, H.  Budde-Meiwes and D.U.  Sauer, “Test methods for dynamic charge acceptance (DCA) of microhybrid starter batteries” presented at 13ELBC European Lead Battery Conference, Paris, 2012

[4.2]	Hund, T., Clark and N.  Baca, W., “Ultrabattery test results for utility cycling applications, The 18th International Seminar on Double Layer Capacitors and Hybrid Energy Storage Devices 12/08”, U.S.A. Available: http://www.ecoult.com/wp-content/uploads/2012/03/Hund-UltraBattery-Utility-Testing-12-08.pdf [Accessed: 28 April 2016]

[4.3]	GNB Industrial Power, “Motive Power block batteries AGM – Spiral wound AS range”.  Available: http://www.exide.com/Media/files/Downloads/IndustEuro/GNB_MP_Block_Overview%20_en.pdf   [Accessed: 28 April 2016]

[4.4]	Yuasa, “YTX9–BS”.  Internet: http://www.halfords.com/motoring-travel/motorcycling/motorcycle-parts/yuasa-ytx9-bs-powersport-motorcycle-battery [Accessed: 28 April 2016]

[4.5]	L.T.  Lam, L and R.  Louey, “Development of ultra-battery for hybrid-electric vehicle applications”, J.  Power Sources, 158, pp.  1140-1148, 2006. Available: http://dx.doi.org/10.1016/j.jpowsour.2006.03.022

[4.6]	K.  Nakamura, M.  Shiomi, K.  Takahashi and M.  Tsubota, “Failure modes of valve-regulated lead/acid batteries”, J.  Power Sources, 59, pp.  153, 1996. Available: http://dx.doi.org/10.1016/j.jpowsour.2008.08.059

[4.7]	M.  Thele, J.  Schiffer, E.  Karden, E.  Surewaard and D.U.  Sauera, “Modelling of the charge acceptance of lead–acid batteries”, J.  Power Sources, 168, pp.  31-39, 2007. Available: http://dx.doi.org/10.1016/j.jpowsour.2006.11.088

[4.8]	P.T.  Moseley, “Consequences of including carbon in the negative plates of valve-regulated-Lead-Acid batteries exposed to high-rate partial-state-of-charge operation”, J.  Power Sources, 191, pp.  134-138, 2009. Available: http://dx.doi.org/10.1016/j.jpowsour.2008.08.084

[4.9]	 H.  Budde-Meiwes, D.  Schulte, J.  Kowal, D.U.  Sauer, R.  Hecke, E.  Karden, “Dynamic charge acceptance of lead–acid batteries: Comparison of methods for conditioning and testing”, J.  Power Sources, 207, pp.  30-36, 2007. Available: http://dx.doi.org/10.1016/j.jpowsour.2011.12.045

[4.10] 	P.  T.  Mosely, D.  A.  J. Rand, B.  Monahov, “Designing lead-acid batteries to meet energy and power requirements of future automobiles”, J.  Power Sources, 219, pp. 75-79, 2012. Available: http://dx.doi.org/10.1016/j.jpowsour.2012.07.040

## [4.11]	S.  Shaeck, A.  O.  Stoermer, F.  Kaiser, L.  Koehler, J.  Albers, H.  Kabza, “Lead-acid batteried in micro-hybrid applications. Part 1. Selected key parameters”, J.  Power Sources, 196, pp. 1541-1554, 2011. Available: http://dx.doi.org/10.1016/j.jpowsour.2010.08.077

# Discussion

As the results have been presented in chapter 4 this chapter will evaluate some of the interesting points and comment on the scope for further study.  Firstly a summary of what this thesis has presented is given before the results are discussed

This thesis has presented a dynamic charge acceptance (DCA) characterisation of two high carbon lead-acid (PbA) battery types containing differing carbon technologies – the Furukawa FTZ12–HEV 12V UltraBattery and the high carbon 6V Exide AS 06 024 C spiral wound PbA battery, allowing for comparisons between the two.  A third battery, the Yuasa YTX9–BS 12V motorcycle battery – a commercial off the shelf VRLA, was also compared as a control measure.  The first chapter presented the way in which automotive batteries within electric vehicles (EVs) are operated as well as presenting the argument for the implementation of PbA batteries over lithium ion and nickel metal hydride for EVs with low levels of hybridisation.  The concept of DCA as a measure of assessing a batteries ability within EVs was introduced and the test procedure used for this piece of research was outlined.

In Chapter 2 an explanation of the whole test setup, consisting of a test rig, a temperature cooling chamber and a control PC, was given.  Specific requirements of the test rig were also given and the chapter provided details on how rig components work.

Chapter 3, then provided information on the software used to control the rig during testing.  The main tasks of the test were explained as well as how they were assigned to a separate software programs.  These programs were then explained, giving details of how their main tasks were achieved and how they interacted with each other.  The functions used for applying current, setting voltage limits and acquiring and recording data while the programs main tasks were completed were also explained.

The results of the DCA tests, as well as descriptions of the test batteries, were then presented in chapter 4.  These were split into two sections, 1.67C and 4C, based on the charging current value used during testing.  An overview trend of the tests for the FTZ12–HEV and YTX9–BS at 1.67C was given before presenting the full DCA test data.  During this section it was identified that the charging current levels were insufficient in providing a clear picture of the battery technologies and, as such, it was increased to 4C.  The results for the higher charging current were presented in the same manner as those of the 1.67C testing with the addition of presenting, for the test at 20°C, the relationship between DCA and the OCV immediately before the sets of microcycles.

## Results discussion

When the results were presented the initial overview of the 10th microcycle for each test SoC in the 1.67C tests gave a clear indication that the ability of the FTX12-HEV exceeded that of the control battery especially during the discharging steps.  However the graphs showing the full results indicated that only viewing one response out of a set of 20 microcycles was not sufficient, therefore all results were presented for all temperatures.  As well as the set test SoCs the OCV values at the beginning of each microcycle set were included to allow for comparative results between not just the SoC but also OCV.  While the FTZ12–HEV behaviour consistently remained preferable to that of the YTX9–BS the full results indicated that the preferable discharging steps in the overview were less stable than those in the charging steps, with values for consecutive microcycles sharply decreasing.  Therefore it may be assumed that, while knowing the behaviour of the battery after a discharge is desirable, the charging steps are a preferable method in consistent DCA measurement characteristics..  It was also apparent that an increase in rest times also had a stabilising effect on the DCA result therefore an investigation into the effects on open circuit resting time for different battery technologies may lead to more predictable results.  However, it has also been shown that an increased rest time has an effect on charge acceptance levels for standard VRLA batteries with a longer resting time resulting in a lower charge acceptance  [5.1].

After the initials tests the charging current was increased to 4C and the string of two high carbon Exide batteries was added to the test batteries.  While the FTZ12–HEV continued its superior DCA behaviour during these tests the Exide batteries did not offer a significant increase in DCA results when compared to the control battery.

When considering EV traction applications the results in this piece of work suggest that the FTZ12–HEV is the most suitable choice due to its consistent superior DCA behaviour when comparing it to the control battery – the YXT9–BS – and to the high carbon Exide batteries. As outlined in chapter 1 this will result in a more efficient recuperation of energy during regenerative braking. While the Exide batteries displayed an improvement when compared to the control battery this was significantly lower than the FTZ12–HEV. As well as this, when comparing the dimensions of the batteries, given in table 4.1 in chapter 4, while the             FTZ12–HEV is of a similar size and weight to the control battery the combination of the two      6 V Exides will result in an area and weight that is just over three times larger than the          YXT9–BS. As weight is an important factor in automotive applications, and considering the PbA batteries already diminished specific energy when compared to other battery types, the Exide string presents a less viable option compared to the FTZ12–HEV.

The breadth of test results in this work, across a full range of SoC and after both charge and discharge periods, gives rise for an opportunity to consider a metric of the DCA characteristics of automotive batteries. A definitive concrete metric has the potential be added to datasheets to aid in the selection of an appropriate battery. From the DCA vs OCV results, presented in figures 4.22 to 4.24 in section 4.2.2 of chapter 4, an envelope of the DCA behaviour for each of the test batteries was observed.  When a line is drawn through the 10th microcycle of each set of microcycles, as seen in figure 5.1, a clear picture of the DCA characteristics for the test batteries at 20°C can been seen. When comparing these envelopes for the test batteries a clear picture of the batteries behaviour is quickly and easily observed. For example, it is apparent that at the lower SoC the FTZ12–HEV outperforms the other tests batteries for both the discharging and charging steps. It is also clear, however, that the FTZ12–HEV has the greatest difference in behaviour for both sets of SoC steps. When compared to the Exide there is not as great an improvement in DCA when compared to the YXT9–BS however the behaviour of the discharging and charging SoC steps are more consistent with each other.

High OCV

Low OCV

Figure 5.1 – A potential metric for adding DCA characteristics to data sheers is presented as the envelopes shapes of the DCA results of all three test batteries at 20°C. DCA has been plotted against OCV for both charging and discharging SoC steps and the lines of the envelope go through the 10th microcycle from each set of 20 microcycles

It must be recognised, however, that, in-keeping with all standard tests, there may be a variable relationship between a batteries performance in a DCA test and its performance in real-life

## Future study

## While the increase of the charging current to 4C obtained an enhanced picture of the behaviour of the batteries, the true performance of the FTZ12–HEV whilst in the lowest SoC is still unknown.  Therefore, the current would need to be increased to ensure that the battery would limit at all SoCs.  As the current limit of the rig used in this piece of work is limited to 100 A it was not possible to increase the current whilst still including the string of Exide batteries. Therefore work is currently ongoing in to this area with equipment capable of applying higher currents.

When viewing the two sets of results it appears that an increase in microcycle charging current leads to an increase in DCA even when the battery is in a higher SoC and is therefore limiting.  When, for example, the FTZ12–HEV consistently limits during the 90% SoC discharging set of microcycles the two sets of results limit at different values.  The results for the 1.67C tests have the 90% discharging steps limit around 0.5 A/Ah with a maximum of 1A\Ah being reached for 40°C while, for the 4C set of results, the DCA only limits at 0.5 during the 0°C and reaches 2.9 A/Ah during the test at 40°C.  The current fall time in both sets of tests remains fairly constant at ~3-4 seconds regardless of initial charging pulse value.  As the voltage also remains consistent during the pulses the impedance of the test battery can be investigated, focusing on before and after high rate, to determine why the current falls away at the same rate.  These impedance tests can also be completed at the set test SoCs, so as to give insight into how the impedance changes with SoC and what effects this may have on DCA.  These tests can be completed before and after a full series of tests to gain insight into what effect this testing has on the impedance of the battery and therefore how they affect the battery’s state of health.  These investigations can be expanded to gauge what effect the higher voltage limit of 16 V has on the battery, even when applied for a short time.  As the YTX9–BS failed before the 4C series of testing could be completed, the increase in upper voltage limit may be having a detrimental effect on the battery.  Therefore these DCA tests can be completed again with a decreased upper voltage limit of 14.8 V giving an insight into how the upper voltage limit during microcycles effects the battery’s state of health.  This will also allow a comparison between any benefits to DCA the increased limit may have and how this effects the change in impedance before and after testing

Although the gradient of increasing DCA values with decreasing SoC is fairly smooth, occasionally there is a “jump” in values from one SoC test to another.  This is usually in the charging steps and around the 30% SoC step.  As the cooling chamber is only in control of the ambient temperature the battery may be heating up at this point allowing for an increase in charge acceptance.  This test can be repeated with the battery temperature being set by a water bath or, if repeated with the same cooling system, with the battery temperature being monitored throughout testing.

As the limit of 4C for the charging current resulted in a less than complete picture of the behaviour of all the batteries, with even the YXT9–BS control battery still accepting the full pulse when in the lowest SoCs for the highest temperature, further tests will an increased current should be completed. Additionally,  as this work was completed in relation to suitability of PbA batteries for EV operation the batteries currently being utilised in EV, nickel metal hydride and lithium ion, need to tested as well

## References

[5.1]	Y.  Yamaguchi, M.  Shiota, M.  Hosokawa, Y.  Nakayama, N.  Hirai, S.  Hara, “Study of charge acceptance for the lead-acid battery through in situ EC-AFM observation — influence of the open-circuit standing time on the negative electrode” J.  Power Sources, 102, pp.  155-161, 2001. Available: http://dx.doi.org/10.1016/S0378-7753(01)00794-7

# Appendix 1 – Test procedure flow diagram

# Appendix 2 – Software State Diagram

As described in chapter 3, five virtual instruments (VIs) – one master VI used to control four slave Vis – were created in LabVIEW (Laboratory Virtual Instrument Engineering Workbench) to be used to complete the tests outlined in chapter 1.  Each of these VIs was created using a template architecture provided by LabVIEW called Top Level Baseline Prime (TLB’).  Within this architecture each task that the program completes is broken down and compartmentalised into “actions”.  A separate management system is used to monitor the current position of the program, known as its state, and uses triggers within these states to determine which actions should be completed.  As demonstrated in the state diagram figure A2.1, triggers can be used to transition either into a new state or back in to its current state where each trigger contains a list of actions that the program will complete while it is transitioning.  The appropriate trigger is selected based on inputs sent to the management system either from within an action or from an external event.  It is also shown in figure A2.1 that any action can be called by any trigger within any state, i.e. action 2 is called within trigger 1 and trigger 2 of state 1.

Figure A2.1 – An example of a state diagram containing two states.  State 1 has two triggers one of which is used to transition into state 2 while the other is used to transition back into itself.  The second state has one trigger which used to transition into state 1.  Each trigger contains a list of actions which the program will complete while transitioning