Hot deformation and damage of 
  Free Cutting Steel

Miin Fung Kiu

Thesis submitted for the degree of

Doctor of Philosophy

Department of Mechanical Engineering

June 2015

Abstract

Hot rolling as a manufacturing process of Free Cutting Steel (FCS) can produce products with enhanced properties through controlled thermo-mechanical processing. However, like any other manufacturing process, imperfections at various scales can appear during hot rolling therefore affecting product quality and cost effectiveness of the industrial process. Hot rolled FCS in particular suffers mainly from edge cracking taking place during the rolling process at high homologous temperature. Research studies have been conducted in order to understand the cause of such problem. Stress triaxiality and local microstructural inhomogeneities leading to damage formation are of particular interest in the current research. High temperature laboratory tests with specimen geometries specifically designed to generate stress triaxiality levels comparable to those experienced by the material during the hot rolling process have been conducted to initiate damage at the surface of these specimens. Particular attention has been paid to the influence of Manganese-Sulfide (MnS) inclusions on damage formation during these tests. A new experimental procedure has been developed to measure strain distributions at the scale of the microstructure in order to study the effect of strain localisation on damage formation and how this localisation is affected by the presence of  MnS inclusions. A microgrid technique has been used to measure intra-granular strains in specimens deformed at temperatures up to 1200⁰C typical of a hot rolling process. Strain maps have been produced over relatively large areas of the microstructure in non-transformable austenitic stainless steels representative of the behaviour of FCS at high temperature and produced specifically for this research. Tests on FCS have also been conducted at lower temperatures including tensile tests inside a scanning electron microscope with full-field strain measurements obtained using Digital Image Correlation (DIC)  to study damage development over a range of temperatures and scales.

Results have shown that local deformation and local damage at high temperature are highly influenced by the presence of grain boundaries and inclusions. Strain distribution maps highlight such influence on strain localisation. Moreover, the deformation temperature has a significant effect on the mechanism of local deformation and damage in FCS with damage nucleation along grain boundaries observed at the surface of the specimens deformed 1000⁰C as opposed to intra-granular cracking involving inclusions observed at the subsurface.

Acknowledgements

This work would not have been possible without permission to access the information and equipment available in Tata Steel: Swinden Technology Centre, Sorby Centre, Mechanical Engineering and Materials Science Engineering departments of the University of Sheffield.

I wish to express my sincere gratitude to my supervisors Dr. C. Pinna, and Dr D. Farrugia for their encouragement, constructive discussions and continuous support throughout the course of this research. It has truly been an honour to work so closely alongside such experts in the field. For without their valuable input and knowledge this thesis would not have been possible.

I wish to acknowledge the technicians of Mechanical Engineering and Material Science Engineering departments whose help was quintessential for this research. I extend my gratitude to Mr. Karl Rotchell, Mr. Dave Webster, Mr. Paul Downs and all of whom I had the opportunity to work with. I would also like to thank all staff members at the Sorby Centre, in particularly Dr. P. Korgul for his kind assistance with microscopy related works and also his companionship throughout this research.

Above all, I thank God for providing guidance and comfort in my life. I would like to express my deepest gratitude to my parents, Mr. Kiu Mee Sung and Mrs. Ngang Kiu Ung for being a strong pillar of support in every decision along the way. I must also extend my appreciation for Aunty Ruth who was always there for me during period of difficulties in Sheffield. My time in Sheffield would not have been as fulfilling as it was  without the comradeship of my brothers, Mr. Darius Cheong, Mr. Guan-Wei Tsang, Mr. Daniel Ooi, Mr. David Khoo, Mr. Joven Lim and Mr. Avin Wong. I would like to say thank you to a lovely couple, Dr. Adrian Lim and Dr. Sue Foong who have always treated me as part of their family and showered me with unfailing support. My utmost appreciation also goes to Dr. Venus Ho who was there to give me a much-needed push in times of setbacks. Nevertheless, I would like to show my deepest gratitude to Miss Junn Loh who take initiative to offer her helping hand in my thesis completion. Lastly, I would like to express my gratitude to Miss Sophie Lin who stood by every step of the way. This thesis is dedicated to all of them.

Contents

1	Introduction	18

1.1	Engineering context and project driving force	18

1.2	Aim and objectives of the research	20

1.3	Outline of Thesis	21

2	Literature Review	22

2.1	Rolling process	22

2.2	Microstructure evolution at high homologous temperature	23

2.3	Damage formation and cracks	25

2.3.1	Types of damage	25

2.3.2	Factors affecting damage and crack formation	28

2.3.2.1	Conditions and modes of deformation	28

2.3.2.2	Effect of the microstructure on damage formation	30

2.4	Microstructure-based damage modelling	32

2.5	Mechanical Testing: damage generation	35

2.6	Experimental techniques for strain measurements and damage observation at the scale of microstructures	37

2.7	Summary	40

3	Experimental Procedures	42

3.1	Machines and Specimen Designs	42

3.1.1	Introduction	42

3.1.1.1	Finite Element modelling for specimen design	42

3.1.2	Hot compression test in air	45

3.1.2.1	Thermo-Mechanical Compressions machine (TMC)	45

3.1.2.2	Specimen design for TMC machine	46

3.1.3	Hot compression test under vacuum	53

3.1.3.1	Gleeble machine	53

3.1.3.2	Specimen design for Gleeble machine	54

3.1.4	Room temperature in-situ tensile testing	57

3.1.4.1	Deben Tensile machine	57

3.1.4.2	Specimen design for Deben Tensile machine	58

3.2	Materials, Sample preparation, Test conditions, and Strain measurement	61

3.2.1	Materials	61

3.2.1.1	Microstructure	63

3.2.2	Sample preparation and test conditions	64

3.2.2.1	Microgrids	65

3.2.2.2	Plane Strain Compression test using TMC	69

3.2.2.3	Compression test in Gleeble machine	71

3.2.2.4	Micro-DIC coupled Tensile test in Deben machine	72

3.2.3	Strain measurement	74

3.2.3.1	Microgrid	74

3.2.3.2	DIC	75

4	Results	77

4.1	TMC Test Results	77

4.1.1	Stress/strain curves	77

4.1.2	Microgrid results	79

4.1.2.1	Fe-30wt%Ni	79

4.1.2.2	Fe-30wt%Ni+S	83

4.1.2.3	Modified compression specimen	84

4.1.3	Summary	86

4.2	Gleeble Compression Test Results	87

4.2.1	Stress/strain Curves	87

4.2.1.1	Thermal etching	88

4.2.2	Observation in FCS	91

4.2.2.1	Microstructure observation in FCS after deformation at high temperature	96

4.2.2.2	Microstructure observation for the simulation alloys deformed at 1000⁰C	102

4.2.3	FE simulation validation through strain measurements	104

4.2.4	Local Strain analysis at the microstructural scale	107

4.2.4.1	Fe-30wt%Ni +S	107

4.2.4.2	FCS	114

4.2.4.3	Fe-30wt%Ni	116

4.2.5	Multiple-pass test	123

4.2.6	Microgrid error analysis	125

4.2.7	Subsurface damage development in FCS at 1000⁰C	129

4.2.8	Summary	134

4.3	Room temperature micro- tensile test results	135

4.3.1	Stress/ strain curves	135

4.3.2	Deformation comparison between the simulation alloys and FCS	137

4.3.3	Summary	148

5	Discussions	149

5.1	Mechanical testing procedure	149

5.2	Local Deformation	150

5.3	Damage mechanisms	153

5.4	Summary	160

6	Conclusions and Future Work	161

6.1	Conclusions	161

6.2	Future work	164

7	References	166

8	Appendix	172

8.1	.Data	172

8.1.1	TMC data correction	172

8.1.1.1	Origin correction	172

8.1.1.2	Compliance correction	173

8.1.1.3	Breadth spreading correction	173

8.1.1.4	Friction correction	174

8.1.1.5	Stress and strain value calculated	174

8.1.2	Stress/ strain curves obtained from Gleeble machine	175

8.2	Deformed specimens	176

8.3	Heat treatments	177

8.4	Grinding and polishing	177

8.5	Etching conditions	178

8.5.1	Chemical etching of Fe-30wt%Ni+S	178

8.6	Microgrid	179

8.7	Microgrid after test	180

List of Figures

Figure 1.1 Yearly steel production [1]	18

Figure 1.2 a) Hot rolled steel during the industrial process and b) end product with edge cracks	19

Figure 1.3 Mechanisms of chip formation during machining of FCS [7]	20

Figure 2.1 Grains sizes of an austenitic steel corresponded to applied strains [17]	23

Figure 2.2 (a) Microstructure and its corresponding material properties (b) Phase diagram of steel [16]	24

Figure 2.3 (a) Microstructure during hot rolling [16] (b) Interference micrograph of thermal etched alloy [22]	24

Figure 2.4 The three stages in damage development [12]	25

Figure 2.5 a) Macro damage coalescence and b) damage cavity initiation in Ti-6Al-4V located at the grain boundary after high temperature tensile deformation [35]	27

Figure 2.6 Observed damages and cracks generated by (a) low (0.1s-1)  and high (10 s27) strain rate deformation at 1000⁰C [37]	27

Figure 2.7 Cross-sectional view of billet during hot rolling [20]	28

Figure 2.8 a) simulation of hot rolled steel b) strains to rupture graph against stress triaxiality [18]	29

Figure 2.9 a) Stress triaxiality map over given specimen designs b) temperature and stress triaxiality effects towards modes of damage [11]	30

Figure 2.10 Hot damage formation in 316LN stainless steel [52]	31

Figure 2.11 Energy-Dispersive X-ray (EDX) analysis of cross-sectioned FCS [56]	32

Figure 2.12 a) Simulation model of inclusion and steel matrix b) Simulated equivalent strain distribution in steel matrix [57]	32

Figure 2.13 Simulated strain distribution with appearance of voids [59]	33

Figure 2.14 a) Simulated strain distribution of inclusions and steel matrix [15] b) Simulated stress distribution of inclusions and steel matrix [12]	33

Figure 2.15 a) 3-D simulation of inclusions and steel matrix b) 3-D simulation of damage formation between inclusions [56]	34

Figure 2.16 Simulation results with strain distributions predicted by a model with a) GBM and b) NGBM [60]	34

Figure 2.17 a) Simulation of tensile specimen with unique stress triaxiality b) Stress triaxiality effect on strain to fracture and mode of fracture [51]	36

Figure 2.18 a) Revised compressive specimen b) 2-D illustration of revised compressive specimen [10]	36

Figure 2.19 a) Compressed specimen and cross-sectional area b) Microstructure of cross-sectioned specimen [10]	37

Figure 2.20 a) Dimension of revised compressive specimen b) Simulation model of revised compressive specimen [18]	37

Figure 2.21 3-D X-ray tomography of FCS during hot tensile test [54]	38

Figure 2.22 3-D X-ray tomography of FCS in damage development [54]	39

Figure 3.1 a) First iteration b) Second iteration in an increment [89]	43

Figure 3.2 a)Stress strain curves of FCS at 1000⁰C at various strain rates and [90] b) 1/8 of PSC specimen in contact with tools (rigid body) with boundaries conditions	44

Figure 3.3 Different views of the Thermo-Mechanical Compression machine: a)Front view; b) side view of the robot which drives the specimen; and c) control unit	46

Figure 3.4 Dimensions of PSC specimen	47

Figure 3.5 PSC specimen model before and after deformation (von Mises stress in MPa)	47

Figure 3.6 Stress triaxiality from the edge to the centre of the PSC specimen	47

Figure 3.7 a) Dimensions of PSC specimen with square slot for microgrids inserts (samples) [94] b) welding of microgrids inserts into PSC specimen	48

Figure 3.8 Dimensions of PSC specimen with taper of 45⁰	48

Figure 3.9 Tapered PSC specimen model before and after deformation (von Mises stress in MPa)	49

Figure 3.10 Stress triaxiality from the edge to the centre of the tapered PSC specimen	49

Figure 3.11 Dimensions of modified taper specimen	50

Figure 3.12 Modified tapered PSC specimen model before and after deformation (von Mises stress in MPa)	50

Figure 3.13 Stress triaxiality from the edge to the centre of the modified taper PSC specimen	51

Figure 3.14 a) Dimensions of modified specimen and b) exploded view of specimen with inserts [90]	51

Figure 3.15 From left to right: PSC, Tapered PSC, Revised tapered PSC specimens [90]	52

Figure 3.16 Comparisons of stress triaxiality from the edge of three specimens	52

Figure 3.17 Gleeble machine model:3800	53

Figure 3.18 Resultant force directions due to applied force of a) rolling b) compression and c) dimensions of the Gleeble specimen	54

Figure 3.19 Simulated Gleeble specimen a) undeformed b)deformed with desired stress triaxiality highlighted c) plane view with equivalent strain d) plane view with desired stress triaxiality highlighted e) section with desired stress triaxiality highlighted and f) close-up view of the same section with desired stress triaxiality highlighted	55

Figure 3.20 Simulated Gleeble specimen deformed by 75% a) plane view with equivalent strains b) plane view with desired stress triaxiality highlighted c) section with desired stress triaxiality highlighted and d) close view of the same section with desired stress triaxiality highlighted	56

Figure 3.21 a) Deben tensile machine b) Tensile machine inserted into the SEM	57

Figure 3.22 a) Dimensions of tensile specimen based on US tensile test standard b) 1/8th of simulation model	58

Figure 3.23 Equivalent stress (MPa) distribution along the tensile specimen with a geometry based on US standards	59

Figure 3.24 a) Dimensions of revised tensile specimen b) simulation model with equivalent stress (MPa) distribution	60

Figure 3.25 Inclusions found in a) Fe-30wt%Ni+S and b) FCS	62

Figure 3.26 a) Various types of inclusions and b) effect of the composition on types of inclusions formed [7]	62

Figure 3.27 Microstructure of FCS a) Pearlite, Ferrite and inclusions b) Pearlite	63

Figure 3.28 Composition of a) inclusions and b) inclusions with lead	63

Figure 3.29 a) Microstructure of Fe-30wt%Ni b) Inclusions distribution in Fe-30wt%Ni+0.3wt%S	64

Figure 3.30 Resin application machine a) overall view b)rotational disc with sample holder	65

Figure 3.31 SEM: Philips 500 a) SEM control panel with NPGS system b) Microscope components	66

Figure 3.32 Burnt resin removed	67

Figure 3.33 Sputtering machine: Emscope SC500	67

Figure 3.34 a) Ultrasonic bath b) Specimen with gold microgrid	68

Figure 3.35 a) Deposited resin exposed to electron beam, b) irradiated resin is removed, c) overlaying gold on the area d) gold microgrid appears after remaining resin is removed	68

Figure 3.36 a) Inserts with deposited gold microgrid b) assembly of microgrid insert into the PSC specimen	69

Figure 3.37 a) Asymmetric view and b) plane view of specimen and TMC machine's tools c) Deformed PSC specimen and extraction of the microgrid inserts	70

Figure 3.38 a) Fe-30wt%Ni+S with inserts welded b) revised inserts holder	70

Figure 3.39 Modified compression specimen a) Exploded view of specimen with inserts [90] b) Components welded together	71

Figure 3.40 a) Microgrid deposited onto a Gleeble specimen b) deformed Gleeble specimen	71

Figure 3.41 Tensile test a) with optical camera d) DIC measured strain on tensile specimen	72

Figure 3.42 Tensile specimens a) regular size b) revised	72

Figure 3.43 a) Tensile specimen fit onto a tensile machine b) Deben tensile machine	73

Figure 3.44 Gauge length of the tensile specimen with close-up view of the selected area of interest at higher magnification	73

Figure 3.45 (a,b) Schematic of the deformed and undeformed configurations, respectively, of a single microgrid square, showing the vectors used for the determination of the deformation gradient tensor.	75

Figure 4.1 Stress/strain curves at 800⁰C	78

Figure 4.2 Stress/strain curves at 1000⁰C	78

Figure 4.3 Stress/strain curves at 1200⁰C	79

Figure 4.4 a) Deformed Fe-30wt%Ni PSC specimen b) Deformed PSC specimen and extraction of the microgrid inserts	80

Figure 4.5 Deformed Fe-30wt%Ni microstructure a) secondary electrons imaging and b) backscattered electrons imaging of the same area	81

Figure 4.6 Deformed microstructure with measured compressive strain	82

Figure 4.7 Un-deformed microstructure and deformed microstructure of Fe-30wt%Ni	83

Figure 4.8 Strain-yy map over the un-deformed microstructure of Fe-30wt%Ni a) without interpolation b) with interpolation	83

Figure 4.9 Fe-30wt%Ni +S with microgrid a) before test b) after test	84

Figure 4.10 2.5 micron pitch size microgrid a) 4 sets b) close view of microgrids	84

Figure 4.11 Modified compressive specimen after deformation	85

Figure 4.12 a) Insert of revised compressive specimen b) oxide scale formed	85

Figure 4.13 Stress strain curves of FCS, Fe-30wt%Ni , Fe-30wt%Ni +S at 1000⁰C	88

Figure 4.14 Stress strain curve of FCS deformed at 850⁰C	88

Figure 4.15 Fe-30wt%Ni+S a) before thermal etching b) after thermal etching	89

Figure 4.16 Thermal etched Fe-30wt%Ni +S a) voids around inclusions b) crack along grain boundaries	90

Figure 4.17 Thermal etched FCS	91

Figure 4.18 FCS with deposited microgrids a) before b) after the test at 850⁰C	92

Figure 4.19 FCS with deposited microgrids a) before b) after test at 1000⁰C	92

Figure 4.20 a) Grid length measurements of an un-deformed inclusion and b) Grid length measurements of the same deformed inclusion	93

Figure 4.21 a) Rotation of the inclusion due to the plastic deformation of the matrix and b) path of the matrix deformation	94

Figure 4.22 Microstructure of FCS at the centre of the deformed specimen	95

Figure 4.23 20 micron pitch microgrid after deformation at 850⁰C on FCS	96

Figure 4.24 Microstructure of FCS after deformation at 1000⁰C  a) within the deformation zone, b) in the un-deformed area (thermally etched only) of the specimen and c) global view of the specimen	97

Figure 4.25 Microstructure of FCS after deformation at 1000⁰C  a) voids around inclusions and b) crack propagation along grain boundaries affected by voids around inclusions	98

Figure 4.26 Microstructure of FCS after deformation at 1000⁰C	99

Figure 4.27 Microstructure of FCS: a) Thermal etched Phase 2, b) chemically etched FCS and c) thermal etched Phase 1	99

Figure 4.28 Microstructure of FCS a) before the test with Pearlite highlighted and b) after the test at 850⁰C	100

Figure 4.29 Microstructure of FCS after the test at 1000⁰C with the highlighted region where major cracks are observed	100

Figure 4.30 Microstructure of FCS a) before and b) after an applied strain of 25% at 850⁰C, c) close-up view of an un-transformed region after deformation at 850⁰C, (d) large deformation bands in the transformed regions and e) FCS deformed at 1000⁰C	102

Figure 4.31 Microstructure of Fe-30wt%Ni after the test at 1000⁰C	103

Figure 4.32 Microstructure of deformed Fe-30wt%Ni +S after the test at 1000⁰C with a) an uniform slip system orientation and b) with different slips system orientations across a grain boundary	104

Figure 4.33 Microgrids over the deformed Fe-30wt%Ni  with highlighted macrogrids	105

Figure 4.34 a) Global view of the specimen, b) equivalent strain distribution after 25% applied strain measured using microgrids and c) predicted by the FE simulation	106

Figure 4.35 a) Simulation model superimposed onto a micrograph of the deformed sample with b) local microgrids before deformation and c) after deformation with their respective close up views in d) and e)	108

Figure 4.36 Simulation results of a deformed Gleeble specimen with a) full specimen and b) plane view of the sectioned Gleeble specimen with positive and negative Strain-zz highlighted	109

Figure 4.37 a) Simulated stress triaxiality superimposed onto the photomicrograph b) microgrid over inclusions cluster in Fe-30wt%Ni+S	110

Figure 4.38 Equivalent strain map over the area of the microstructure a) without voids exclusion and b) with voids exclusion in strain measurement	111

Figure 4.39 a) Original micrograph of an inclusion cluster in Fe-30wt%Ni+S, b) after thresholding and c) final processed micrograph	112

Figure 4.40 a) Processed micrograph of inclusion cluster in Fe-30wt%Ni+S with b) change of resolution, c) identification of inclusions location, d) processed inclusions location superimposed to original micrograph,  e) superimposition of equivalent strain distribution values and f) transformed image with selected inclusions within white squares and red squares considered as inclusions surrounding	113

Figure 4.41 Histogram of equivalent strain in the austenitic phase around and away from the inclusions	113

Figure 4.42 Measured equivalent strain distribution over the Fe-30wt%Ni+S microstructure with a) a microgrid pitch size of 12.5microns and b) a microgrid pitch size of 2.5 microns	114

Figure 4.43 FCS deformed at 850⁰C: a) effect of inclusions on strain localisation highlighted with red arrows, b) phase transformed regions with high strain localisation highlighted with yellow arrows, c) equivalent strain map plotted over the FCS microstructure and d) regions with and without phase transformation for the 2.5 micron grid	116

Figure 4.44 a) Simulated strain-yy with two regions highlighted (A and B),  b) simulated stress triaxiality, c) micrograph of deformed microgrid in region A and d) experimentally measured strain-yy distribution over the deformed microstructure in region A	117

Figure 4.45 Histograms of a) strain-yy distribution, b) strain-xx distribution c) strain-zz distribution d) Strain-zz over region A	119

Figure 4.46 a) Micrograph of deformed microgrid in region B and b) experimental strain-yy distribution over region B with region C highlighted	120

Figure 4.47 Secondary electron image of Region C	120

Figure 4.48 a) Secondary image of Fe-30wt%Ni after deformation at 1000⁰C with b) its location with respect to the deformed zone in the FE model, c) strain-yy map  and d) strain-xx over an area of 16 mm2	122

Figure 4.49 Two-pass compression test on Fe-30wt%Ni : a) deformed microstructure after first pass (25% applied strain) b) secondary image of the same area of the microstructure after the second pass (15% additional applied strain and c)  backscattered image after the second pass	124

Figure 4.50 Initial grids length measurement of a) one grid b) 7grids	125

Figure 4.51 Microgrid intersection points with precision error	126

Figure 4.52 Undeformed microgrid	126

Figure 4.53 Error map a) XX component b) YY component c) equivalent strain	128

Figure 4.54 Sectioning of deformed Gleeble specimens	129

Figure 4.55 Inclusions in FCS at a) the centre of the specimen and b) at the subsurface	130

Figure 4.56 Microstructure of FCS at the centre of the (ND,TD) plane	130

Figure 4.57 a) Microstructure of FCS at the subsurface and b) close-up view of damage propagating along grain boundaries	131

Figure 4.58 a) Damage away from the specimen’s surface for FCS b) evidence of the influence of  inclusions on intragranular cracking	132

Figure 4.59 a) Distance from the surface where damage can be found in FCS deformed at 1000⁰C b) stress triaxiality distribution at the subsurface with c) close-up view	133

Figure 4.60 Force against extension for FCS deformed up to fracture using tensile testing in the SEM	135

Figure 4.61 Stress strain curves of the three materials	137

Figure 4.62 Micrograph of tensile specimens before failure	138

Figure 4.63 Micrograph of FCS a) before deformation and b) close to failure	139

Figure 4.64 Progressive deformation of Fe-30wt%Ni	139

Figure 4.65 Progressive deformation of region A in Fe-30wt%Ni	140

Figure 4.66 Progressive deformation and damage found in Fe-30wt%Ni +S	140

Figure 4.67 Inclusions before and after deformation in FCS	141

Figure 4.68 a) Damage formation around inclusions in FCS b) Measured local strain right before damage formed in FCS c) Measured local strain right before damage formed in Fe-30wt%Ni+S	141

Figure 4.69 The development of local shear band in between inclusions in FCS	141

Figure 4.70 a) FCS microstructure before fracture  b) failure cracks after propagation in the same region	142

Figure 4.71 Strain-yy distribution across the microstructure of FCS	143

Figure 4.72 Progressive local deformation of FCS	143

Figure 4.73 Etched FCS with microgrid a) before deformation and b) after deformation up to the UTS	144

Figure 4.74 Force-extension curve for FCS showing the regular intervals to take images for DIC analysis	144

Figure 4.75 Strain-yy map measured by a) DIC b) Microgrid	145

Figure 4.76 Process for digitally separating the 3 phases of FCS: a) original micrograph of the microstructure, b) Ferrite in white, c) inclusions and d) Pearlite	146

Figure 4.77 a) Strain-yy map  superimposed onto the filtered micrograph, b) strain histogram of each phase using DIC, c) manual phase separation with pearlite and inclusions highlighted  and d) strain histogram of each phase using microgrids	148

Figure 5.1 Coalescence of damage between inclusions at a) 850⁰C and b) room temperature	156

Figure 5.2 FCS a) before and b) after deformation with c) observed shear bands at room temperature. FCS d) before and e) after deformation with f) observed shear bands at 850⁰C	159

Figure 5.3 FCS microstructure deformed at a) room temperature, b) 850⁰C and c) 1000⁰C	159

Figure 5.4 a) Schematic of damage mechanism observed in this work at 1000oC at the surface and subsurface with references b) [22] c) [42] d) [56] e) [10] f)[54]	160

Figure 8.1 Load against displacement graph of raw data from TMC	172

Figure 8.2 Load against displacement graph with origin correction	173

Figure 8.3 Load against displacement graph with compliance correction	173

Figure 8.4 Stress against strain graph with strain rate	175

Figure 8.5 Stress strain curves of FCS, Fe-30wt%Ni+S and Fe-30wt%Ni	176

Figure 8.6 Stress strain curves of FCS at 850⁰C	176

Figure 8.7 a) Inserts welded into the PSC holder b) fail test specimen c) deformed specimen	177

Figure 8.8 Microstructure of Fe-30wt%Ni after heat treated for a) 10mins b) 15mins c) 20mins	177

Figure 8.9 Fe-30wt%Ni surface with a) poor polishing and etching b) improved polishing but poor etching c) well-polished and right etching condition	178

Figure 8.10 Microstructure of Fe-30wt%Ni after a) dip in solution for 45s b) pour solution on top of specimen surface c) wipe specimen’s surface with solution wetted cotton	178

Figure 8.11 Chemically etched Fe-30wt%Ni+S	179

Figure 8.12 a) Detached resin from the surface b) un-even microgrid c) resin removal from the surface	179

Figure 8.13 a) Microdots b) partially distributed microgrids c) resin trapped under gold layer	180

Figure 8.14 Microgird on Fe-30wt%Ni after test at 1200⁰C a) secondary electron signal imaging b) backscattered electron signal imaging	180

Figure 8.15 Fe-30wt%Ni after test at 1000⁰C a) test 1 b) test 2	181

Figure 8.16 Fe-30wt%Ni+S after test at 1000⁰C a) test 1 b) test 2	181

Nomenclature

FCS		Free Cutting Steel

DIC		Digital Image Correlation

TMC		Thermo-Mechanical Compression

LAP		Low As Possible

MnS		Manganese Sulphide

Bi-S		Bismuth Sulphide

Fe		Iron

Ni		Nickel

T		Temperature

Tm		Melting Temperature

Wt%		Weight Percentage

FE		Finite element

FEA		Finite Element Analysis

ε		Strain rate (s-1)

s		Stress (MPa)

ECT		Equicohesive Temperature

EDX 		Energy-dispersive X-ray

SEM		Scanning Electron Microscope

PSC		Plane Strain Compression

FTTU 		Fast Thermal Treatment Unit

PMMA	Polymethyl Methacrylate

RD		Rolling Direction

TD		Transverse Direction

ND		Normal Direction

F		Force (N)

A		Cross-sectional Area (mm2)

L		Length (mm)

HfO2		Hafnium Oxide

F		Deformation Gradient Tensor

V, v		Vectors

e		Strain

eq		Equaivalent

log		True Strain

x		Elongation/displacement (mm)

E		Young’s Modulus (GPa)

K		Stiffness (N/mm)

m		Graph gradient

τ		Shear Stress (MPa)

UTS		Ultimate Tensile Strength (MPa)

Chapter 1

# Introduction

## Engineering context and project driving force

Each year, millions of tonnes of steel are produced with continuous growth as shown in Figure 1.1 [1].

Figure 1.1 Yearly steel production [1]

For centuries, steel has been a popular choice for many applications partly because of its durability and relatively low cost. Table 1.1 shows the relatively low cost of steel compared to other materials in 2014 [2]. A major reason behind such competitive price for steel is the abundance of iron in the earth, as its main chemical component.

| Material | Steel | Aluminium | Copper | Zinc | Lead | Nickel | Magnesium | Tin |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Approximate relative cost | 1.0 | 2.5 | 8.5 | 2.9 | 2.5 | 20.6 | 6.4 | 25.8 |

Table 1.1 Relative cost of materials [2]

Another reason for the popularity of steel is the flexibility with which its properties can be changed through controlled manufacturing processes. These properties are determined by the microstructure of the material which can be changed by varying its chemical composition (e.g. carbon content) and controlling parameters of the manufacturing process (e.g. temperature and deformation conditions) [3].

Rolling is one of the most effective manufacturing processes to produce steels with desired properties through controlled thermo-mechanical processing [4]. Hot rolling (Figure 1.2 a), is usually used in the early stages of the forming process to apply large reduction ratios and to breakdown the cast microstructure of an ingot. Although hot rolling is successful in enhancing the properties of steel by refining its microstructure, defects such as inhomogeneous microstructure, zipper cracks in the centre of the rolled product and edge cracking (Figure 1.2 b) are commonly found [5, 6]. Such problems require further processing which in turn add to the production cost.

Figure 1.2 a) Hot rolled steel during the industrial process and b) end product with edge cracks

One of the most sought after steels in the automotive industry, especially of great interest for Tata Steel, is free-machining or free-cutting steel (FCS). This steel is highly valued for its machinability as the alloy can be machined relatively easily without generating too much damage to the tools. Sulphur additions in such steel react with manganese to form manganese sulphide (MnS) which then appears as non-metallic inclusions. These inclusions not only act as a catalyst in increasing the steel’s machinability by boosting chip formation as shown in Figure 1.3 [7], they also serve as a dry lubricant [8]. Additionally, bismuth, tellurium and lead are often added during casting to form internal lubricants in FCS [9].

Figure 1.3 Mechanisms of chip formation during machining of FCS [7]

Surface defects and especially edge cracking is commonly observed during the hot rolling process of FCS. Previous studies [10-15] suggest that edge cracking is influenced by both the levels of stress triaxiality (mean stress over equivalent stress) experienced by the material during the hot rolling process and the inhomogeneities of the microstructure, especially MnS inclusions. However, the damage mechanisms responsible for edge cracking are still poorly understood and novel approaches are needed to generate more physical understanding of the deformation process leading to damage at the scale of the microstructure.

## Aim and objectives of the research

The aim of this work is to generate new insight into the formation of damage under thermo-mechanical conditions similar to those leading to edge cracking in FCS during industrial hot rolling.

To achieve this, laboratory tests will be designed to simulate such conditions in a controlled manner with observations of the microstructure after the test. Damage formation will be studied by analysing the way the applied deformation localises in the microstructure of the material. A new experimental procedure will therefore be developed to quantify strain distributions at the grain scale and at high homologous temperatures. Further information about the evolution of the damage process will also be studied as well as the effect of temperature on local deformation and damage at the scale of the microstructure by conducting in-situ mechanical testing inside the chamber of a scanning electron microscope (SEM).

## Outline of Thesis

Chapter 2 reports the literature review which starts with generic information about industrial rolling and the main parameters controlling the process. This is followed by a review of microstructure evolution during rolling and the various types of damage found under hot deformation conditions. Potential factors responsible for hot damage formation are then presented. Lastly, results from experimental investigations related to mechanical testing for damage generation at high temperature and available characterisation techniques within the field of hot damage are reviewed.

Chapter 3 presents the experimental procedures developed in this work starting with  the variety of test machines used to study damage formation over a range of temperatures. This chapter includes a large section on finite element modelling used to design very specific specimen geometries necessary to generate the required levels of stress triaxiality representative of hot rolling conditions leading to edge cracking. Results from these computer simulations are also presented. This chapter also includes procedures involved for sample preparation, applied test conditions, and strain measurement techniques namely microgrid and Digital Image Correlation (DIC).

Chapter 4 is broken down into 3 sub-chapters to report the experimental results obtained from the various tests. Results are analysed in relation to damage formation from different perspectives and for different deformation and temperature conditions.

Chapter 5 discusses the effect of local deformation on damage formation within the investigated materials at various temperatures in relation to published results from the literature.

Chapter 6 concludes the work done in this study with a summary of the main results and analysis carried out to provide new insight into damage development in FCS. The chapter ends with suggestions for future work.

The Appendix consists of details of processing procedures of data collected from the TMC machine, challenges faced in sample preparations (failed microgrid, failed specimens), heat treatments trials, examples of sample polishing, trials for etching conditions, and damaged test specimens (due to oxidation).

Chapter 2

# Literature Review

## Rolling process

Rolling is the most widely used metalworking process [4, 16] because of its high production rate and a close control of the end product. It is a solid-state forming operation where material properties can be tailored by controlling the thermo-mechanical process. This process involves passing working materials between rolls and a reduction in their cross sectional area through compressive stresses which can be repeated in multiple passes at different rates and at varied temperature ranges.

Parameters in the rolling processes such as temperatures, applied strains, and strain rates have crucial effects on the end product.

There are three ranges of temperature for the rolling process which depend on the melting temperature of the working material, Tm. Firstly, cold rolling where a material is deformed at temperatures less than 30% of Tm. It is usually applied onto hot rolled material to enhance its strength with a good surface finish of the end product. Secondly, warm rolling is when operation temperature ranges between 30-70% of Tm. Finally, hot rolling is where rolling takes place at temperatures above 70% of Tm. The high temperatures will soften the worked piece and thus, enhance its workability. Hot rolling is commonly used to deform as-cast material, which has a dendritic structure and non-uniform grain sizes, in a primary roughing mill. A wrought structure with finer grain size and reduced porosity is created as a result [11]. However, hot rolling also produces poor surface finish due to the heat involved which commonly leads to oxidation of the surface.

The amount of applied compression has a direct impact on the microstructure that develops in the worked piece during rolling as shown in Figure 2.1 [17]. For instance, 5% reduction gives smaller grains size compared to a specimen without deformation. Likewise, a 75% reduction generates much finer grain sizes with high strength compared to the less deformed material. The applied strain is determined based on the desired properties of the end product as well as its formability- the ability to undergo plastic deformation before damage is formed.

Figure 2.1 Grains sizes of an austenitic steel corresponded to applied strains [17]

Strain rate is the time rate of change in the gradient of deformation. The increased strain rate has an adverse effect on material properties [11] with the flow stress of the metal increasing with strain rate. In practice, strain rates vary significantly during a rolling operation from 0.1 to 10 s-1 [18] based on process requirements. The roughing rolling process, as an early stage of a rolling operation used to transform an as-cast ingot into a rolled billet, has generally lower strain rates ranging from 0.1 to 5 s-1.

## Microstructure evolution at high homologous temperature

Due to the heat involved (850-1200⁰C for FCS) in hot rolling, steels do not just experience deformation but also microstructure evolution namely, recovery, recrystallization, grain growth and phase transformation. Recovery is a process whereby the deformed grains reduce their stored energy through the rearrangement of dislocations at high temperature. Recrystallisation is formation of new grain structures and these grains will increase in size as time progresses (grain growth) provided that high temperature is maintained. In general, bigger grain size will reduce the strength and hardness of a steel while increasing its ductility as shown in Figure 2.2 a [16]. Finally, phase transformation is the alteration in the number and character of phases that constitute the microstructure of the alloy. It is a process that depends on material composition, deformation temperatures or heat treatments applied to the material. Figure 2.2 b is a phase diagram of steel based on the temperature and composition namely wt% of Carbon.

Figure 2.2 (a) Microstructure and its corresponding material properties (b) Phase diagram of steel [16]

Besides the microstructure evolution at high temperature as shown in Figure 2.3 a [16], oxide scales can be formed at the surfaces of hot rolled steels due to the heat and air exposure. Such oxide scale can penetrate into the hot rolled steel and be responsible for surface roughness or damage [18-20]. On the other hand, if a hot surface is protected using an inert atmosphere, thermal etching can take place [21]. Thermal-etching reveals prior-austenite grain boundaries which are made visible at room temperature. Such effect was previously studied on a thermally etched Cu-3 wt% Sb alloy through an interference micrograph [22] as shown in Figure 2.3 b. Results show that line tensions are concentrated along grain boundaries which indicate high energy boundaries as supported by Cho and Szpunar [23].

Figure 2.3 (a) Microstructure during hot rolling [16] (b) Interference micrograph of thermal etched alloy [22]

## Damage formation and cracks

Material processing such as hot rolling, induce large plastic deformation which can lead to the enhancement of material properties but, on the other hand, can also lead to damage formation if not controlled.  Micro voids or cracks can nucleate, grow within a material and eventually coalesce to form macro cracks that lead to material failure [24].

Maire et al. [25] describes damage as the appearance of new surface in a material. However, damage can also be a result of the development of pre-existing voids or defects within a material. Therefore, Foster et al. [12] defines it as: The creation and enlargement of internal cavities within a material.

Crack formation includes successive steps of nucleation, growth and coalescence of damage [24, 26, 27] which has been presented by Foster et al. [12] in Figure 2.4. It shows that crucial cracks are formed from micro damage sites at the scale of microstructure which need to be carefully studied.

Figure 2.4 The three stages in damage development [12]

### Types of damage

There are various types of damage which can be generated due to environmental factors, applied strain, microstructure behaviour, mode of deformation, etc. The understanding of the following damage types can be helpful in studying hot damage formation in FCS.

Firstly, creep type damage is formed when a component is subjected to a load over a prolonged period of time (Low strain rate,  ε<1x10-4s-1) and experiences permanent plastic deformation. Creep is a well-known problem associated with high temperature (T>0.6Tm) but, it can occur under low temperature condition if the stress state is high [28]. Ashby and Dyson [29] suggest that creep damage can been categorised into 4 categories: Loss of external section (shape change), degradation of microstructure (e.g. precipitation coarsening), interaction with the environment (e.g. oxidation), and loss of internal section (voiding or cracking).

Superplastic type damage is normally found in extremely ductile materials subjected to high strain [30] especially during warm or hot deformation (T>0.5Tm) conditions. During deformation, grains remain equi-axed and plastic deformation takes place through grain boundaries sliding and grain rotation. Damage occurs when there is a mismatch between interacting grains. When two neighbouring grains interact, some accommodation is required near grain boundaries for grains to keep in contact [31, 32]. Failure in accommodating this process where stress near grain boundaries cannot be relieved will cause void formation. Cheong [31] claimed that there are similarities between creep and superplastic deformation.

Hot working damage (T>0.6Tm) can occur in two forms: along grain boundaries and around non-metallic particles, namely inclusions. Damage along grain boundaries is associated with high mobility of grain boundaries typical for creep and superplastic type of damage [33, 34] as shown in Figure 2.5 a and Figure 2.5 b [35]. On the other hand, hot damage can also be associated with inclusions or point defects [15, 34, 36]. Liu et al.  [37] suggests that strain rate will affect the type of hot working damage: low strain rate ( ε≈1x10-1s-1) will generate more damage along grain boundaries as shown in Figure 2.6 a while high strain rate ( ε>1x10-1s-1)  will generate damage around inclusions as shown in Figure 2.6 b.

Figure 2.5 a) Macro damage coalescence and b) damage cavity initiation in Ti-6Al-4V located at the grain boundary after high temperature tensile deformation [35]

Figure 2.6 Observed damages and cracks generated by (a) low (0.1s-1)  and high (10 s27) strain rate deformation at 1000⁰C [37]

Ductile type damage which mainly occurs during cold working (T<0.3Tm) is associated with point defects within the material such as inclusions and pores. These defects play an important role in concentrating stresses and strains around them which causes localised plastic straining leading to void initiation and growth.  Coalescence of voids will then form macro cracks which lead to material failure [24, 38].

In general, damage formation at high temperature in FCS can be found either around second phase particle (e.g. inclusions) or grain boundaries depending on deformation conditions.

### Factors affecting damage and crack formation

Edge cracking is the most common type of crack found in hot rolled FCS. Hellan [39] describes crack formation as a loss of contact between different parts of a body. There are many factors that influence crack formation, such as temperature, strain rate, material composition, grain size, precipitates, non-metallic inclusions, inhomogeneous texture distribution and prior thermal and mechanical treatments [5, 6, 40-43]. These factors has been categorised into the conditions and modes of deformation and damage in microstructures.

#### Conditions and modes of deformation

Due to the heat involved in hot rolling, oxidation is expected and is one of the important factors influencing surface crack formation [18-20]. However, oxidation does not explain why cracks are formed primarily at the edge of hot rolled steel. Therefore, Kim et al. [20] investigated the penetration path of the oxide scale into Bi-S based FCS. Results show that the oxide scale penetrated into the material through pearlite bands which were formed during the rolling process (along the edge of rolled billet). Such pearlite bands as shown in Figure 2.7 have therefore become preferred paths for oxide scales penetration into the rolled FCS.

Figure 2.7 Cross-sectional view of billet during hot rolling [20]

On the other hand, Duan and Sheppard [44] suggest that friction between the roll and the stock is an important factor for  surface crack formation. This has been confirmed by Xie et al. [45] who claimed that lowering the friction between work piece and rolls lowers the rate of crack initiation and propagation, hence minimising edge cracking. Thomason [46] suggests that zero friction between die and test-piece will lead to no or less crack formation. However in practice, zero friction is unreachable. Therefore, research studies in tribology are trying to minimise friction [45] in rolling.

On the other hand, both Thomson et al. and Schey [47, 48] claimed that edge cracks are caused mainly by limited ductility, uneven deformation during rolling and transverse variations in stresses. These variations in stresses that cause fracture have been represented through a mechanical parameter known as stress triaxiality [49]. Stress triaxiality is the ratio of mean stress over equivalent stress at a given point and characterises the mode of deformation.

Stress Triaxiality= σ1+σ2+σ3312×σ1-σ22+σ2-σ32+σ3-σ12  [50]

Stress triaxiality in hot rolling ranges from -0.4 to 1.6 [11] and Farrugia et al. [18] identified critical stress triaxiality values ranging from 0.3 to 0.5 to cause fracture in steel under minimum strain. Figure 2.8 a demonstrated part of a hot rolled steel simulation and Figure 2.8 b shows a graph of strain values to rupture against stress triaxility.

Figure 2.8 a) simulation of hot rolled steel b) strains to rupture graph against stress triaxiality [18]

Stress triaxiality has been the basis for specific specimen designs used to study experimentally damage formation under conditions representative of hot rolling [11, 12, 18, 34, 51]. Several compression specimens designs were analysed (Figure 2.9 a) by Kaye [11] in relation to stress triaxiality. The effect of stress triaxiality and temperature on the mode of damage and crack formation has been summarised in Figure 2.9 b. Stress triaxiality values ranging from 0 to -0.33 introduced damage through micro-shearing of inclusions within the material. On the other hand, stress triaxiality levels ranging from 0.1 to 0.4 encourage damage formation through void initiation and expansion around inclusions at temperatures ranging from 900⁰C to 1000⁰C. However, for higher temperature ranges, damage mechanisms involving both inclusions and grain boundaries were observed for stress triaxiality values ranging from 0.1 to 0.4.

Figure 2.9 a) Stress triaxiality map over given specimen designs b) temperature and stress triaxiality effects towards modes of damage [11]

#### Effect of the microstructure on damage formation

Microstructure plays a key role on damage formation leading to cracks. The heat involved in hot rolling has not only an effect on microstructure evolution but also affects the mode of failure in the material. The concept of Equicohesive temperature (ECT) [4] was introduced where the strength of grains and grain boundaries are equal at this temperature. In other words, a testing temperature above ECT weakens the grain boundaries and leads to intergranular fracture while a testing temperature below ECT weakens grains and leads to intra-granular fracture. ECT values are dependent on materials and strain rate. Low strain rates are usually associated with low ECTs and therefore the tendency for intergranular fracture increases as reported in [4], which agrees with Liu et al.’s results [37] who found more grain boundary damage at lower strain rates compared to tests conducted at high strain rates.

On the other hand, Xiuzhi et al. [52] suggests that recrystallisation at high temperature has a crucial effect on crack formation. Their results (Figure 2.10) show that crack formation concentrated in a region where rapid recrystallisation took place. However, the fraction of recrystallization reduces from the centre to the surface of a hot rolled billet [44], which suggests that recrystallisation may not have a direct effect on edge cracking.

Figure 2.10 Hot damage formation in 316LN stainless steel [52]

Generally, non-metallic phase particles, or inclusions, are always found to be responsible for damage formation regardless of the temperature range [10, 14, 53-55]. An Energy-Dispersive X-ray (EDX) analysis was done on a cross sectional area of a FCS specimen with an edge crack after deformation above 850⁰C (Figure 2.11) [56]. The result suggests that the distribution of inclusions, shown within the yellow circles in Figure 2.11, plays an important role on damage formation as well as on coalescence between inclusions.

Figure 2.11 Energy-Dispersive X-ray (EDX) analysis of cross-sectioned FCS [56]

## Microstructure-based damage modelling

Inclusions are well-known for acting as damage nucleation sites in a material. Luo et al. [57] modelled the influence of non-metallic inclusions on the plastic deformation of metals. Another study from the same authors analysed the localisation of deformation close to inclusions in hot rolling [58]. Modelling results show the effect of one single inclusion on strain localisation in steel matrix as shown in Figure 2.12 a and b.

Figure 2.12 a) Simulation model of inclusion and steel matrix b) Simulated equivalent strain distribution in steel matrix [57]

The effect of the inclusion on strain localisation was clearly demonstrated while in 2004, Bandstra et al. [59] studied the effect of voids distribution and size on strain localisation in a HY-100 steel. Figure 2.13 shows comparison between uniformly distributed voids and randomly distributed voids which emphasises the significant effect of voids distribution and their sizes on the strain localisation patterns and intensity.

Figure 2.13 Simulated strain distribution with appearance of voids [59]

Farrugia [15] modelled FCS with a cluster of inclusions deformed at high temperature and showed similar strain localisation effects due to inclusion distributions and sizes (Figure 2.14 a).  Foster et al. [12] found that damage growth and coalescence are directly related to inclusion size and distribution as shown in Figure 2.14 b. The ratio of inclusions size to spacing (diameter/spacing) was suggested to be an important parameter governing damage growth and failure in materials.

Figure 2.14 a) Simulated strain distribution of inclusions and steel matrix [15] b) Simulated stress distribution of inclusions and steel matrix [12]

Three-Dimensional models have also been developed to study the effect of inclusions on damage formation [56]. The effect on void growth and coalescence is shown in Figure 2.15 a and b which demonstrated the influence of inclusions on damage coalescence and crack formation.  The formation of cracks at the surface can result from a coalescence effect of voids located at the subsurface, which traditional two-dimensional models cannot predict. Therefore, the development of three-dimensional models can provide better understanding of the physical damage mechanism. The model in Figure 2.15 b was developed to study the coalescence effect of two neighbouring inclusions which can be further developed to study the effect of a cluster of inclusions.

Figure 2.15 a) 3-D simulation of inclusions and steel matrix b) 3-D simulation of damage formation between inclusions [56]

Apart from inclusions, grain boundaries have been shown to be alternative damage nucleation sites for metals deformed at elevated temperatures by Liu et al. [37]. Wu et al. [60] developed a microstructural model to simulate a tensile test conducted at 440⁰C on Al-Cu-Mg alloy. They concluded that a model with grain boundary (GBM) damage shows better agreement with experimental results in terms of strain localisation compared to a model without grain boundaries (NGBM). Figure 2.16 a and b demonstrate the difference in the prediction of shear band locations by considering or not considering grain boundaries in the model.

Figure 2.16 Simulation results with strain distributions predicted by a model with a) GBM and b) NGBM [60]

## Mechanical Testing: damage generation

Mechanical testing is a fundamental way of understanding the behaviour of materials under loading conditions. Local deformation and damage formation during these tests are usually responsible for the observed behaviour. Therefore, essential information from these experiments such as local strain distributions at the scale of the microstructure of the material are required to provide physical insight for the development of reliable simulation models [61]. The study of damage formation as a result of strain localisation can be studied relatively easily at room temperature [62-65]. However, studies conducted at high temperature are much more challenging mainly due to experimental difficulty including equipment reliability [66], complex microstructural evolution of the material [67] and oxidation issues [68].

In order to study edge cracking in hot rolled FCS, the most straight forward test is laboratory hot rolling which has been carried out in several studies [69-71]. Relatively close replication of industrial rolling can be achieved by laboratory rolling mills which give some insight into rolling processes of interest. Cusminsky et al. [72] reported that by adding chamfer angles onto pre-rolled steels, stress states could be controlled and therefore generate desired cracks profiles for their study. However, there is a lack of user control on precise material temperatures, strain rates and strain paths which are usually heterogeneous, hence limited information can be extracted from these tests.

A simple uniaxial tension test is one of the fundamental controlled tests used to study the behaviour of materials. However, ductility in a tensile test is usually limited in comparison to rolling due to the geometry of the specimen, with necking taking place after relatively small strain values. High stress triaxiality levels ranging from 0.33 to 1.5 have been calculated in the necking region of a tensile specimen in [11] with another study showing the effect on stress triaxiality on accelerated failure [26]. Several studies have been carried out to analyse stress triaxiality states in the necking region of standard tensile specimens [26, 37, 73] or tensile specimens modified with single [26, 27] or double notches [74] with different notch radii and their effect on fracture. Bao and Wierzbicki [51] designed a unique specimen geometry to alter stress triaxiality within a tensile specimen as shown in Figure 2.17 a. They successfully demonstrated how stress triaxiality affected the mode of deformation, the mode of failure and the strain to fracture (Figure 2.17 b). It can be observed from the figure that the strain to fracture increases significantly under a shear mode with stress triaxiality values ranging between 0 to -1/3. Gurson [75] agrees that the rate of damage growth and coalescence increases exponentially with an increase in triaxiality.

Figure 2.17 a) Simulation of tensile specimen with unique stress triaxiality b) Stress triaxiality effect on strain to fracture and mode of fracture [51]

Foster et al. [10] suggests that tensile tests only provide limited information about material plasticity and failure, which is not sufficient to understand the damage mechanisms of hot rolled FCS. As a result, a specially designed compressive specimen (Figure 2.18) was made with stress states representative to those found in hot rolled FCS. A chamfer with specific angle was designed for specimens deformed at high temperature.

Figure 2.18 a) Revised compressive specimen b) 2-D illustration of revised compressive specimen [10]

Sectioning and polishing was done on highly compressed specimens to analyse damage mechanisms. Foster et al.’s results from a 1200⁰C compressed FCS suggested that the crack preferably formed around inclusions as shown in Figure 2.19 b

Figure 2.19 a) Compressed specimen and cross-sectional area b) Microstructure of cross-sectioned specimen [10]

Later on, a new designed compressive specimen geometry [18] was developed with tapers at 30⁰ along the sides of the specimen as shown in Figure 2.20 a [18]. This particular geometry creates stress triaxiality levels ranging from 0.3 to 0.5 that promote damage formation on the surface of the specimen when subjected to compression. Such new design has a key advantage over the previous design because the area of interest is located at the surface and therefore, no sectioning of the specimen is required after the test. Compression tests were conducted using this geometry at relatively high temperature (up to 1200⁰C) using a Gleeble machine.

Figure 2.20 a) Dimension of revised compressive specimen b) Simulation model of revised compressive specimen [18]

## Experimental techniques for strain measurements and damage observation at the scale of microstructures

Damage initiated at the scale of microstructures can neither be explained nor studied using macroscopic scale theories or observations [55, 76]. Kachanov [77], in 1958, was the first to investigate and model damage at the microscopic scale [12], while Nicholson et al. [78] started to observe coalescing voids in steels. Baker and Charles [79] later showed damage nucleation around MnS inclusions during hot rolling using optical techniques. As technology moved forward, equipment such as Scanning Electron Microscopy (SEM), Energy Dispersive X-ray (EDX) and Wavelength Dispersive X-ray (WDX) were introduced to analyse the microstructure and local chemical composition of materials and their effect on damage nucleation and coalescence [69]. However, these methods are usually destructive and require sectioning of the test piece, which might affect test results [11]. X-ray tomography is a relatively recently developed non-destructive technique which allows 3D imaging of internal damages and which can be  coupled with cold tensile test to obtain in situ damage development in metals [25]. As this technique developed further, Puncreobutr et al. [54] managed to run a X-ray tomography coupled tensile test at temperature as high as 1000⁰C in 2012 up to failure. Without the need for sectioning the test specimen or further material processing after the test, Puncreobutr et al. [54] demonstrates the direct connection between inclusions and damage coalescence at subsurface of a free cutting steel under high temperature tensile test as shown in Figure 2.21 and Figure 2.22. Several studies including Puncreobutr et al. [10, 14, 53-55] identify inclusions as the most important factor to damage formation and crack propagation.

Figure 2.21 3-D X-ray tomography of FCS during hot tensile test [54]

Figure 2.22 3-D X-ray tomography of FCS in damage development [54]

Damage is initiated as a result of the deformation of microstructures during testing. Strain measurements at that scale therefore represent invaluable physical insight into the development of damage in materials. Digital Image Correlation (DIC) is a modern technique which is now commonly used for full-field strain measurements. The technique is most commonly used in combination with optical cameras for strain measurement on specimen’s surface during mechanical testing. Advances in imaging technologies namely high image acquisition speed and high resolution cameras have improved the quality of strain measurements provided by the DIC technique dramatically. DIC has been used in various studies with mechanical testing [63, 64, 80] and in recently years applied to measure local strains in bone callus [62] in the medical field. Mechanical tests with DIC have also been conducted at temperatures as high as 1200⁰C [81]. However, oxidation is a problem which affects strain measurements and inert test environment is highly recommended [68]. Due to the relative ease of implementation and use, the DIC technique has also been applied to strain measurements at the scale of microstructures with the help of Scanning Electron Microscopes (SEM) and developed software. It was used to study damage formation at the microscopic scale in Advanced High Strength Steels by Ghadbeigi et al. [82] by carrying out tensile testing at room temperature in a SEM chamber. This experimental procedure has also been used to study damage formation in tensile specimens at 110⁰C [83] in 2011. Recently in 2014, a tensile test within a SEM has been successfully conducted at temperatures as high as 950⁰C [84] to study hot damage in several materials. However, deformation conditions from the tensile test carried out in the latter study are not representative of the large compression experienced by hot rolled metals [10].

The microgrid technique is another full-field strain measurement technique which has been used to quantify the deformation of materials at the scale of their microstructure [85]. The technique has also been successfully applied at temperatures as high as 1050⁰C in a plane strain compression test using a specimen geometry modified to lay microgrids at the surface of an insert welded to the rest of the specimen [86]. The same experimental procedure was then applied in reference [87] at 950⁰C. However, during these tests, microgrids were engraved at the surface of the metal, which is affecting the local strain measurement resolution and potentially subsequent microstructure evolution, including damage, due to the grooves generated at the surface. It was also required to seal the insert with the rest of the specimen to avoid oxidation. Therefore, the microgrid technique is not suitable for surface crack studies when tests are conducted in unprotected environment. However, Soula et al. [88] successfully demonstrated the use of microgrids to study the creep behaviour of a superalloy NR6 at the surface of a tensile specimen tested at temperature up to 850⁰C in a creep machine furnace under vacuum (~10-4 Pa).

## Summary

Crack formation along the edges of the hot rolled steel can be caused by many factors including material microstructure and stress triaxiality generated during the rolling process. Since limited information can be extracted from a laboratory rolling test, there is need for developing a relatively simple but controlled test which replicates critical thermo-mechanical conditions for damage formation representative to those leading to edge cracking during industrial rolling. A tensile test is a simple test but it is not representative of hot rolling conditions, in terms of plastic deformation experienced by the material and stress triaxiality. Critical stress triaxiality states leading to edge cracking have been identified by Farrugia et al. [18] through hot rolling finite element simulations. Revised compression test geometries have been proved to effectively generate damage and cracks at the surface of the specimens deformed under thermo-mechanical conditions representative to those leading to edge cracking during hot rolling [18].

At the scale of the microstructure, damage formation in FCS is highly related to second phase particles. Published studies have clearly shown the effect of inclusion clustering  on damage formation with modelling studies simulating the effect of inclusion distributions on stress and strain fields at high temperature [10-12, 15, 54]. However, there is no experimental validation of these microstructural models due to the experimental difficulty in measuring local strain fields around inclusions at the scale of the microstructure of metals deformed under conditions representative of hot rolling leading to edge cracking.

Therefore, this work will focus on developing a new experimental procedure to measure strain distributions within the grains of a steel deformed at temperatures typical of hot rolling operations under controlled laboratory conditions using compression testing and specimen geometries generating levels of stress triaxiality representative of those leading to edge cracking during the hot rolling of FCS. A microgrid technique has been selected for this study as DIC cannot be used at the scale of the microstructure during hot compression tests carried out on conventional testing machines. New model materials will also be used for the experimental programme to simulate the behaviour of FCS at high temperature, and to keep the microgrids deformed at high temperature upon cooling without any phase transformation. It is believed that results from this new experimental procedure combined with microstructure analysis should provide novel insight into the localisation of deformation in the microstructure of hot deformed FCS leading to damage development under mechanical conditions similar to those leading to edge cracking in hot rolled products.

Chapter 3

# Experimental Procedures

## Machines and Specimen Designs

### Introduction

This chapter introduces test machines involved in this project and demonstrates the necessity of computer simulation to design specimen geometries suitable for the study of damage formation in FCS and acquire useful information from the finite element models.

Edge cracking occurring during hot rolling is a complex process to analyse. The formation of damage from the surface of the rolled steel under thermo-mechanical conditions representative to those experienced by the material during hot rolling can however be studied effectively by combining experimental work and finite element (FE) analysis. FE models of hot rolling run by Farrugia et al. [18] provided much insight and understanding of critical stress states leading to damage formation in hot rolling. Based on the information from the hot rolling simulation, namely stress triaxiality levels of 0.3-0.5, a much simplified experiment can be designed and run in the laboratory under controlled thermo-mechanical conditions.

The large compression of the material experienced during hot rolling was first simulated in laboratory using a state-of-art 500kN Thermo-Mechanical Compressions machine (TMC) at the University, which can apply high strain rates and complex thermal cycles. However, tests are conducted in air using the TMC machine. Due to this limitation, the Gleeble machine available at Tata Steel was then used in this research to carry out tests under vacuum. Finally, real time microstructure deformation and damage evolution was observed at room temperature by carrying out tensile tests inside the chamber of a scanning electron microscope (SEM).

#### Finite Element modelling for specimen design

FE simulations in the current work are reported under experimental procedures as part of the specimen design procedure necessary for conducting laboratory tests. Therefore, it is an essential tool for specimen designs and planning for the study of damage formation during the hot compression tests. All models are also run based on the material data collected from experimental tests, namely stress strain curves of the materials.

FE simulations of hot compression tests involve three types of non-linearities due to the large deformation experienced by the material, the elasto-visco-plastic behaviour of the material and contact conditions between the anvil and the deformed steel. The simulation is broken down into increments with iterations within each increment until convergence is obtained. Figure 3.1 illustrates the iteration process for plastic strain calculations for every load increment. The residual or difference between a linear estimate of the force and the actual value derived from the experimental stress/strain curve, introduced in the model, is checked against the tolerance value set as an input to the model. If the residual value is higher than the tolerance value then the code computes a new slope value for the tangent to the experimental stress/strain curve using the strain value computed from the last iteration using the linear estimate and the actual force value of the stress/strain curve. This process carries on until convergence has been reached for the particular load increment.

Figure 3.1 a) First iteration b) Second iteration in an increment [89]

Implicit FE models with isotropic hardening material model and von Mises yield criterion which is available in ABAQUS [89] were used for simulations. The experimental uniaxial compression strain-rate-dependent and temperature-dependent test results were introduced in a table (Figure 3.2 a [90]) in ABAQUS. Models were assigned with constants properties such as Young’s modulus (106 GPa) and Poisson’s ratio (0.34). 3D continuum, coupled displacement-temperature 8 nodes solid element (C3D8T) with non-linear quadratic interpolation functions was used for models. Meshed models were deformed by rigid body tools which were initially set at operation temperature and in contact with the test-piece with a constant friction coefficient of 0.2 [91, 92]. Models are normally simulated using 1/8th  or 1/4th  of the original test piece geometry by taking advantage of the symmetry for both geometry and loading conditions. Therefore, boundary conditions such as symmetric conditions are set on faces where a mirror images of the results are expected. This is a common way used to reduce the computing time of the simulations. The partial model can then be visualised as a complete model by adding adequate viewing settings provided by ABAQUS[89]. An example of such simulations is shown in Figure 3.2 b.

Figure 3.2 a)Stress strain curves of FCS at 1000⁰C at various strain rates and [90] b) 1/8 of PSC specimen in contact with tools (rigid body) with boundaries conditions

### Hot compression test in air

#### Thermo-Mechanical Compressions machine (TMC)

Plane Strain Compression (PSC) tests were the very first high temperature test run in this project using the TMC machine (Figure 3.3). The capability of the machine in terms of the range of strain rates and thermal simulation enables the simulation of both industrial hot and cold rolling in a laboratory [93]. The temperature of the test piece can be monitored throughout the test using thermo-couples located in a hole drilled at mid-thickness into the specimen. Test specimens can be heated before or after deformation using a Fast Thermal Treatment Unit (FTTU) at high, controlled rates of heating and cooling. This project, in particular, was concerned with tests carried out at temperatures ranging from 800oC to 1200oC.

Because of the temperatures involved in the tests, the machine requires a long setup time with precise tools alignment before a test can be conducted. Common errors such as tools misalignment can greatly affect the collected data and the duration of the test programme as any such errors can only be corrected after the machine has cooled down to room temperature naturally. A full day is usually required to fix such a problem. Tests were also often delayed to following months due to its busy schedule. Therefore, it is extremely important to check every technical step to avoid losing any precious time for the experiments.

Even with perfect tool alignment, collected data namely displacement and applied force, are still expected to contain errors due to the heat involved and tool reliability. Therefore, a range of corrections were set in order to obtain reliable and useful results [66]. A series of corrections including origin correction, compliance correction, breadth spreading correction and friction correction are the major corrections applied to the raw data. The principle of these corrections is reported in Appendix 8.1.1.

Figure 3.3 Different views of the Thermo-Mechanical Compression machine: a)Front view; b) side view of the robot which drives the specimen; and c) control unit

#### Specimen design for TMC machine

Tests were first conducted in plane strain condition where dimensions of test specimen are shown in Figure 3.4. Simulation models (Figure 3.5) shows that stress triaxiality levels are in negative values in the centre as shown in Figure 3.6. Results also show that such specimen has maximum stress triaxiality of 0.06 on its free surface at the edge. However, the desired stress triaxiality required to form hot rolling damage ranges from 0.3 to 0.5.

Figure 3.4 Dimensions of PSC specimen

Figure 3.5 PSC specimen model before and after deformation (von Mises stress in MPa)

Figure 3.6 Stress triaxiality from the edge to the centre of the PSC specimen

Even though a PSC test (negative stress triaxiality) does not represent the mechanical conditions leading to edge cracking in hot rolling, it is still a useful test to study the deformation of the microstructure under similar compression levels. Therefore, a similar test to that reported in Castillo et al. [94] was conducted as shown in Figure 3.7 a with an embedded sample/insert. Inserts are used in combination with microgrids to measure strain distributions at the grain scale (see section 3.2.3.1) and were sealed to the main PSC specimen holder though welding (Figure 3.7 b).

Figure 3.7 a) Dimensions of PSC specimen with square slot for microgrids inserts (samples) [94] b) welding of microgrids inserts into PSC specimen

Later on in this project, a taper of 45⁰ was added to the regular specimen as shown in Figure 3.8 in order to generate stress triaxiality levels ranging from 0.3 to 0.5 on a PSC specimen. This modification was based on the work reported by Cusminsky and Ellis [72] who added a chamfer to a pre-rolled steel specimen to control its stress triaxiality as well as work by Farrugia who developed the RPS test [18]. A tapered specimen was modelled and subjected to a compressive strain of 25% as shown in Figure 3.9.

Figure 3.8 Dimensions of PSC specimen with taper of 45⁰

Figure 3.9 Tapered PSC specimen model before and after deformation (von Mises stress in MPa)

Figure 3.10 shows that the maximum stress triaxiality at the edges of the specimen is significantly increased from 0.06 to 0.44 when a taper is introduced. This result shows that tapers not only control stress triaxiality in rolled specimens but also in a compression specimen. The stress triaxiality, however, drops dramatically and rapidly away from the surface of the specimen as shown in Figure 3.10. Since stress triaxiality levels ranging from 0.3 to 0.5 are of interest for this study, further changes to the specimen geometry were needed to extend the region with suitable stress triaxiality levels.

Figure 3.10 Stress triaxiality from the edge to the centre of the tapered PSC specimen

The design of the specimens was therefore further modified by Brink [90], through a Masters project, as shown in Figure 3.11 and Figure 3.12 to extend the high stress triaxiality region. Figure 3.13 shows that the region with high stress triaxiality levels has been extended up to 4mm from the edge into the specimen, thus, increasing the area of interest for this study.

Figure 3.11 Dimensions of modified taper specimen

Figure 3.12 Modified tapered PSC specimen model before and after deformation (von Mises stress in MPa)

Figure 3.13 Stress triaxiality from the edge to the centre of the modified taper PSC specimen

The ideal areas for the study of damage formation are located at the surface of the specimen. However, the non-protective test environment of the TMC machine will encourage oxidation and therefore make the test specimen’s surface unexploitable. Therefore, there is a need to produce a separate insert to be sealed within the main test specimen. Inserts can then be extracted from the specimen after the test and analysed. The newly designed specimen geometry with inserts is shown in Figure 3.14 a and Figure 3.14 b [90] where parts are held together through welding.

Figure 3.14 a) Dimensions of modified specimen and b) exploded view of specimen with inserts [90]

It can be concluded that the introduction of a taper is an ideal way to increase the surface stress triaxiality level. However, stress triaxiality values drop dramatically and rapidly away from the surface. The final modification to the tapered specimen [90] geometry generates lower triaxiality levels at the surface compared to the previous tapered specimen geometry, but the region with stress triaxiality of 0.3-0.5 has been extended significantly (from 1mm depth from the surface to 4mm) as shown in Figure 3.16. This improvement therefore enables the study of damage development below the surface, therefore avoiding oxidation problems, and through the depth of the specimen using an insert.

Figure 3.15 shows the summary of the PSC specimen design evolution and the corresponding stress triaxiality profile variation due to the change in geometry (Figure 3.16). Revised compression specimen geometries will then be machined and tested with results shown in Chapter 3.2.

Figure 3.15 From left to right: PSC, Tapered PSC, Revised tapered PSC specimens [90]

Figure 3.16 Comparisons of stress triaxiality from the edge of three specimens

### Hot compression test under vacuum

#### Gleeble machine

Due to the limitations of the TMC machine in terms of test environment, additional testing was carried out on a Gleeble machine under vacuum to study damage formation at high temperature without oxidation problems.

Gleeble 3800 (Figure 3.17) which is available at Swinden Technology Centre, Tata Steel is capable of running both tensile and compression tests with fully customisable tools and at temperatures up to melting temperature of test materials. Its high load capacity (20 tons of static force in compression or 10 tons in tension) and high displacement rate (up to 2000mm/second) allows a wide range of tests to be conducted with various sample geometries. Test specimens with thermo-couples welded on the sample surface can be heated up by direct resistance heating at rates up to 10000oC/s. The Gleeble machine also provides a test chamber with high vacuum (up to 10-3Pa) that protects the hot test specimen from oxidation.

Due to operational reasons, tests on the Gleeble machine were run with the help of technical staff at Tata Steel. Given the complexity of the test procedure and the long time needed to set up high temperatures and vacuum conditions, only a few tests were run per session. Additionally given the limited access to the machine, only a limited number of tests could be conducted on the Gleeble.

Figure 3.17 Gleeble machine model:3800

#### Specimen design for Gleeble machine

One of the key factors causing cracking along the edge of the hot rolled steel is the limited ductility combined with stress triaxiality values as shown in Figure 2.8. Simulation results showed that critical stress triaxiality values ranging from 0.3 to 0.5 with equivalent strain values ranging from 0.01 to 0.03 are required to generate rupture as shown in Figure 2.8 [18] .

Figure 3.18 b shows the specimen geometry designed by Farrugia [18] to generate cracking at the surface of specimens tested in the Gleeble machine with Figure 3.18 a showing the corresponding Rolling Direction (RD), Transverse Direction (TD), and Normal Direction (ND) in an industrial rolling process. The same specimen geometry has been used in this work (Figure 3.18 c). Most of the deformation takes place along  RD while a limited amount of spread takes place along TD, especially at the free surface where cracks are found. Such designed geometry has been shown to generate the right levels of stress triaxiality to generate cracks at the surface of the specimen but is different from the geometry recommended by the good practice guide to measure stress/strain curves under plane strain compression [66].

Figure 3.18 Resultant force directions due to applied force of a) rolling b) compression and c) dimensions of the Gleeble specimen

Figure 3.19 a shows a 3D simulation image of the undeformed Gleeble specimen and Figure 3.19 b-f the deformed specimen with required stress triaxiality levels highlighted. 25% compressive strain was applied to the Gleeble specimen which gave a maximum equivalent strain of 30% on the surface of interest as shown in Figure 3.19 c. On the other hand, Figure 3.19 d shows the corresponding stress triaxiality distribution on the same surface of the specimen with required values of 0.3-0.5 highlighted. Sectioning of the Gleeble specimen along the centre plane (ND,TD) is shown in Figure 3.19 e. Figure 3.19 f shows the stress triaxiality distribution on that plane with values of 0.3-0.5 highlighted. Results show that only a 0.5 mm depth below the surface experiences triaxiality levels between 0.3 and 0.5.

Figure 3.19 Simulated Gleeble specimen a) undeformed b)deformed with desired stress triaxiality highlighted c) plane view with equivalent strain d) plane view with desired stress triaxiality highlighted e) section with desired stress triaxiality highlighted and f) close-up view of the same section with desired stress triaxiality highlighted

Results for 75% applied compressive strain are shown in Figure 3.20. Figure 3.20 a shows the equivalent strain distribution on the area of interest with values between 110% and 165% highlighted in the figure. The stress triaxiality distribution on the same surface is shown in Figure 3.20 b with values between 0.3 and 0.5 highlighted. Figure 3.20 c and Figure 3.20 d show stress triaxiality distributions along the centre plane (ND,TD) with values between 0.3 and 0.5 highlighted.

Figure 3.20 Simulated Gleeble specimen deformed by 75% a) plane view with equivalent strains b) plane view with desired stress triaxiality highlighted c) section with desired stress triaxiality highlighted and d) close view of the same section with desired stress triaxiality highlighted

As a conclusion, the Gleeble specimen geometry is ideal for the study of damage formation for tests carried out under vacuum as the right stress triaxiality levels are generated on the surface of the specimen without oxidation problems.

### Room temperature in-situ tensile testing

#### Deben Tensile machine

In parallel to the high temperature tests providing ex-situ results, a readily available testing facility in the University of Sheffield has enabled additional in-situ tensile tests to be conducted to study progressive local damage evolution in FCS at room temperature. Even though both testing temperature and stress triaxiality levels are not representative of the critical conditions for edge cracking during rolling, results from these tensile tests are useful to observe and quantify microstructure deformation leading to progressive failure and compare mechanisms with those observed at high temperature. These tests are conducted on a relatively small Deben tensile stage which can fit into  CamScan SII (SEM) to study local damage development in materials. It has a load capacity of 5kN and a maximum tensile extension length of 10mm. Figure 3.21 a shows the tensile machine and Figure 3.21 b shows its installation into a SEM.

Such tensile tests were conducted within the SEM and required a total of 16 hours per test due to the long time required for setting up the loading stage in the microscope, obtaining the right vacuum level after opening the door of the chamber and conducting the test using the procedure described in section 3.2.2.4. Process included a long image acquisition time required for subsequent strain analysis using Digital Image Correlation (DIC).

Figure 3.21 a) Deben tensile machine b) Tensile machine inserted into the SEM

#### Specimen design for Deben Tensile machine

A tensile test is a fundamental test that has been run for decades and standards have been established to allow good comparison between materials. Therefore, the specimen was initially designed based on standards and accounting for machine limitations. The ultimate tensile strength of  low carbon steel is sUTS=740MPa while the maximum load considered for the  tensile machine was Fmax=3kN (taking into account a safety factor). The maximum cross sectional area of the tensile specimen, Amax can be obtained as 4mm2 through Amax=FmaxloadσUTS .  Assuming that the original cross section area Ao prior to deformation is equal to Amax, the initial gauge length of the specimen, L, was calculated as 9 mm based on the US tensile test standard which recommends that  LAo=4.5. Therefore, a drawing of the tensile specimen was made based on these calculations and is shown in Figure 3.22 a. A computer simulation was run for validation of the specimen design. Only 1/8th of the specimen geometry was generated as shown in Figure 3.22 b to save computation time with materials stress strain curve inputted into the model.

Figure 3.22 a) Dimensions of tensile specimen based on US tensile test standard b) 1/8th of simulation model

Results can be viewed on the whole model by applying symmetrical view and show that the down-scaled standard tensile geometry works fine as it deforms within the limits of tensile machine as shown in Figure 3.23. Simulation results indeed show a maximum load of 2.94kN and high stress values concentrated along the whole gauge length.

Figure 3.23 Equivalent stress (MPa) distribution along the tensile specimen with a geometry based on US standards

However, during the tensile test, damage can appear anywhere along the gauge length of 9mm, which is not ideal for tracking damage development at high magnification . Therefore, the gauge length was minimised so that damage initiation and propagation could be captured within a reasonable sized area.

A revised tensile specimen geometry was therefore generated following the work reported by Ghadbeigi et al. [82] and is shown in Figure 3.24 a. The ratio of the gauge length over the square root of the cross sectional area was therefore 1 instead of 4.5 (US standard). Observations of local deformation and damage mechanisms in the microstructure can be done on such a design. Figure 3.24 b shows the simulation of the tensile specimen with the new geometry with high strain concentration within the short gauge length and a maximum predicted load of 2kN only.

Figure 3.24 a) Dimensions of revised tensile specimen b) simulation model with equivalent stress (MPa) distribution

## Materials, Sample preparation, Test conditions, and Strain measurement

### Materials

Three materials were provided by Tata Steel Europe. The primary studied material is as-cast FCS, which experiences crack formation as well as microstructure evolution during hot rolling. The second metal, hot rolled Fe-30wt%Ni, specially-made by Tata Steel, is a non-transformable simulation material with high content of nickel as an austenitic stabiliser. It remains in the austenitic phase even at room temperature.  Finally, a similar simulation material also produced by Tata Steel but with a higher sulphur content (as-cast Fe-30wt%Ni+S) was investigated in this study. The chemical composition of the materials is given in Table 3.1.

Table 3.1 Materials composition (LAP= low as possible)

FCS is the main material of interest as far as applications are concerned. However, due to the microstructure evolution taking place in FCS at high temperature during the hot rolling process, as discussed in the Literature Review, there is a need to cast a simulation material, which represents the FCS’s austenitic phase while preventing microstructure evolution namely, phase transformation, for observations and analysis of the microstructure at room temperature. This simulation alloy, Fe-30wt%Ni, cast and hot rolled at Tata Steel, has been shown to have similar stress/strain responses and stacking fault energy to that of austenite in any transformable carbon steel [67]. It was used in the first part of this work to develop the experimental procedure required since it was readily available. The material was heat treated at 1200⁰C for 10minutes to form equi-axed grains in the microstructure. Further casting was done by Tata Steel to produce a new Fe-30wt%Ni alloy with 0.3wt% addition of sulphur with the aim of forming manganese sulphide inclusions similar to those observed in FCS. However, the optimum casting conditions are yet to be found since the inclusion types and distributions in Fe-30wt%Ni+S (Figure 3.25 a) are in general different from those found in FCS (Figure 3.25 b). However, globular type inclusions commonly observed in FCS can also be found in Fe-30wt%Ni+S which can therefore be used as a simulation material to study the influence of such inclusions on local deformation and damage.

Figure 3.25 Inclusions found in a) Fe-30wt%Ni+S and b) FCS

Inclusions found in the FCS are similar to what Moore refers as inclusions of type I (globular) [7] as shown in Figure 3.26 a while a large proportion of inclusions found in Fe-30wt%Ni+S corresponds to the Type II mentioned by Moore [7]. Moore suggests that the formation of Type I and Type II inclusions is related to their chemical composition and especially the proportion of carbon and aluminium content, as shown in Figure 3.26 b. The aluminium content has also a direct effect on the distribution of inclusions [7].

Figure 3.26 a) Various types of inclusions and b) effect of the composition on types of inclusions formed [7]

In summary, all three materials will be studied at both room and high temperature. Limitations related to the phase transformation in FCS will be overcome by studying the behaviour of the two simulation austenitic alloys as far as local deformation and damage are concerned.

#### Microstructure

After several trials and errors, optimal chemical etching conditions were found to reveal the microstructure of FCS using 3% Nital (97ml Methanol + 3ml Nitric acid) for 15seconds. As-cast FCS’s microstructure consists of ferrite and pearlite with MnS inclusions as shown in Figure 3.27 a. An Energy-dispersive X-ray (EDX) analysis was carried out in the SEM to confirm the composition of the inclusions (Figure 3.28 a) as MnS with lead attached with some inclusions (Figure 3.28 b). Inclusions and pearlite islands appear to be randomly distributed in the ferrite matrix with approximate grain size of 50-150microns .

Figure 3.27 Microstructure of FCS a) Pearlite, Ferrite and inclusions b) Pearlite

Figure 3.28 Composition of a) inclusions and b) inclusions with lead

Several trials were also made to find out the optimal etching conditions for the simulation material, Fe-30wt%Ni. Due to the high nickel content, Fe-30wt%Ni cannot be etched through immersion in a weak acid as for FCS. The microstructure of Fe-30wt%Ni can only be revealed by wiping the polished surface of samples with a piece of cotton with a solution of 70% Nitric acid and 30% water. Figure 3.29 a shows the austenitic grains of Fe-30wt%Ni which are in general much bigger (~300-500microns) compared to the FCS’s ferrite grain size ( ~50-150microns). However  Fe-30wt%Ni+S cannot be etched to reveal grain boundaries using the solution of 70% Nitric acid and 30% water due to the  presence of inclusions (failed etched microstructure shown in Appendix 8.5). Figure 3.29 b only shows the inclusions distribution of Fe-30wt%Ni + 0.3wt%S without revealing grain boundaries. However, Figure 3.29 b suggests that inclusions are located along grain boundaries which gives an approximate grain size of ~160-350microns.

Figure 3.29 a) Microstructure of Fe-30wt%Ni b) Inclusions distribution in Fe-30wt%Ni+0.3wt%S

### Sample preparation and test conditions

As explained in section 3.1 three types of tests are carried out in this project with different setup and unique specimen geometries for each test. Specimens were first machined according to the designed geometries reported in section 3.1. In general, all specimens or inserts are ground and polished before each test. Chemical etching is then done on some selected test specimens depending on each experimental requirement.

#### Microgrids

The microgrid technique is the adopted technique among available techniques reported in Chapter 2 to perform local strain measurements in the microstructure of metals. Following surface preparation, microgrids have been deposited on most test specimens used in this study.

Gold was selected as the microgrid material due to its high melting point, good deformability and good chemical contrast. Soula et al. [88] suggest that Hafnium Oxide, HfO2 is another good choice of material for high temperature microgrid applications but gold provided successful results in this study (see section 4) .

- The surface of interest on the specimen was mechanical ground and polished (down to 1 µm diamond paste) to remove surface scratches

- The microstructure of the specimen was revealed by chemical etching depending on each test requirement.

- A thin layer of electro-sensitive polymethyl methacrylate (PMMA) resin was deposited onto the surface. In order to create a thin resin film, the sample was fasten to a disc rotating at 1200 rpm for 1minute as shown in Figure 3.30 a and b. Specially designed sample holders allow samples of different sizes to be fitted in. The sample is then heated at 140⁰C for 30 minutes to polymerise the resin.

Figure 3.30 Resin application machine a) overall view b)rotational disc with sample holder

- PMMA resin is then irradiated by the SEM (Philips 500) electron beam which was controlled externally by the Nanometer Pattern Generation System (NPGS) [95] to perform microgrid printing. SEM and NPGS system are shown in Figure 3.31 a and b

Figure 3.31 SEM: Philips 500 a) SEM control panel with NPGS system b) Microscope components

NPGS is a software/system that controls or monitors the electron beam of a SEM. An AutoCAD drawing (.dwg) is created as a pattern of microgrids which is then imported and calibrated to match the NPGS format. A run file is then created with parameters, such as the beam current, and printing time (Dwell), which are optimised through trials and errors. The microgrid printing will take place once the calibration between the NPGS and SEM is done. Due to the complex and time consuming procedures needed without guarantee of successful grids deposition, multiple trials and failures were carried out in order to obtain optimised parameters for NPGS and recorded in Table 3.2.

| Pitch size (Microns) | Beam Current (pA) | Dwell (Micro-Sec) | Area covered (Micron2) | Total Run Time (Min) |
| --- | --- | --- | --- | --- |
| 40 | 20 | 225 | 2640x2640 | 30 |
| 20 | 22 | 350 | 4100x4100 | 120 |
| 10 | 25 | 300 | 1320x1320 | 76 |
| 2.5 | 15 | 250 | 264x264 | 72 |

Table 3.2 Optimised parameters for various microgrid printing conditions

- Irradiated resin can then be removed using a solution of 75% propanol and 25% 22-Butanone. The removal of irradiated resin reveals lines printed by the electron beam which are ready for gold deposition. Figure 3.32 shows an optical image after removal of the irradiated resin.

Figure 3.32 Burnt resin removed

The machine (Emscope SC500) used to sputter gold at the surface of the specimens is shown in Figure 3.33. The gold thickness has to be controlled through a deposition time duration in order to produce the best quality grid, which also requires several trials and errors.

Figure 3.33 Sputtering machine: Emscope SC500

- The remaining resin was removed using ethyl acetate in an ultrasonic bath and the specimen surface will finally left with a complete set of gold microgrids as shown in Figure 3.34 b (20micron pitched grids).

Figure 3.34 a) Ultrasonic bath b) Specimen with gold microgrid

Figure 3.35 is a 3D illustration summarising the various steps of microgrid deposition.

Figure 3.35 a) Deposited resin exposed to electron beam, b) irradiated resin is removed, c) overlaying gold on the area d) gold microgrid appears after remaining resin is removed

Producing microgrid is a time consuming and challenging process due to the multiple steps involved. There is also little indication whether a step is successful until the whole process is completed. Examples of failed microgrid deposition can be found in Appendix 8.6. Besides the limited availability of equipment to be coordinated across various Departments, each session for microgrid deposition can only produce 2 to 3 sets of microgrids only depending on the required microgrid pitch size and covered microstructure area. A typical duration of 10 hours is needed to complete the experimental procedure. Therefore, planning needs to be done months ahead and each step is done with extreme care. Such complex procedures make microgrid samples extremely valuable.

#### Plane Strain Compression test using TMC

Plane Strain Compression (PSC) tests were conducted at high temperature in air using the TMC machine described in section 3.1.2. Specimens were subjected to deformation at a strain rate of 1s-1 (typical value within the roughing rolling range of 0.1 to 5s-1) at temperatures ranging from 800oC to 1200oC. Both displacement and applied force were recorded during the tests. Raw data were corrected according to a good practice guide [66]. Details of these corrections including origin correction, compliance correction, breadth spreading correction and friction correction can be found in Appendix 8.1.1.

##### PSC tests with embedded microgrids

Due to the high temperature involved in the compressive tests without protective atmosphere, all inserts with deposited microgrids had to be sealed through welding to the main specimen holder before conducting a test,  as shown in Figure 3.36 a and b. This was required to avoid oxidation of the surface of the inserts that would cover the microgrids and therefore make the test unexploitable.

Figure 3.36 a) Inserts with deposited gold microgrid b) assembly of microgrid insert into the PSC specimen

After deformation as shown in Figure 3.37 a and b, specimens are machined to separate inserts from specimen holders as shown in Figure 3.37 c and the deformed microgrids are then visualised using a SEM.

Figure 3.37 a) Asymmetric view and b) plane view of specimen and TMC machine's tools c) Deformed PSC specimen and extraction of the microgrid inserts

This procedure has been successfully applied to Fe-30wt%Ni as discussed later in Chapter 4. However, Fe-30wt%Ni+S was shown to have poor weld-ability as shown in Figure 3.38 a, and therefore successful results could not be obtained using this method. Therefore, an alternative procedure was devised which involved new designed specimen holders made of Fe-30wt%Ni with Fe-30wt%Ni+S inserts not welded to the holder, as shown in Figure 3.38 b. Welding was therefore only applied to Fe-30wt%Ni along the external joint lines. Since Fe-30wt%Ni was proven to have a similar stress strain response to that of Fe-30wt%Ni+S (see Chapter 4), deformation incompatibility between insert and holder was therefore minimised during the test. Therefore, the design shown in Figure 3.38 b was adopted. Such PSC tests were carried out to test the suitability of gold microgrids at such high deformation temperatures and to analyse the deformation of microstructures under plane strain conditions.

Figure 3.38 a) Fe-30wt%Ni+S with inserts welded b) revised inserts holder

##### Modified compression test specimen with embedded microgrids

The modified compression specimen designed by Blink [90] and run as part of this project is shown in Figure 3.39 a. showed that stress triaxiality values ranged between 0.3 to 0.5 in the region beneath the edge. Microgrid inserts (Figure 3.39 a) produced in this work were sealed through welding as shown in Figure 3.39 b before undergoing deformation. Results obtained will be discussed in the Chapter 4.

Figure 3.39 Modified compression specimen a) Exploded view of specimen with inserts [90] b) Components welded together

#### Compression test in Gleeble machine

Compressive tests were conducted under vacuum using the Gleeble machine as discussed in section 3.1.3. Critical microstructure changes and crack formation are expected on the surface of the specimen normal to TD. Gold microgrids were therefore laid onto that surface as shown in Figure 3.40 a to measure strain distributions at the scale of the microstructure. Before microgrid deposition the sample’s face of interest was ground, polished and chemically etched to reveal the microstructure. All tests were conducted at a strain rate of 1s-1 with various temperatures ranging from 850oC to 1000⁰C for the three investigated materials. Figure 3.40 b shows a deformed specimen within a Gleeble machine.

Figure 3.40 a) Microgrid deposited onto a Gleeble specimen b) deformed Gleeble specimen

#### Micro-DIC coupled Tensile test in Deben machine

Digital image correlation (DIC) coupled with tensile test provides not only material information such as, modulus of elasticity, yield strength, ultimate tensile strength, but also the full-field strain distribution over the specimen surface which provides insight into the local strain variation and deformation behaviour. Figure 3.41 a shows a tensile test specimen with a high resolution optical camera. Specimens are normally sprayed with a random speckle pattern on the surface in order for DIC to be operated. Figure 3.41 b shows a DIC result of a deformed tensile specimen before the specimen breaks.

Figure 3.41 Tensile test a) with optical camera d) DIC measured strain on tensile specimen

DIC coupled with tensile testing is a very useful tool to extract information such as local strain to fracture. However, damage initiation and propagation can only be obtained at the scale of microstructures [55] and therefore the resolution offered by optical cameras is not sufficient enough. Therefore, a down-scaled tensile test has therefore been conducted within a scanning electron microscope (SEM) to study local damage mechanisms. The design of test specimens was described in section 3.1.4. Figure 3.42 shows a comparison between a standard tensile specimen and a down-scaled tensile specimen.

Figure 3.42 Tensile specimens a) regular size b) revised

Tensile specimens are ground and polished down to 6 micron diamond paste, which gives the specimen a mirror-like finish and yet, with minor scratches on the surface as shown in Figure 3.43 a. These scratches are important tracing marks that allow DIC to compute local displacements at the surface of the specimen. The specimen is attached to the tensile machine through pins as shown in Figure 3.43 b.

Figure 3.43 a) Tensile specimen fit onto a tensile machine b) Deben tensile machine

After zeroing the load, the tensile test runs at a displacement rate of 0.1mm/min, and is stopped every 10 seconds for image acquisition. Before the test starts, magnification, brightness and contrast settings need to be selected carefully, in order to obtain useful images of an area of interest to be subsequently processed using DIC for local strain calculations. The selected area is normally located at the centre of the gauge length where damage and crack are expected to appear. Figure 3.44 shows an example of a focused area during the test on FCS with small scratches helping the subsequent image correlation for strain calculations.

Figure 3.44 Gauge length of the tensile specimen with close-up view of the selected area of interest at higher magnification

### Strain measurement

Strain measurements at the scale of microstructure is one of the main objectives of the project which allows understanding of microstructure deformation and damage formation in relation to local strain distribution. This extracted information can also be used to inform simulation models or to validate models. Two main strain measurement methods were adopted in this project namely, Microgrid technique and Digital Image Correlation technique which will be discussed next.

#### Microgrid

The microgrid technique deposits uniform and identical grids over an area with the overall area size and microgrid pitch defined by the scanning parameters in the SEM during irradiation with the electron beam (see Table 3.2). After deformation, the initial square grids become distorted, and therefore strain values can be computed from the distortion of the grids.

A MATLAB script was programmed by Gutierrez [96] to first record the position of every microgrid line intersection through manual clicking. Every small microgrid element defined by the position of its 4 corner points is then compared to a  corresponding square element before deformation to compute strain values for every microgrid element. The program can calculate the Green-Lagrange or Logarithmic strain components (11, 22, 12) and the equivalent strain (eq) for every square of the microgrid, derived for the displacement of the microgrid intersections due to deformation, following the procedure described by Allais et al [85].

The deformation gradient tensor F, is introduced to characterise the transformation of every grid element from the undeformed to deformed configurations. The coordinates of the four corner points  of each microgrid element are used to define the two vectors V1 and V2 for the undeformed configuration (Figure 3.45 a). Likewise, v1 and v2 are vectors defined for the deformed configuration (Figure 3.45 b). They can be defined as follows:
V1 = Ai + Bj

V2 = Ci + Dj

v1 = ai + bj

v2 = ci + dj

| a) |  | b) |  |
| --- | --- | --- | --- |

Figure 3.45 (a,b) Schematic of the deformed and undeformed configurations, respectively, of a single microgrid square, showing the vectors used for the determination of the deformation gradient tensor.

From these vectors the in-plane deformation gradient tensor is determined as follows:

(3.1)

F is a result of a rigid body rotation tensor, R and a distortion tensor, U as follows:

(3.2)

For Logarithmic strain calculations, the distortion tensor, U can be diagonalised as follows:

(3.3)

where Q is the tensor which gives the orientation of the principal directions of the distortion and D is the diagonal tensor. t stands for transposition. The Logarithmic strain tensor can then be derived as:

(3.4)

The equivalent strain is then determined from the strain components, using the following equation:

(3.5)

#### DIC

The technique discretises the undeformed image into small interrogation or subset windows, each having a unique pixel intensity array. A correlation algorithm is tracking windows in the deformed images and compute displacement vectors at the centre of each subset. After that, in-plane strain values can be generated through differentiation.

Two commercial software, namely DaVis and Vic-2D were available for strain calculations. Ghadbeigi et al. [65] suggested that DaVis gives better correlation, for DIC applied to SEM images of microstructures using the natural features of microstructures, compared to Vic-2D and thus, provides more reliable strain measurements. Therefore, DaVis is the selected software for analysing local deformation in this work.

DaVis [97] defines the strain tensor, Eij as linear gradients of the displacement field (Equation 3.6). A central difference scheme as shown in Equation 3.7 is used to generate strain values. Firstly, the displacement vectors to the left and to the right (or to the top and to the bottom) of a given point of coordinate (n,m) at the centre of the considered interrogation window are found, then the difference is divided by the distance, r, between these neighbouring vectors to compute the strain component.. The total engineering strain, E, is obtained from the total displacement vector measured in the final image by reference to the un-deformed image and true strain values are computed using Equation (3.8).

(3.6)

(3.7)

(3.8)

Chapter 4

# Results

## TMC Test Results

Each compression test with microgrids inserted in specimens represents extremely valuable data due to the complexity of the preparation procedure for each sample reported in section 3.2.2. Therefore, every individual test was conducted and handled with extreme care.

### Stress/strain curves

Data recorded by the TMC machine is formatted and recognised by commercial software such as Microsoft Excel. Important raw data such as load, displacement, temperature, and displacement speed are then inputted into a pre-formatted excel macro to perform the data correction as mentioned in session 3.1.2 with detailed steps described in Appendix 8.1.1. After extensive correction, processed data will then be used to construct stress/strain graphes.

Comparison can be made between FCS and simulation materials. Figure 4.1 shows results for FCS and Fe-30wt%Ni+S at 800⁰C and strain rate of 1s-1. Fe-30wt%Ni+S required a maximum compression stress of 290MPa compared to 120MPa for FCS to perform 35% reduction. Such difference in behaviour is expected since the simulation material was designed to simulate the austenitic phase of FCS and 800⁰C is still below the ferrite-to -austenite phase transformation temperature for FCS (910oC).

Figure 4.1 Stress/strain curves at 800⁰C

At 1000⁰C, both simulation materials subjected to a strain rate of 1s-1 have similar maximum compressive stresses at around 140MPa even though the hardening behaviour is very different with a much higher hardening rate for Fe-30wt%Ni+S likely due to the effect of MnS inclusions. By comparison the maximum stress for FCS is lower at around 110MPa. Despite this slight difference between FCS and the two simulation materials, the stress strain curves of FCS and simulation materials are relatively close to each other as shown in Figure 4.2.

Figure 4.2 Stress/strain curves at 1000⁰C

Finally, the stress strain curves of the simulation material Fe-30wt%Ni and FCS for compression tests ran at 1200⁰C are shown in Figure 4.3. The graph shows that at low strain values up to 10%, the behaviour of these two materials is similar. However beyond 10%, the curve for Fe-30wt%Ni keeps increasing while the flow stress for FCS reaches a maximum value at about 12% strain before starting to drop significantly.  This softening of FCS is typical of dynamic recrystallization which is not found in the simulation material.

Figure 4.3 Stress/strain curves at 1200⁰C

Given the results obtained at the three investigated temperatures it is clear that the optimum temperature to test the simulation materials is 1000⁰C as the stress/strain curves are closer to that of FCS which should be fully austenitic at that temperature without experiencing dynamic recrystallisation up to 17% and limited recrystallization up to 25% (Figure 4.2 at 1000oC).

### Microgrid results

#### Fe-30wt%Ni

Apart from the recorded data, the deformed test specimen was collected from the TMC machine after water spray cooling. Figure 4.4 a shows a deformed specimen covered with a layer of oxide after a test at 1000⁰C. The deformed specimen is then machined to extract the insert (microgrid specimen) as shown on Figure 4.4 b. Steps for the extraction of the insert were challenging. Due to the welding and deformation taking place at high temperature, inserts were very well bonded together after the test. Insert extraction steps included milling off the top and bottom parts of the deformed specimen to remove the welded layers, careful machining to separate the inserts from the main specimen holder and finally, separating inserts from each other. The last step was the most critical step as the deformed inserts were relatively small in size and still bonded closely to each other. The last step was therefore done manually to prevent damaging the inserts and more importantly the microgrids. During the process of separation, relative sliding of the two inserts must indeed be avoided to prevent damaging the gold microgrids, which can be easily removed through contact with fingers, and therefore losing all valuable results from the surface. Therefore, extreme care and hours were spent to obtain only one exploitable sample.

Figure 4.4 a) Deformed Fe-30wt%Ni PSC specimen b) Deformed PSC specimen and extraction of the microgrid inserts

Extracted microgrid inserts were then viewed using a SEM. Figure 4.5 clearly demonstrates that the gold microgrids survived the test at 1000oC. However, the visualisation of both microstructure and microgrids can be difficult due to the close contact of the surfaces of the two parts of the insert during deformation. However, with the help of photomicrography acquisition modes in the SEM, the image quality of both the microstructure and microgrids can be improved. Figure 4.5 demonstrates two modes of imaging of the same area: secondary electrons imaging (Figure 4.5 a) and backscattered electrons imaging (Figure 4.5 b). Figure 4.5 a shows a better view of the microstructure while Figure 4.5 b highlights the microgrid patterns.

Figure 4.5 Deformed Fe-30wt%Ni microstructure a) secondary electrons imaging and b) backscattered electrons imaging of the same area

With the help of different SEM imaging modes, images can be optimised and analysed accurately. After processing the image using the Matlab script described in section 3.2.3.1, an strain-yy distribution map has been constructed using the commercial mapping software Surfer [98] and results are superimposed onto the photomicrograph as shown in Figure 4.6 with grain boundaries highlighted. For an applied compressive strain of 20%, the strain map shows wide variation of strain values locally. This result provides a valuable insight into the heterogeneity of local deformation in the microstructure of Fe-30wt%Ni with local strain values ranging from -6% to -62%. High strains may be observed as localised near grain boundaries which indicates that grains deform more near grain boundaries or experience grain boundary sliding as reported in [94]. However, clear grain boundary sliding could not be observed in this current work. Due to the limited region covered by the strain map, results may not be representative of the overall microstructure. Therefore, a strain map covering a wider area could be helpful in drawing a more definite conclusion.

Figure 4.6 Deformed microstructure with measured compressive strain

Another insert was extracted from a test conducted at 1000⁰C with an applied strain of 25%. Figure 4.7 b shows clear deformed microgrids after the test using back-scattered diffraction imaging. However, the deformed microstructure was not clearly visible and the strain map was instead plotted over the un-deformed microstructure as shown in Figure 4.8. Such procedure allows better observation of the strain distribution over the microstructure. Additionally, Figure 4.8 a shows strain values calculated for each grid as output by the Matlab script and without the interpolation procedure used by Surfer while Figure 4.8 b shows the interpolated strain map over the undeformed microstructure. This result shows very little difference between the two maps.

The map once again shows high local strain heterogeneity with values ranging from -20% to as high as -105%. It is also clear from the results that some grains deform more than others which might be due to different grain orientations. The highest strain localisation is found along the grain boundary located near the right lower corner in the image (highlighted in red circle in Figure 4.8 b). This may suggests that when grain boundaries are found perpendicular to the direction of applied strain, the local strain near such grain boundaries is higher. Again, the covered area is too small to draw a final conclusion which would require analysis on a much larger area.

Figure 4.7 Un-deformed microstructure and deformed microstructure of Fe-30wt%Ni

Figure 4.8 Strain-yy map over the un-deformed microstructure of Fe-30wt%Ni a) without interpolation b) with interpolation

#### Fe-30wt%Ni+S

The microgrid pitch size for this test was refined in order to try resolve strain distributions in inclusions. However due to the limitations of the SEMs used  in this work (Philips 500 and CamScan SII), the minimum grid pitch size achieved after many trials was 2.5 micron as shown in Figure 4.9 a. Such pitch size is smaller than the biggest inclusions size but cannot resolve strain distributions in most inclusions.

Due to the poor weldability of Fe-30wt%Ni+S, an insert made of Fe-30wt%Ni+S was welded inside a Fe-30wt%Ni holder with compression test conditions described in section 3.2.2.2.1. After the test, the insert was extracted and observed using a SEM. Figure 4.9 b shows that oxidation still took place and made the microgrids unexploitable after the compression test at 1000⁰C. After 8 attempts such tests on Fe-30wt%Ni+S were abandoned.

Figure 4.9 Fe-30wt%Ni +S with microgrid a) before test b) after test

#### Modified compression specimen

As explained in section 3.2.2.2.2, a modified compression specimen was machined and 4 sets of 2.5 microns pitch microgrid were deposited onto the inserts. Each microgrid set was covering a wide area of 600 x 600 micron2 of the insert as shown in Figure 4.10 a for Fe-30wt%Ni+S.

Figure 4.10 2.5 micron pitch size microgrid a) 4 sets b) close view of microgrids

After welding the insert to the specimen holder as explained in section 3.2.2.2.2 and applying 20% reduction at 1000⁰C, the sample was quenched with water spray. Figure 4.11 shows the deformed specimen where a crack is found at the edge. This experimental result demonstrates the validity of the assumption made in generating edge cracks under stress triaxiality levels ranging from 0.3 to 0.5 as computed from the FE model. Figure 4.11 also show cracks along the weld as expected for Fe-30wt%Ni+S due to its poor welding profile.

Figure 4.11 Modified compressive specimen after deformation

The specimen was then machined to extract the concealed microgrid insert. Figure 4.12 a shows the top view of the insert that was still attached to part of the specimen holder. Unfortunately due to the exposure to air, the microgrid insert was oxidised as shown in Figure 4.12 b. A layer of oxide was formed during the test and ripped off the surface when opening the sample. Therefore, local strains at the scale of the microstructure could not be measured due to oxidation.

Figure 4.12 a) Insert of revised compressive specimen b) oxide scale formed

### Summary

Limited compression test results were obtained from the TMC machine mainly due to the non-protective test environment. Nevertheless, stress strain curves for each material were obtained for various test conditions, which were used for the FE simulations. Results showed that 1000⁰C is a practical test temperature for both simulation materials and FCS. Local strain measurements at the scale of the microstructure of Fe-30wt%Ni were successfully obtained from the PSC test. For the first time gold microgrids have been successfully proven to survive temperatures up to 1000⁰C. Strain maps plotted over the un-deformed microstructure are particularly useful when the visibility of deformed microstructure is low. Heterogeneous local strain distributions suggest the influence of the microstructure (e.g. grain orientations and grain boundaries) on strain localisation. No exploitable results could be obtained in terms of local strain measurements for Fe-30wt%Ni+S due to the poor weldability of the material when tests are conducted in air.

## Gleeble Compression Test Results

Given the issues reported in the previous section in terms of oxidation of the specimens during the tests conducted in air using the TMC machine, tests have then been carried out using the Gleeble machine available at Tata Steel. However, these tests took place at a relatively late stage in the project and due to the difficulty in accessing such highly used equipment at the company only a limited number of tests could be carried out and results are presented in this section. Tests with microgrids on simulation materials have therefore been limited to a deformation temperature of 1000oC which corresponds to a temperature whereby FCS should be fully austenitic.

### Stress/strain Curves

Figure 4.13 shows the stress strain curves of the 3 different materials deformed at 1000⁰C at a strain rate of 1s-1. In general, the FCS and Fe-30wt%Ni+S curves are very similar and require a flow stress value of 160MPa for a reduction of 25%, while the stress/strain curve of Fe-30wt%Ni is slightly lower with a stress of about 150MPa for the same compression strain. The main reason for such a difference could be that Fe-30wt%Ni was hot rolled and heat treated while FCS and Fe-30wt%Ni+S were as-casted material. Nevertheless, these three materials have similar stress strain curves at this particular temperature.

Figure 4.14 shows the stress/strain curve of FCS deformed at 850⁰C. A stress value of about 170MPa is required to deform  FCS to a 25% reduction at 850⁰C. Even though the temperature difference between 1000⁰C and 850⁰C is significant, FCS deformed at 850⁰C requires slightly higher stress than that at 1000⁰C for the same reduction of 25%.

Figure 4.13 Stress strain curves of FCS, Fe-30wt%Ni , Fe-30wt%Ni +S at 1000⁰C

Figure 4.14 Stress strain curve of FCS deformed at 850⁰C

#### Thermal etching

As explained in section 3.2.1.1, chemical etching used for Fe-30wt%Ni could not be applied to  Fe-30wt%Ni+S  due to the presence of the inclusions. Therefore, thermal etching was adopted instead. The procedure consists of heating up a specimen to 1000oC within 3 minutes and hold at that temperature for one minute with or without deformation, then, cool down slowly to room temperature. As long as the vacuum condition is maintained throughout the process, grain boundaries which could not be revealed through chemical etching (Figure 4.15 a) appear after thermal etching as can be seen from Figure 4.15 b .

Figure 4.15 Fe-30wt%Ni+S a) before thermal etching b) after thermal etching

Besides revealing the grain boundaries, thermal etching also generates voids around inclusions as shown in Figure 4.16 a. Due to the distribution of the inclusions (with voids due to thermal etching) located along the grain boundaries, the formation of a crack along the grain boundaries is encouraged even though there is no strain applied onto the specimen. This phenomenon where crack form due to thermal etching is observed more frequently in Fe-30wt%Ni+S (Figure 4.16 b) in comparison with Fe-30wt%Ni and FCS.  This result seems in line with [22] which suggests that high energy grain boundaries are revealed through thermal etching (see Figure 2.3 in section 2.2).

Figure 4.16 Thermal etched Fe-30wt%Ni +S a) voids around inclusions b) crack along grain boundaries

Besides the simulation materials, FCS can also be subjected to thermal etching when undergoing the same heat treatment. Figure 4.17 shows that grain boundaries are revealed in FCS after heating up a specimen to 1000oC within 3 minutes and holding it for one minute without deformation, before cooling it down to room temperature. Large grains (size > 40 microns in diameter) suggests that thermally etched grains are likely to be prior-austenitic grains [21]. Besides revealing grain boundaries, voids generated around inclusions are also observed as in the  simulation material.

Therefore, it is concluded that chemical etching can reveal Ferrite and Pearlite in FCS while thermal etching reveals prior-austenitic grain boundaries. Moreover high energy grain boundaries encourage the formation of cracks when inclusions are located along grain boundaries, as observed in Fe-30wt%Ni+S.

Figure 4.17 Thermal etched FCS

### Observation in FCS

Before testing the two simulation materials, tests were conducted on FCS with microgrid laid on its surface. The obtained results were interesting and helpful in understanding both local microstructure evolution and deformation when FCS was deformed at high temperature.

At 850⁰C, FCS was expected to experience partial phase transformation as the phase diagram suggests in Figure 2.2 b. Microgrids deposited on the surface of FCS  appear to have provided some clues about the phase transformation. Figure 4.18 a shows the 2.5 micron pitch microgrids before the test, and Figure 4.18 b shows the partially disappeared grids which covered the same area before and after applying 25% compressive strain at 850⁰C. Even though lost grids affect strain measurements, they appear to reveal  the partially transformed microstructure in those regions.

Figure 4.18 b shows regions with and without phase transformation. Results suggest that deformation and cracks are mainly observed in the transformed regions. One major crack is joining two inclusions in the transformed region. On the other hand, the non-transformed regions show uniform grids which suggest minimum or no local deformation in those regions. Nevertheless, some small-scale cracks can be found in the non-transformed regions which could be cracks running along grain boundaries (more supporting evidence in section 4.2.2.1).

Figure 4.18 FCS with deposited microgrids a) before b) after the test at 850⁰C

For a test conducted at 1000⁰C, FCS is expected to experience complete phase transformation as suggested by the phase diagram (Figure 2.2 b), except for inclusions. This seems to be confirmed by the disappearance of the 2.5 micron pitch microgrids as shown in Figure 4.19 b (backscattered electron imaging) while microgrids within inclusions still remain visible.

Figure 4.19 FCS with deposited microgrids a) before b) after test at 1000⁰C

Even though such results cannot be used to quantify strain distributions in the microstructure due to the loss of visibility of the microgrids, they can be used to identify the microstructure evolution, namely phase transformation in FCS, which may be useful for understanding the microstructure behaviour at high temperature. Nevertheless, the highly visible microgrid within inclusions after the test allows some strain measurements in inclusions

Manual strain measurements were carried out by comparing the undeformed (Figure 4.20 a) and deformed images (Figure 4.20 b) of the inclusion. Results give a strain-xx along the horizontal axis of 1.3% and a strain-yy along the vertical axis of -3.75%. The result shows that the steel matrix was highly distorted during the applied compression with a void around the inclusion expanding significantly. Although the steel matrix around the inclusion deformed greatly, the inclusion itself only experienced minimal deformation.

Figure 4.20 a) Grid length measurements of an un-deformed inclusion and b) Grid length measurements of the same deformed inclusion

Apart from the small strain experienced by inclusions, Figure 4.21 a also shows an inclusion rotation of 32.7⁰ with reference to the nearby inclusion which had hardly rotated during deformation. This results therefore suggests that inclusions on the surface not only experience minimal deformation but also rotate as rigid bodies due to the applied compression after debonding of the interface with the steel matrix. It may also be an indicator that suggests the mode of local deformation as shown in Figure 4.21 b. For instance, it indicates the flow of matrix around the inclusion locally when subjected to the applied compressive strain. Again, more tests would be required to confirm this suggestion.

Figure 4.21 a) Rotation of the inclusion due to the plastic deformation of the matrix and b) path of the matrix deformation

The very small deformation of inclusions is unexpected since the literature shows that inclusions can be highly deformable during hot forming as evidenced by the elongated inclusions commonly seen in sectioned hot rolled steel [99]. Therefore, a further examination was done by sectioning the same specimen which had been deformed at high temperature as shown in Figure 4.22. Unlike the surface, results show that inclusions in the subsurface are deformed (elongated) as much as the steel matrix and yet form no or little voids around inclusions. Figure 4.22 shows the midplane of the specimen with the microstructure of FCS chemically etched after the test. This finding is in line with the commonly found elongated inclusions in hot rolled steels.

Apart from the difference observed between inclusions at the surface and in the bulk of the specimen in terms of deformation, Figure 4.22 also shows the formation of new pearlite islands at the centre of the specimen, with these islands arranged perpendicular to the direction of the strain applied. Such pearlite arrangement is identical to the pearlite bands found in [20].

Figure 4.22 Microstructure of FCS at the centre of the deformed specimen

Besides the test run with a fine pitch microgrid (2.5 micron) at 850⁰C on FCS, another test was run at the same temperature on FCS with a 20 microns pitch grid. The obtained result was unexpected since the grids were still highly visible after an applied strain of 25% at 850⁰C as shown in Figure 4.23. This result suggests that the phase transformation did not affect much the 20 micron pitch grid. This may be due to the thickness of the grid as 20 micron pitch grids are thicker than the 2.5 micron pitch grid. Based on this result, which was unexpected and obtained late in the project,  high pitch sized microgrid are potentially a very useful technique to study the local deformation of transformable steels at high temperature but more tests would be required to confirm this hypothesis. The analysis of the deformed grids will be reported in Section 4.2.4.

Figure 4.23 20 micron pitch microgrid after deformation at 850⁰C on FCS

#### Microstructure observation in FCS after deformation at high temperature

Apart from the tests run with microgrids, few FCS samples were tested without microgrids at high temperature (850⁰C and 1000⁰C) to observe the microstructure behaviour when deformed at high temperature. A strain of 25% was applied to the FCS specimen deformed in the Gleeble at 1000⁰C. In the deformed region, Figure 4.24 a shows that cracks generated along the grain boundaries and voids appeared around the inclusions. On the other hand, Figure 4.24 b shows a region away from the deformation zone which only experienced thermal etching. In this image, prior austenitic grain boundaries are revealed as well as voids around inclusions.

Figure 4.24 Microstructure of FCS after deformation at 1000⁰C  a) within the deformation zone, b) in the un-deformed area (thermally etched only) of the specimen and c) global view of the specimen

A large number of voids were observed around inclusions over a wide area of 4mm by 4mm and were always expected when tests were conducted at high temperature with or without deformation. Such voids increase in size when FCS was subjected to deformation. However, no coalescence connecting two nearby voids together was observed despite the large local deformation taking place as shown in Figure 4.25 a. Therefore these voids and inclusions found on the surface of the specimens do not seem to contribute significantly to crack formation but they do promote crack extension when they are located along grain boundaries when the test was conducted at high temperature as shown in Figure 4.25 b.

Figure 4.25 Microstructure of FCS after deformation at 1000⁰C  a) voids around inclusions and b) crack propagation along grain boundaries affected by voids around inclusions

Additionally, a test carried out at 1000⁰C had revealed two different phases in FCS based on two very distinct grain sizes observed in different regions of the microstructure as shown in Figure 4.26. These two phases have been  named phase 1 (size ≈ 15 microns in diameter) and phase 2 (Size > 30 microns in diameter). These grains are compared side-by-side with chemically etched ferrite in Figure 4.27. Phase 2 has a grain size that is much bigger than chemically etched Ferrite thus, phase 2 is likely to correspond to the prior-austenitic phase as shown in Figure 4.27 a. Phase 1 on the other hand, has a similar size compared to the Ferrite phase size as shown in Figure 4.27 b and c. Therefore, Phase 1 could be either recrystallised austenite or thermally etched ferrite phase.

Figure 4.26 Microstructure of FCS after deformation at 1000⁰C

Figure 4.27 Microstructure of FCS: a) Thermal etched Phase 2, b) chemically etched FCS and c) thermal etched Phase 1

Another test was run with micrographs taken before and after the test in order to be compared side-by-side. For instance, images of the same area of the FCS microstructure before and after a test carried out at 850⁰C are shown in Figure 4.28 a and b. After the test, phases 1 was discovered in Figure 4.28 b at the same location where a pearlite island was observed before the test (Figure 4.28 a). This shows that pearlite phases were transformed into an austenitic phase with a smaller grain size than that produced by the transformation of the ferrite phase during the test at high temperature. According to these observations, Phase 1 could also be the result of the transformation of pearlite into austenite phase.

Figure 4.28 Microstructure of FCS a) before the test with Pearlite highlighted and b) after the test at 850⁰C

Besides revealing some clues about the microstructure evolution in FCS, the surface normal to TD of such specimens promotes the formation of damage and cracks that can be studied without further sample processing. Results show that damage is generally found along grain boundaries of both phase 1 and phase 2 in FCS. However, major cracks are only found along the grain boundaries of phase 2 (prior austenitic phase) where inclusions can be a catalyst to form a bigger crack as shown in Figure 4.29.

Figure 4.29 Microstructure of FCS after the test at 1000⁰C with the highlighted region where major cracks are observed

Differences in terms of deformation of the microstructure and crack development at the surface of  FCS samples were compared between tests carried out at 1000⁰C and 850oC. At 850oC, plastic deformation is much more heterogeneous with many 45o localised shear bands found as shown in Figure 4.30 d. Such intense and large deformation bands have not been found in FCS deformed at 1000⁰C (Figure 4.30 e). Additionally, much smaller cracks are observed in the microstructure deformed at 850oC (Figure 4.30 c) compared to those found in FCS deformed at 1000⁰C (Figure 4.30 e). Results also reveal that damage development in FCS at 1000oC is dominated by intergranular cracking, while at 850oC, it instead consists of both intergranular and intragranular cracking. Figure 4.30 a and b indeed show what appears to be transgranular damage formed within a ferrite grain as the same area of the microstructure has been found after deformation (Figure 4.30b) and can be compared to the undeformed image (Figure 4.30 a). The crack is located in an area which corresponds to a previous ferrite grain (Figure 4.30 a) and which appears to have experienced rather low deformation in comparison to regions around it where intense deformation bands can be observed. This region might therefore correspond to the un-transformed phase, as shown in Figure 4.30 c, which does not appear to deform much given the rather small distortion of the microgrids.

In conclusion, there seems to be a clear transition in terms of both deformation and damage mechanisms between 1000oC and 850oC in FCS.

Figure 4.30 Microstructure of FCS a) before and b) after an applied strain of 25% at 850⁰C, c) close-up view of an un-transformed region after deformation at 850⁰C, (d) large deformation bands in the transformed regions and e) FCS deformed at 1000⁰C

#### Microstructure observation for the simulation alloys deformed at 1000⁰C

The limitation associated with FCS tests especially in terms of quantifying strain distributions in the microstructure of the commercial alloy due to phase transformations can be overcome through testing of the simulation materials which do not experience any phase transformation  upon heating or cooling for the temperatures considered in this work. Therefore, the same test condition (1000⁰C) was applied onto Fe-30wt%Ni as a  simulation material to study the deformation of the austenitic phase of FCS at high temperature. Results also show that cracks are generated along grain boundaries at this temperature as shown in Figure 4.31. This finding is similar to results reported for FCS at 1000oC. The larger grain size in Fe-30wt%Ni (~300-500microns) compared to FCS (~50-150microns) has shown less grain boundaries in a given area. Therefore, even though the damage mechanism appears similar the extent of grain boundaries damage is lower for the simulation material.

Apart from damage, the bigger grain size in Fe-30wt%Ni allows a clearer visualisation of the deformation mechanisms within each grain. In the Fe-30wt%Ni microstructure, deformation within grains can be observed in the form of activated slip systems with different orientations in relation to the applied strain as shown Figure 4.31. Moreover, local strain values can be measured though the analysis of the distorted grids as shown later in section 4.2.4.

Figure 4.31 Microstructure of Fe-30wt%Ni after the test at 1000⁰C

The other simulation material, Fe-30wt%Ni+S, was also tested under the same conditions at 1000⁰C. Similarly, Fe-30wt%Ni+S also shows crack formation along grain boundaries where inclusions are located as shown in Figure 4.32 b. However, some areas of the deformed microstructure with inclusions spread across a large area indicate no sign of crack formation as shown in Figure 4.32 a while large cracks are clearly observed along grain boundaries in other areas as shown in Figure 4.32 b.

Besides the formation of cracks, an obvious difference between these two images can be seen in terms of slip system orientation. In Figure 4.32 a, there is a uniform slip orientation across a wide region likely to cross several grains and with only one slip system activated while Figure 4.32 b shows that the slip orientation in each grain changes direction (highlighted with red lines) on either side of a likely grain boundary. This results suggests that formation of cracks along grain boundaries may be affected by grain orientations likely to generate stress/strain concentrations at grain boundaries with high misorientations.

Figure 4.32 Microstructure of deformed Fe-30wt%Ni +S after the test at 1000⁰C with a) an uniform slip system orientation and b) with different slips system orientations across a grain boundary

The microgrid visibility was good enough for both Fe-30wt%Ni and Fe-30wt%Ni+S after the tests to enable further study of crack formation as a function of local strain measurement (section 4.2.4).

### FE simulation validation through strain measurements

Before carrying out a detailed analysis at the grain scale, strain values measured over a large area of the microstructure using microgrids were used to validate the simulation models. Due to the relatively small grid pitch (20 microns) over the large area of 4100 x 4100 micron2 on Fe-30wt%Ni, some adjustments have been made to analyse the microgrid effectively. Instead of processing 42025 small grid elements, data points have been selected at few microgrid intersection points along both horizontal and vertical directions in order to measure strain values over a grid with a much bigger pitch size (820 microns) as shown in Figure 4.33 with red lines marking the revised grid. In other words, the microgrid with a pitch size of 20 microns was transformed into a ‘macrogrid’ with pitch size of 820 microns.

Figure 4.33 Microgrids over the deformed Fe-30wt%Ni  with highlighted macrogrids

After analysing the grid with the Matlab script, a strain map was plotted for the Gleeble specimen deformed by 25% reduction as shown in Figure 4.34 b. Results shows a wide variation of equivalent strain values ranging from 34% to 9%. These experimental results and FE simulation results are not identical besides similar strain distribution ranges as shown in Figure 4.34 c. The difference in the results can be attributed to the local grain structure, which is quite coarse and which has not been taken into account in the simulation. Additionally, it is clear from Figure 4.34 b that there was a slight tool misalignment during the test (the black lines highlight the deformed area of the specimen from the images recorded using the SEM as shown in Figure 4.34 a) which has not been considered in the simulation.

Figure 4.34 a) Global view of the specimen, b) equivalent strain distribution after 25% applied strain measured using microgrids and c) predicted by the FE simulation

### Local Strain analysis at the microstructural scale

After validation of the FE simulation results using ‘macrogrid’ measurements, further analysis was carried out at a finer scale using all microgrid elements to study intra-granular strain distributions at high temperature.

#### Fe-30wt%Ni +S

A compression strain of 25% was applied to a Fe-30wt%Ni+S specimen at 1000oC. Superimposing simulation results onto a micrograph of the deformed sample (Figure 4.35 a) provides better insight into the deformation of the analysed areas shown before and after deformation in Figure 4.35 b) and c) respectively. Strain component yy in the FE model ranges from 0 to -15% over the total simulated area. The mesh element (350x350 micron2) highlighted in Figure 4.35 a corresponds to the size of the analysed microstructural area shown in Figure 4.35 b). For the comparison with strain calculations from the FE model, experimental strain values have been calculated by selecting the four corners of the total microgrid area shown in Figure 4.35 b) and c). Hence, direct comparison between simulation strain calculations and measured strain values can be done for this particular mesh element as shown in Table 4.1. For these strain calculations the experimental value for the out-of-plane strain component along the z direction has been computed by assuming plastic incompressibility (zz = - (xx + yy)). Results show a good agreement between model and experimental measurements.

Figure 4.35 a) Simulation model superimposed onto a micrograph of the deformed sample with b) local microgrids before deformation and c) after deformation with their respective close up views in d) and e)

|  | Strain-xx (%) | Strain-yy(%) | Strain-zz(%) |
| --- | --- | --- | --- |
| FE model | 23.5336 | -10.0597 | -13.4738 |
| Experiment | 23.5513 | -9.934 | -13.618 |

Table 4.1 Comparison between FE and Experimental strain values over the area of 350x350 micron2

After the applied compression, the surface normal to TD expanded along the x direction as shown in Table 4.1. However, both measured and simulated strain-zz were found to be compressive which might seem surprising. Therefore, the cross-sectional area of the model was studied in more detail. Figure 4.36 a shows the sectional plane of a deformed Gleeble specimen and Figure 4.36 b is the plane view of the sectioned Gleeble specimen after deformation. Strain contours have been set up to differentiate the parts of the specimen which experience tensile strain-zz (light grey) and compressive strain-zz (dark grey). It is therefore clear from this result that after deformation, although most of the specimen expanded along the TD direction, the material at the surface experienced a compressive strain along TD as confirmed by the experimental results .

Figure 4.36 Simulation results of a deformed Gleeble specimen with a) full specimen and b) plane view of the sectioned Gleeble specimen with positive and negative Strain-zz highlighted

Further analysis of the distorted microgrid was then carried out at a finer scale by computing strain values in every microgrid element. Figure 4.37 b shows the deformed microgrids over the microstructure of Fe-30wt%Ni+S located in the region of the specimen highlighted in Figure 4.37 a where equivalent strain values of about 20% and stress triaxiality values ranging from 0.3 to 0.4 were computed from the model (Figure 4.37 a).

Following the analysis of the grid using the Matlab script, an equivalent strain map was produced over the microstructure as shown in Figure 4.38 a. Results show high strain heterogeneity with equivalent strain values ranging from 8 to 68%. High strain values are mainly found along shear bands running at about 25o with respect to the loading direction within grains (highlighted in purple line in Figure 4.38 b). The equivalent strain map shows localised strain values of about 70% located around inclusions as shown in Figure 4.38 a. However, the strain map was corrected to remove strain distributions around voids since the interpolation method used in Surfer [98] was creating unrealistic strain values at the void locations. The corrected strain map shown in Figure 4.38 b therefore gives a maximum localised strain value of 60% with most of the high strain values located along shear bands.

Results show that for an applied strain of 25%, most of the deformation is accommodated along local shear bands which appear to be crossing several grains. In addition, the strain distribution map unveiled secondary shear bands which would not be otherwise noticed. These secondary shear bands are orientated at 75⁰  with respect to the primary shear bands (highlighted in red line as shown in Figure 4.38 b). These results show no sign of crack formation even with localised strain values as high as 60%.

Figure 4.37 a) Simulated stress triaxiality superimposed onto the photomicrograph b) microgrid over inclusions cluster in Fe-30wt%Ni+S

Figure 4.38 Equivalent strain map over the area of the microstructure a) without voids exclusion and b) with voids exclusion in strain measurement

In order to study the effect of inclusions on strain distribution as simulated by modellers [13, 18], image processing and further analysis was done. First of all, the micrograph was filtered to produce an image with inclusions appearing in black on a white background as shown in Figure 4.39 c. Such process includes filtering the original micrograph (Figure 4.39 a) through a threshold value set  in SigmaScan Pro 5 [100] to produce Figure 4.39 b which is then manually processed to produce Figure 4.39 c. The resolution of the image is then transformed from 896 x 896 pixels (each pixel is 0.156 x 0.156 micron2) into 56 x 56 pixels (each pixel is 2.5 x 2.5 micron2) using a Matlab script developed by Chalon [101] as shown in Figure 4.40 b. The new pixel size is selected to correspond to the microgrid pitch over which single strain values are calculated. By selecting the right grey level threshold value, the Matlab script identifies inclusions and produce the image shown in Figure 4.40 c. At this stage, the micrograph has been transformed into a pixelated image with coordinates of the inclusions recorded. It is then superimposed onto the original micrograph as shown in Figure 4.40 d. Due to the coarse elements, small inclusions (< 2.5 microns) are excluded by the matlab script and inclusions are highlighted through white grids as shown in Figure 4.40 d. It is worth noting that the procedure is somehow inaccurate with some errors created during the image resolution transformation which has missed some inclusions  and with also some final coordinates shifted from their real location. Nevertheless, the procedure used is able to identify the majority of the inclusions in the micrograph accurately.

Next, the strain map (without interpolation) is superimposed onto the filtered micrograph as shown in Figure 4.40 c. Each element is then allocated one strain value as shown in Figure 4.40 e. Inclusions are marked by white squares and red regions of 2.5 x 2.5 micron2 regions located around inclusions as shown in Figure 4.40 f are found using an Excel program. Finally, a histogram was plotted comparing strain distributions in the regions that are 2.5 micron away from the inclusions (red squares) and strain distributions in the austenitic matrix around these regions as shown in Figure 4.41. Results show that strain distribution histograms around inclusions and away from inclusions are similar. The main conclusion from this quantification of strain distributions around inclusions is that there is no distinctive effect created by inclusions on strain localisation for this particular area of the microstructure with measurements obtained using the 2.5 micron pitch microgrid.

Figure 4.39 a) Original micrograph of an inclusion cluster in Fe-30wt%Ni+S, b) after thresholding and c) final processed micrograph

Figure 4.40 a) Processed micrograph of inclusion cluster in Fe-30wt%Ni+S with b) change of resolution, c) identification of inclusions location, d) processed inclusions location superimposed to original micrograph,  e) superimposition of equivalent strain distribution values and f) transformed image with selected inclusions within white squares and red squares considered as inclusions surrounding

Figure 4.41 Histogram of equivalent strain in the austenitic phase around and away from the inclusions

Figure 4.42 shows the effect of the microgrid pitch size on local strain values. The same area of the microstructure was analysed by first selecting grid intersection points located 12.5 microns apart (Figure 4.42 a) and then by using all microgrid intersection points (2.5 micron grid pitch in Figure 4.42 b). Equivalent strain maps results clearly show the effect of the microgrid pitch size when calculating strain distribution values over the microstructure. Figure 4.42 a shows a maximum measured strain value of 38% with the bigger pitch size while strain values as high as 75% are measured around the grain boundaries where cracking is found with the smaller pitch size (Figure 4.42 b). On the other hand, strain values as high as 50% have been measured within a grain as shown in Figure 4.42 b. using the smaller pitch size. Hence, it is clear from this result the strain map resolution is very much dependent on the microgrid pitch size which should be reduced as much as possible to resolve high strain gradients especially around grain boundaries (where cracks are generated in this material) or close to the interface between matrix and inclusions.

Figure 4.42 Measured equivalent strain distribution over the Fe-30wt%Ni+S microstructure with a) a microgrid pitch size of 12.5microns and b) a microgrid pitch size of 2.5 microns

#### FCS

After studying the strain map at 1000oC and the effect of inclusions on strain distribution for the simulation material, another strain map was constructed using a set of 20 micron pitch grid deposited on FCS tested at 850oC. After 25% strain applied at 850oC, the grids were still highly visible as shown in Figure 4.23 unlike the 2.5 micron grid which was shown to disappear after testing FCS at both 850oC and 1000oC tests (Figure 4.18 and Figure 4.19).

After analysing the grid the equivalent strain distribution was mapped over an area of the deformed FCS microstructure as shown in Figure 4.43 c. Results show a very high level of strain heterogeneity with local strain values ranging from 0 to 100% for an applied strain of 25%. The strain map clearly shows the formation of intense shear bands orientated at 45o with respect to the loading axis in the microstructure of FCS deformed at 850oC. Without the strain map, it is not possible to identify the influence of inclusions on the microstructure deformation. For instance, Figure 4.43 a clearly highlights the strong influence of inclusions on strain localisation with the particular alignment of inclusions creating a high distortion of the microgrids as shown by the red arrows. However, results also show that strain localisation is not only caused by the presence of inclusions but is also the result of plastic deformation mechanisms in regions where no inclusions can be observed. For instance, Figure 4.43 b shows strain concentration caused by inclusions (Red arrow) as  well as in regions without inclusions (yellow arrows). In the latter case deformation patterns are similar to those observed in the transformed regions of the FCS microstructure after the test carried out at 850oC using a 2.5 micron pitch microgrid as shown in Figure 4.43 d. where intense localised bands of deformation can be observed. These regions might therefore correspond to regions where phase transformation takes place.

Results show that these regions deform to very high levels with strain values as high as 100% for the applied strain of 25%. This shows that such regions are preferable deformation zone over the non-transformed regions. Inclusions found within the transformed regions further promote strain concentration and potentially generate cracks as shown in Figure 4.18 b (test result at 850oC with a 2.5 micron grid reported in section 4.2.2).

Figure 4.43 FCS deformed at 850⁰C: a) effect of inclusions on strain localisation highlighted with red arrows, b) phase transformed regions with high strain localisation highlighted with yellow arrows, c) equivalent strain map plotted over the FCS microstructure and d) regions with and without phase transformation for the 2.5 micron grid

#### Fe-30wt%Ni

Fe-30wt%Ni, which is simulating the austenitic phase of FCS without the influence of inclusions, was also tested with local deformation analysed using microgrids. Fe-30wt%Ni was deformed up to 25% at 1000oC.

After the test, micrographs were taken and compared side-to-side with the FE simulation results. Figure 4.44 a shows the FE results in terms of strain-yy through the thickness of the specimen with two regions A and B highlighted over which microgrid strain measurements have been carried out. Figure 4.44 b shows the stress triaxiality results with values ranging from 0.3 to 0.5 on the surface normal to TD and within the analysed regions A and B. Region A corresponds to a 1600x1460 micron2 area of the microstructure shown in Figure 4.44 c where the highest strain values have been computed in the FE simulation. Figure 4.44 d shows the corresponding yy strain map after analysis of the microgrid distortion for region A. Figure 4.44 a clearly shows the strain heterogeneity across the thickness due to the particular geometry of the specimen with maximum strain values of 15% on that particular surface of the specimen for 25% applied compression. Figure 4.44 d clearly shows the strain heterogeneity experienced by the material at the scale of the microstructure with strain values ranging from 0 to 75% for 25% applied strain. This heterogeneity is observed between grains and also within grains where strain values are generally higher close to grain boundaries. The intergranular heterogeneity is likely due to differences in grain orientations but can also be the result of the location of the grains with respect to the heterogeneous macroscopic strain patterns observed in Figure 4.44 a.

Figure 4.44 a) Simulated strain-yy with two regions highlighted (A and B),  b) simulated stress triaxiality, c) micrograph of deformed microgrid in region A and d) experimentally measured strain-yy distribution over the deformed microstructure in region A

The average yy strain value over the area shown in Figure 4.44 d has been computed from both the modelling and experimental results for comparison purposes. Table 4.2 shows a direct comparison between simulation strain calculations and measured strain values in region A. Values of -13.92% (simulated strain) and -14.17% (average measured strain) have been found respectively and show reasonable agreement between the two results. However, both strain-xx and strain-zz show more discrepancies. These differences are not surprising given the small area analysed and the fact that the FE simulation is a continuum model which does not take into consideration the effect of local grain orientations.

The histogram shown in Figure 4.45 a quantifies the strain-yy heterogeneity recorded over the analysed area of the microstructure with a mean value of 14.17% and a standard deviation of 9.1%. The histogram is skewed towards the low strain values with high strain values ranging from 30% to 80% contributing only to 7% of the overall frequency distribution. This is likely due to the localisation of high strain values near grain boundaries which represent a small fraction of the total microstructure area given the coarse grain size of the material. The heterogeneity of strain-xx values over the analysed area can also be observed in Figure 4.45 b with a mean value of 15.9%.  Similarly, the strain-zz histogram in Figure 4.45 c shows the large variation of the out of plane strain component with both positive and negative values and a mean value close to 0%. This latter result indicates that some grains sink and others move out of the plane during compression as shown in Figure 4.45 d.

|  | Strain-xx (%) | Strain-yy(%) | Strain-zz(%) |
| --- | --- | --- | --- |
| FE model | 25.95 | -13.92 | -12.03 |
| Experiment | 15.90 | -14.17 | -1.73 |

Table 4.2 Comparison between FE and experimental strain values over the region A

Figure 4.45 Histograms of a) strain-yy distribution, b) strain-xx distribution c) strain-zz distribution d) Strain-zz over region A

Figure 4.46 a shows results for region B highlighted in Figure 4.44 a. Figure 4.46 b shows the corresponding strain-yy distribution over the microstructure with a lower range of strain values compared to region A due to the location of region B in the transition zone between the deformed zone and the un-deformed zone of the specimen as shown in Figure 4.46 a. Localisation of deformation can still be observed in region B with local values of 40% in compression. A key difference in region B compared to region A is the clear appearance of a crack along one grain boundary in the bottom left corner of the image in a region where relatively low strain values have been recorded. One region (region C) of the map with high strain values has been highlighted in Figure 4.46 b.

Figure 4.46 a) Micrograph of deformed microgrid in region B and b) experimental strain-yy distribution over region B with region C highlighted

A secondary electron image of region C is shown in Figure 4.47. The image clearly shows slip bands activated in grains on both sides of the grain boundary due to plastic deformation. In the bottom grain secondary slip bands seem to have formed in a small region close to the grain boundary to accommodate the higher strain level recorded by the microgrids at this particular location in the grain. This intra-granular heterogeneity is the result of plastic deformation mechanisms accommodating the applied deformation and is likely affected by local misorientations [102, 103].

Figure 4.47 Secondary electron image of Region C

The full microgrid area (4 mm x 4 mm) was analysed and results in terms of strain-yy and strain-xx are shown in Figure 4.48 c and d respectively. Analysing an area of 16 mm2 with 20 micron pitch microgrids, through manual clicking of the microgrid intersection points using the Matlab script is an extremely tedious and time consuming task. Therefore, the analysis has been divided into 9 areas with each area taking hours or a day to complete. Results show a very large number of low strain values in this test due to the offset of the microgrid with respect to the centre of the deformation zone in the specimen with the region on the right hand side, highlighted by the deep blue/purple colours, close to the undeformed part of the specimen.

Some regions highlighted in pink are thought to be errors in both Figure 4.48 c and d. These small values are indeed attributed to errors associated with the analysis of the distorted grid through manual clicking of the intersection of the microgrid lines using the Matlab script as will be demonstrated in section 4.2.6. It is interesting to see from the strain map that very low strain values are also recorded in several grains located in the main deformation zone of the specimen. The applied deformation appears to be accommodated through the formation of bands of deformation running at ± 45o with respect to the compression axis, especially visible in the strain-yy map. Moreover, very high strain localisation is recorded along some grain boundaries preferably orientated with respect to the direction of these bands. These deformation patterns are very different from those predicted by the FE model (Figure 4.48 b) where such localised bands cannot be observed. This is not surprising since the continuum FE model does not take into account the effect of the crystalline structure of the material. Experimental results do show the influence of the crystalline structure with some grains deforming more than others, which is likely due to the effect of different crystallographic orientations. Therefore there seems to be a better correlation between crack locations and high tensile strain-xx values as seen in Figure 4.48 d.

Several cracks can be observed along some of the grain boundaries and these cracks have been highlighted in Figure 4.48 a using secondary electron imaging. It is interesting to note that the back-scattered image appears to show more “cracks” although the dark contrast generated along some of the grain boundaries is due to out-of-plane deformation as revealed by the secondary electron image.  Cracks appear to be orientated in different directions with several of them orientated along a direction close to that of the compression axis. Cracks seems to be also located in regions of relatively small equivalent strain values as also observed in region B (Figure 4.44).

Figure 4.48 a) Secondary image of Fe-30wt%Ni after deformation at 1000⁰C with b) its location with respect to the deformed zone in the FE model, c) strain-yy map  and d) strain-xx over an area of 16 mm2

### Multiple-pass test

A two-pass testing procedure was attempted to check the feasibility of studying damage development as a function of local strain distributions measured at the surface of the specimen. The Fe-30wt%Ni alloy initially deformed with 25% applied strain as reported in the previous section (Figure 4.49 a) was reloaded in the Gleeble machine and deformed under the same conditions as in the first pass except for the applied compression strain which was limited to 15%. The deformed microstructure after the second pass is shown in Figure 4.49 b using secondary electron imaging and in Figure 4.49 c using back-scattered imaging. Figure 4.49 a and Figure 4.49 b highlight the development of damage over the two stages with the appearance of new damage sites,  highlighted with yellow circles in Figure 4.49 b, while damage sites observed after the first pass are highlighted in red.  Unfortunately, Figure 4.49 c show the poor resolution of the microgrids after the second pass which prevented strain calculations. The reason for this poor image quality is due to the fact that the two passes were carried out months apart, given the limited availability of the Gleeble machine, which therefore, led to the deterioration of the sample’s surface quality. However, these results can be analysed in terms of new damage formation after the second pass in relation to strain distributions after the first pass. Close comparison between Figure 4.49 b and Figure 4.48 d reveals that new cracks have nucleated along grain boundaries in regions of relatively small strain values (less than 25%).

These results are therefore very encouraging and it is anticipated that the experimental procedure would lead to even more exploitable results if the second pass was conducted after a relatively short time interval.

Figure 4.49 Two-pass compression test on Fe-30wt%Ni : a) deformed microstructure after first pass (25% applied strain) b) secondary image of the same area of the microstructure after the second pass (15% additional applied strain and c)  backscattered image after the second pass

### Microgrid error analysis

Every technique has its limitation and errors which determine its accuracy in terms of strain measurements. Two main types of errors for the microgrid technique have been analysed in detail. The first type of errors relates to the inaccuracy of the electron beam of the SEM in irradiating the PMMA resin used to print the microgrids. Even though the scanning parameters of the SEM were set to print, for instance, a 20 micron pitch size, small drifts occur during irradiation. This can be visualised in Figure 4.50, where a single microgrid element might have the 20 micron required pitch (Figure 4.50 a) while measurements carried out over several rows of the grid reveal a slight deviation, 20.3 microns averaged over the 7 analysed rows, from the set microgrid pitch (Figure 4.50 b).

Figure 4.50 Initial grids length measurement of a) one grid b) 7grids

Even though this error accumulates over several rows, it remains relatively small for each microgrid element over which local strain values are computed. By analysing a large number of microgrid elements randomly distributed over a particular grid, an error of 1.5% has been estimated. This value is therefore very small in comparison to the large strain values recorded in this work after the large applied compression.

The second type of errors relates to the precision of locating the microgrid intersection points during manual mouse clicking used in the Matlab script.

Clicking the centre of the intersection points can never be perfect. Figure 4.51 a shows that the microgrid lines are 3.5 microns in width. Figure 4.51 b shows the red intersection point of two microgrid lines, while a few blue manual clicking points are shown as examples of the potential in clicking errors that record the position of the intersection point for subsequent strain measurements.

Figure 4.51 Microgrid intersection points with precision error

Such error can be quantified by analysing a sufficient number of manual clicking data points over an un-deformed microgrid micrograph which was analysed using the Matlab script. Figure 4.52 shows the un-deformed microgrid.

Figure 4.52 Undeformed microgrid

A regular grid analysis procedure was carried out with every single intersection points manually picked through the Matlab interface. Then, strain components are calculated. All calculated strain values can be plotted on a map which is then called the ‘error map’ which included both types of errors mentioned. Figure 4.53 a shows the strain map for the strain-xx component, Figure 4.53 b shows the map for the strain-yy component and Figure 4.53 c the map for the equivalent strain. Both strain-xx and strain-yy maps show a range of errors of about +/- 5% while the mean error for strain-xx component is as low as 0.089% and the mean error for strain-yy component is about 0.19%. In both Figure 4.53 a and Figure 4.53 b, the maps show linear patterns which demonstrate the drift of the SEM irradiation for several scanning lines. The equivalent strain map shows errors ranging from 0.4% to 6.4% with a mean value of 2.56%. However, once again, the recorded errors remain negligible in comparison to the very high strain values recorded after the large compression applied in all tests conducted in this work.

Figure 4.53 Error map a) XX component b) YY component c) equivalent strain

### Subsurface damage development in FCS at 1000⁰C

Strain measurements and damage formation observed at the surface of Gleeble specimens have drawn much insight into the early stages of damage development at high temperature test  under mechanical conditions similar to those leading to edge cracking during the hot rolling of FCS. However these results were limited as far as crack propagation is concerned. In order to study further damage development, deformed Gleeble specimens were sectioned along the mid-plane shown in Figure 4.54, polished and then viewed in a SEM.

Figure 4.54 Sectioning of deformed Gleeble specimens

In the centre of the FCS specimen, inclusions are highly deformed (elongated) as shown in Figure 4.55 a and are similar to those found in hot rolled steel. Inclusions deformation is therefore high compared to those found at the sub-surface of the specimen (Figure 4.55 b). This difference in the deformed shape of the inclusions is a further evidence of the variation of strain-zz from the centre of the specimen to the surface as computed by the FE model. The tensile nature of strain-zz towards the centre elongates the inclusions in that direction while compressive strain-zz values close to the surface tend to maintain the spherical shape of the inclusions in the plane of observation. Additionally, no voids can be observed around inclusions in FCS below the surface. This finding suggests that there is a different damage mechanism in relation to inclusions at the surface and below the surface when FCS is deformed at 1000⁰C.

Figure 4.55 b also provides some clues about damage propagation from the surface of the specimen. The image first demonstrates the large amount of out-of-plane deformation of the surface normal to TD which was recorded in the strain maps in section 4.2.4.2. This image also provides clear evidence of damage propagating along TD from the surface which further demonstrates the suitability of the testing procedure in simulating the mechanical conditions leading to edge cracking in industrial rolling. Without chemical etching, the micrograph may suggest the influence of inclusions in crack propagation right beneath the damage surface as shown in Figure 4.55 b.

Figure 4.55 Inclusions in FCS at a) the centre of the specimen and b) at the subsurface

Therefore, in order to better examine the crack mechanisms in relation to microstructural features, FCS was chemically etched with 3% Nital. Etching revealed the microstructure and the  pearlite phase aligned mostly along grain boundaries (Figure 4.56). This pearlite distribution has been named as pearlite band in Kim et al. [20].

Figure 4.56 Microstructure of FCS at the centre of the (ND,TD) plane

At the edge of the sample (right beneath the surface), clear cracks are observed after chemical etching, which propagate along grain boundaries as shown in Figure 4.57. The surface cracks generated along grain boundaries at the surface therefore propagate into the material through the same mechanisms.

Figure 4.57 a) Microstructure of FCS at the subsurface and b) close-up view of damage propagating along grain boundaries

Further into the material (away from the surface) significant damage is found, as shown in Figure 4.58 a. Figure 4.58 b shows a close-up view of the damage area located 370 microns away from the surface (as shown in Figure 4.59 a) where clear evidence of the influence of inclusions on damage formation can be seen. This result not only highlights the important role of inclusions in crack formation but also shows an intragranular damage mechanism at this location in the sample.

It may be argued that such damage can be produced during the surface preparation process which involves sectioning and polishing. However, Figure 4.58 a clearly shows that the pearlite band alignment has been disturbed around the damaged area, which indicates that the damage event has taken place during the hot deformation of the specimen.

Figure 4.58 a) Damage away from the specimen’s surface for FCS b) evidence of the influence of  inclusions on intragranular cracking

Major cracks and large voids shown in Figure 4.58 are found in a sub-surface  area no larger than 368 microns away from the surface as shown in Figure 4.59 a. On the other hand, the FE model shows that stress triaxiality values ranging from 0.3 to 0.5 are only found up to 0.3mm beneath the edge surface as shown in Figure 4.59 c. This result is therefore, in line with the experimental observations as far as damage is concerned.

Figure 4.59 a) Distance from the surface where damage can be found in FCS deformed at 1000⁰C b) stress triaxiality distribution at the subsurface with c) close-up view

### Summary

Local strain measurements in relation to damage formation at high temperature at the scale of the microstructure have been made possible with the new experimental procedure developed in this work, which combines compression test at high temperature under protective environment with gold microgrids deposited at the surface of tapered specimens. Early damage development has been observed along grain boundaries in all materials investigated with strain maps generated over large areas of the microstructure. FCS deformed at 850⁰C showed very heterogeneous local deformation mainly due to both partial phase transformation and the influence of inclusions. On the other hand, FCS deformed at 1000⁰C mainly showed grain boundaries damage at the surface of the deformed specimens while a trans-granular damage caused by inclusion was observed at the subsurface. Results therefore suggest that there is a strong surface effect on damage formation in FCS when the material is deformed at high temperature, namely 1000⁰C. Moreover, results for the two simulation materials are supporting such findings with damage mainly observed along grain boundaries at the surface of the compressed specimens and local strain histograms showing no significant effect of the inclusions on strain localisation at the surface.

## Room temperature micro- tensile test results

### Stress/ strain curves

Figure 4.60 shows the load-displacement data recorded during a tensile test carried out on FCS in the SEM. The graph shows regular drops in force along the curve, which correspond to several instances during the test when the electric motor of the loading stage is stopped in order to acquire images of the microstructure for subsequent DIC analysis. These drops in force therefore correspond to an elastic relaxation of the machine.

Figure 4.60 Force against extension for FCS deformed up to fracture using tensile testing in the SEM

The raw data collected from the machine require a series of corrections. The total measured elongation, xTotal includes both machine and sample elongation:

xTotal=xMachine+xSample					(4.1)

Correction for machine  stiffness, Kmachine, was estimated as follows:

xtotal=FKmachine+F∙LA∙E=1Kmachine+LA∙EF

∴F=1Kmachine+LA∙E-1xtotal				(4.2)

Where L=gauge length, A= cross sectional area, E= Young’s modulus

The elastic region of the graph (measured from the experiment) provides a gradient value from which the machine stiffness is calculated.

m=1Kmachine+LA∙E-1

∴Kmachine=A∙E∙mA∙E-L∙m						(4.3)

The contribution of the elastic deformation of the machine to the total elongation can therefore be removed through Equation 4.1:

xsample=xtotal-xMachine

The corrected data can then be used to construct an engineering stress/strain curve, where stress is force divided by cross-sectional area, 4mm2, while strain is extension divided by the initial gauge length of 2mm. Figure 4.61 shows the corrected stress/strain curve for the three materials investigated in this work.

Fe-30wt%Ni has the highest ultimate tensile stress of about 450MPa and has the highest  strain to fracture (about 130%). On the other hand, FCS and Fe-30wt%Ni+S have similar strain to failure, which is about 65%. However, FCS has a slightly higher ultimate tensile stress than Fe-30wt%Ni+S. The higher strength for Fe-30wt%Ni is likely due to the process history as Fe-30wt%Ni was hot rolled and heat treated whereas the other two materials were only in as-cast condition. The lower strain to fracture for both Fe-30wt%Ni+S and FCS is likely due to the non-metallic inclusions which encourage the formation of damage within the material during tensile testing

Figure 4.61 Stress strain curves of the three materials

### Deformation comparison between the simulation alloys and FCS

Both FCS and Fe-30wt%Ni showed more uniform plastic deformation along the gauge length of the tensile specimens before failure compared to Fe-30wt%Ni+S. Figure 4.62 shows that both the FCS and Fe-30wt%Ni specimens failed through localised necking while several cracks were observed along the gauge length for Fe-30wt%Ni+S.

Figure 4.62 Micrograph of tensile specimens before failure

Figure 4.63 a shows the micrograph of FCS before deformation and Figure 4.63 b the same area of the microstructure close to failure. Results show crack propagation across a grain highlighted by the red box. On the other hand, Figure 4.64 shows the progressive deformation of Fe-30wt%Ni with a grain highlighted with a red arrow where a crack eventually form as shown in Figure 4.65. These results show that Fe-30wt%Ni heavily deforms before transgranular damage is generated (Figure 4.65). Figure 4.66 shows the deformation of Fe-30wt%Ni+S as the tensile force increases. Damage starts either through debonding of the interface between inclusions and the steel matrix or through rupture of the inclusions, followed by relatively fast  coalescence of inclusions-induced damage as shown in Figure 4.66. Due to the particular distribution pattern of inclusions in Fe-30wt%Ni+S, which appear to be located along grain boundaries, as discussed in section 3.2.1.1, it therefore seems that cracks in this material are formed along grain boundaries at room temperature due to the coalescence of damage initiated by inclusions.

Figure 4.63 Micrograph of FCS a) before deformation and b) close to failure

Figure 4.64 Progressive deformation of Fe-30wt%Ni

Figure 4.65 Progressive deformation of region A in Fe-30wt%Ni

Figure 4.66 Progressive deformation and damage found in Fe-30wt%Ni +S

During the tensile test on FCS, damage is first found along the interface between inclusions and the steel matrix. Figure 4.67 shows clear separation of the inclusion from the steel matrix in FCS. The local strain to form a void is as low as 1% in Fe-30wt%Ni+S and 2.7% in FCS as shown in Figure 4.68 b and c. These results show the important role of inclusions in void formation.

Figure 4.67 Inclusions before and after deformation in FCS

Figure 4.68 a) Damage formation around inclusions in FCS b) Measured local strain right before damage formed in FCS c) Measured local strain right before damage formed in Fe-30wt%Ni+S

Void formed around inclusions can also generate shear localisation between two inclusions located close to each other, which is the classical mechanism for void coalescence for ductile fracture.  Figure 4.69 shows that as the load was applied along the Y direction, a 45 degree shear band was generated to connect two voids formed around inclusions in FCS.

Figure 4.69 The development of local shear band in between inclusions in FCS

The role of inclusions in crack formation can be fully demonstrated in an in-situ tensile test. Figure 4.70 a shows the surface of FCS before the final crack is formed and Figure 4.70 b shows the same area after fracture. Both figures are highlighted with purple boxes which show identical regions of inclusions before and after fracture. The yellow boxes indicate the subsurface inclusions which were only revealed after the FCS is fractured. Last but not least, the red lines indicate the fracture path of FCS based on the image after fracture.

These results show that the inclusions play a major role in void formation with very clear plastic deformation in the matrix in the form of shear bands in between inclusions with void coalescence influencing the final crack path.

Figure 4.70 a) FCS microstructure before fracture  b) failure cracks after propagation in the same region

Figure 4.71 shows the strain-yy distribution across the microstructure of FCS obtained with DIC. This result clearly demonstrates the 45o shear bands that joint up the voids around the inclusions. In addition, Figure 4.71 also shows that the localised strain values can be as high as 80% just before fracture. This result further demonstrates the key role played by inclusions on both strain localisation in the steel matrix and damage development in FCS.

Figure 4.71 Strain-yy distribution across the microstructure of FCS

Plastic deformation of the steel matrix leads to void growth as shown in Figure 4.72. At room temperature, grain boundaries did not show any particular influence on damage propagation.

Figure 4.72 Progressive local deformation of FCS

In order to validate the DIC strain calculations, another tensile test was conducted with 10 microns pitched microgrids deposited onto a chemically etched FCS. Figure 4.73 a shows the area of focus for FCS before deformation with un-deformed microgrids and Figure 4.73 b shows the same microstructure after deformation up to the Ultimate Tensile Strength (UTS) (Figure 4.74). DIC was also conducted on this area.

Differences between the two strain measurement techniques are related to the resolution of the two techniques. DIC provides a higher spatial resolution over the microgrid technique. However, strain values might not be accurate at the scale of microstructures as, for instance, microstructural features might not be randomly distributed and they must therefore be checked using an independent technique such as the microgrid technique used in this work, which can directly measure absolute strain values without interpolation and optimisation procedures.

Figure 4.73 Etched FCS with microgrid a) before deformation and b) after deformation up to the UTS

Figure 4.74 Force-extension curve for FCS showing the regular intervals to take images for DIC analysis

Strain maps were therefore produced using two independent full-field strain measurement techniques. Figure 4.75 shows the comparison for the strain-yy distribution map obtained using both DIC and Microgrids. The pattern of the strain distribution maps produced by each technique shows good agreement with similar strain ranges. The slight difference between the two strain maps is likely due to higher spatial resolution provided by DIC (1.5 micron pitch size for the grid generated by the centres of all interrogation windows) compared to the 10 micron pitch size of the microgrids. Nevertheless, such results give confidence in the strain measurements obtained using DIC which made use of the natural features of the microstructure for the correlation.

Figure 4.75 Strain-yy map measured by a) DIC b) Microgrid

In order to extract quantified information from this test, the image of the microstructure has been processed using SigmaScan Pro 5 [100] and ‘digitalised’ using the Matlab code code by Chalon [101] into 3 different phases: into 3 different phases: Ferrite, Pearlite and inclusions (section 4.2.4.1 demonstrated the separation between two phases).

This Matlab code was a useful tool for separating and identifying the different phases. However, it can only identify no more than 2 phases within an image. Therefore, in order to use it to analyse the 3 phases of FCS, the Matlab code was run 3 times instead of just once. In the first step, Ferrite was identified by excluding both inclusions and Pearlite using the image in Figure 4.76 a. Then, inclusions and pearlite can be separately identified as shown in Figure 4.76 c and d respectively. Coordinates for each phase are recorded in an output file which can be read in Excel.

Figure 4.76 Process for digitally separating the 3 phases of FCS: a) original micrograph of the microstructure, b) Ferrite in white, c) inclusions and d) Pearlite

360,000 coordinates points (or pixels) were generated by the MATLAB code. The area ratio of each phase was recorded as 71 : 6 : 2 (ferrite : pearlite : inclusions). Each point was associated with one strain value recorded by DIC and a strain histogram was produced as shown in Figure 4.77 b. As local strains could not be resolved within inclusions due to the lack of features to enable the correlation to work, strain values in the ferrite, 1.5micron away from inclusions, have been recorded separately to show the influence of inclusions on strain localisation. The corresponding histogram is referred to as “Ferrite around inclusions” in Figure 4.77 b. Results show that the histogram for the pearlite phase is slightly shifted to the left compared to that for ferrite away from inclusions with a mean value for Pearlite at about 11% and for ferrite at about 16%. However, the histogram for “ferrite around inclusions” clearly shows the strain concentration effect generated by the inclusions with a mean value of about 20% and a high fraction of high strain values. This result therefore clearly demonstrates the influence of inclusions on strain localisation during the deformation of FCS at room temperature.

Additionally, an independent result obtained through manual separation of the phases highlighted in red (inclusions) and purple (pearlite) is shown in Figure 4.77 c. 79 x 100 grids covered the microstructure. Each grid element was then associated with one strain value recorded by the microgrid measurements and a strain histogram was produced as shown in Figure 4.77 d. Similarly to the DIC results, the histogram for the pearlite phase has a lower mean value of about 8.4% while the mean strain value for “ferrite away from inclusions” is about 13.5%. Once again the histogram for “ferrite around inclusions” clearly shows the strain concentration effect generated by the inclusions with a mean value of about 18.7% and a high fraction of high strain values as in the DIC results.

Both independent results obtained from DIC and microgrids show that regions associated with pearlite experience less deformation in comparison with the higher strain values recorded in the ferrite matrix. In addition, both results agree that inclusions play a major role in strain localisation in the ferrite phase.

In conclusion this chapter has reported an extensive number of novel experimental results, given the new experimental procedures developed in this work, about the deformation and damage of FCS, and related simulation materials, at both high and room temperatures. New insight has been generated into the local plastic deformation which takes place in the microstructure of these steels and which affects subsequent damage formation. Strain distributions and localisation have been quantified through rigorous analysis and the effect of inclusions and grain boundaries on damage formation have been identified over a wide range of temperatures. This new insight will be used for the discussion reported in the next chapter.

Figure 4.77 a) Strain-yy map  superimposed onto the filtered micrograph, b) strain histogram of each phase using DIC, c) manual phase separation with pearlite and inclusions highlighted  and d) strain histogram of each phase using microgrids

### Summary

Local strain measurements have been successfully carried out using both DIC and microgrid techniques at room temperature with similar results which have been quantified. Local deformation in FCS is highly dependent on the local microstructural features such as ferrite, pearlite and inclusions when deformation takes place at room temperature. The strong effect of MnS inclusions on both strain localisation and damage formation has been observed and analysed both qualitatively and quantitatively, showing a complete change of damage formation mechanism in the microstructure of FCS with respect to the high temperature tests.

Chapter 5

# Discussions

This chapter has been divided into three parts. First, the new experimental procedures developed in this work to study hot deformation and damage in FCS and associated simulation materials are reviewed. The second part of the discussion is then focused on local deformation mechanisms observed in this work and the third part on damage mechanisms.

## Mechanical testing procedure

Results reported in chapter 4 have shown that the new experimental procedure developed in this work in terms of combining compression testing on tapered specimens with microgrids successfully enable intra-granular strain measurements after the hot deformation of steels at temperatures and deformation conditions representative of those leading to edge cracking in FCS during industrial rolling. Tests conducted in air with the TMC machine showed the limitations of this testing procedure. Even though successful intra-granular strain measurements have been obtained at high temperature in this work (1000⁰C on Fe-30wt%Ni –  Figure 4.6) and in other published studies [86, 87, 104-106] under plane strain compression, local strain measurements close to the edge of the specimen could not be obtained due to oxidation problems, despite several attempts. It is believed that the penetration of oxygen into the surface, especially in conjunction with damage formation, is too fast at high temperature and the subsurface of the specimen is quickly oxidised, therefore not enabling the study of early damage development from the edge of the specimen. These frustrating results, given the amount of time required to prepare and test a single specimen, then led to the testing procedure conducted under vacuum using the Gleeble machine. Given the successful results obtained using the Gleeble machine, it is clear that this testing procedure represents the way forward to analyse the conditions for edge cracking in hot rolled steels. Although such testing procedure brought some physical insight into damage development in the past by demonstrating that specimens with a tapered shape could generate the stress triaxiality levels required to develop edge cracking [10-12, 18], results obtained in this work have revealed and quantified for the first time the local strain distributions that takes place at the scale of the microstructure during compression at high temperatures (e.g. Figure 4.6) in conjunction with the very early phase of damage formation at the surface of the specimens (e.g. Figure 4.48). The combination of these observations with finite element simulations of the deformation of the specimen, validated by experimental measurements of strain distributions across the thickness of the specimens (Figure 4.34 and Table 4.2), have allowed the confirmation that edge cracking takes place for stress triaxiality levels ranging from 0.3 to 0.5 as reported by Farrugia et al. [18]. This new procedure coupling FE simulations with microgrids located at the surface of specimens deformed under vaccum therefore provides the means to study damage development under mechanical conditions representative of edge cracking during rolling. Moreover, gold microgrids used for the first time at temperatures up to 1000⁰C do not influence damage or microstructure evolution unlike etched microgrids used in previous studies [86, 94]. Even though damage was clearly observed at the surface of the specimens, initiation conditions for local damage could not be studied accurately. However, results obtained after a two-pass testing procedure, although not fully exploitable due to the long interval (several months) between the two passes (Figure 4.49), have revealed that it would be possible to study damage development as a function of strain localisation in the microstructure of the hot deformed steel, using a multi-pass testing procedure in the Gleeble machine. Results obtained in Figure 4.49 appear to show new cracks nucleated after the second pass. Analysis of the strain map (Figure 4.48 d) after the first pass in relation to the new crack locations after the second pass has revealed that cracks have nucleated along grain boundaries in regions of relatively small strain values (strain-xx < 25%).  It is worth pointing out that the new cracks might have already nucleated after the first pass but could not be seen due to the lack of resolution of the image

## Local Deformation

The local deformation of the microstructure of FCS and simulation materials has been quantified in this work at high temperature using the microgrid technique and at room temperature using both microgrid and DIC techniques. The procedure used, which superimposes strain maps over the microstructure of the various materials, has enabled the identification of the effect of microstructural features on strain localisation which would not be observed otherwise. Previous published work on the study of hot damage in FCS was limited to microstructure and damage observations without strain quantification [10, 12, 20, 37, 107], apart from one study which made use of x-ray tomography combined with in-situ tensile testing which managed to capture three-dimensional strain distributions within FCS based on inclusions movement [54]. However, results were limited to tensile testing which are not representative of hot rolling conditions and therefore provided limited information for the validation of models at the scale of microstructures [12, 15, 60].

Given that the overall stress strain curves for the three materials investigated were most similar at 1000oC (Figure 4.2) and given that FCS is expected to be in a fully austenitic state at this temperature, most strain maps have therefore been produced at this particular temperature. The simulation materials were indeed produced to simulate the behaviour of FCS in its austenitic range. Moreover, the overall stress/strain curves for the two simulations materials did not show any sign of dynamic recrystallisation which was ideal for the use of microgrids for local strain measurements, as microgrids might have disappeared where new recrystallised grains appear in the microstructure. The same problem with microgrids was expected during the phase transformation of FCS upon heating or cooling. This is why Fe-30wt%Ni and Fe-30wt%Ni+S were produced in order to simulate the behaviour of the austenitic phase of FCS when the test temperature is above 910⁰C, while preserving the microgrids upon heating and cooling.

Strain distribution maps produced at 1000oC, especially for Fe-30wt%Ni, showed that very large plastic deformation (strain-yy values of about 80% for 25% applied strain) takes place along grain boundaries in the austenite phase at this very high temperature, which was quantified for the first time in this work (Figure 4.48). Besides grain boundaries, high localised strains are also found along some twin boundaries (Figure 4.48), which is identical to Hernandez-Castillo’s findings [94].

Phase transformation was indeed observed during the compression test carried out on the Gleeble machine at 850oC (Figure 4.18) where microgrids partially disappeared in some areas of the microstructure. It is assumed that transformation into austenite took  place in these areas upon heating while the areas with still visible microgrids might correspond to non-transformed ferrite grains. Another test carried out at 1000oC on FCS further confirmed this result with the microgrid totally disappearing in the steel matrix while some microgrids were still visible in some of the inclusions (Figure 4.19). However, FCS seemed to experience less strain localisation at 1000oC compared to the result at 850oC as less intense shear bands and damage were observed (Figure 4.30 d and e). Surprisingly another test carried out at 850oC on FCS with a much coarser pitch grid (20 microns as opposed to 2.5 microns in previous tests) showed highly visible microgrids in all areas of the microstructure after the test (Figure 4.23). This unexpected result has enabled the quantification of local strain distributions in the microstructure of FCS with clear evidence of strain localisation in the form of bands running at 45o with respect to the compression axis (Figure 4.43 c). Two types of such bands were observed. One type was due to the particular distribution of MnS inclusions arranged along a line orientated at 45o with respect to the compression axis, which has led to local strain localisation. This result therefore shows the important effect of the spatial distribution of inclusions on strain distributions as also reported in [12, 15]. The other type of bands seemed to be more representative of the deformation of the steel at 850oC with intense bands of deformation (with equivalent strain values up to 100% for 25% applied strain) similar to those observed in the transformed (austenite) phase test carried out at the same temperature with the 2.5 micron pitch grid, which showed intense deformation patterns running at 45o through large areas of the transformed phase (Figure 4.43 b). Unfortunately, this unexpected result was obtained very late in the project and further tests would have to be conducted with an etched microstructure to identify the location of these high strain values with respect to the underlying microstructure. The latter type of deformation bands has also been observed in the austenitic steel Fe-30wt%Ni deformed at 1000oC, therefore without any effect of MnS inclusions, with high strain values (80% for strain-yy) very much localised along grain boundaries (Figure 4.44 d). This result therefore seems in line with the interpretation that the transformed phase observed in Figure 4.43 b would correspond to the austenitic phase. Results from the tests carried out on Fe-30wt%Ni+S at 1000oC with detailed analysis of the effect of inclusions on strain distributions revealed that inclusions had very little effect on strain localisation in the austenitic matrix (Figure 4.41) despite the high density of inclusions seen in the image. This seems in contradiction with microstructural modelling studies carried out on FCS at high temperatures where the spatial distribution of inclusions showed significant effects on strain localisation [12, 15]. More experimental results would be needed to draw a final conclusion as the analysed area is rather small but these unique full-field strain measurements demonstrate how useful these experimental results are, in terms of both strain maps and histograms, in order to provide insight and validation means for microstructural models. However, results obtained at room temperature after tensile testing carried out on FCS have clearly revealed the strong effect of inclusions on strain localisation both qualitatively (Figure 4.77 a) and quantitatively (Figure 4.77 b) .  These two results seem to suggest that the strain localisation generated due to inclusions in FCS at 850oC may have taken place in a non-transformed (ferrite phase) area of the microstructure where inclusions would have a stronger effect on strain distributions. These interpretations would, of course, need more evidence by conducting further tests. Strain quantification in inclusions at both high and room temperatures was very limited in this work. At room temperature the lack of features inside inclusions has prevented the correlation to work for DIC analysis while the microgrid pitch at both room and high temperature was not fine enough to resolve strain distributions within inclusions. However, very few microgrids were still visible in some of the largest inclusions after deformation at 1000oC on FCS (Figure 4.20). Very small strain values have been recorded for these inclusions (-3.75% along the y-axis and 1.3% along the x-axis) which seems very surprising as MnS inclusions are known to be highly deformable as commonly seen after an industrial rolling process, or in some of the published modelling work [15],  but also in Figure 4.55 after cutting the Gleeble specimen along the middle plane (ND, TD) to visualise inclusions away from the edge of the sample. Interestingly, while inclusions towards the centre of the specimen were very elongated, inclusions close to the surface along the TD direction were more spherical in shape. The analysis of FE results in terms of stress triaxiality variation along TD has revealed that compressive strain-zz (strain along TD) values are generated close to the edge of the specimen during the compression due to the tapered shape of the Gleeble sample. It is therefore very surprising that the inclusions at the surface are not more elongated than the measurements show along the x-direction. This might be due to the rupture of the interface between the inclusions and the matrix during thermal etching as observed during this work (Figure 4.17). It has been indeed observed in Figure 4.55 that all sub-surface inclusions remain perfectly attached to the matrix during the applied compression.

## Damage mechanisms

Results reported in Chapter 4 have provided much insight into the mechanical conditions and mechanisms controlling damage development in FCS from temperatures typical of hot rolling forming operations down to room temperature. Results have confirmed Farrugia’s findings as they showed that damage is generated in FCS under stress triaxiality levels ranging from 0.3 to 0.5 and equivalent strain values above 2 to 3% (Figure 4.44 and Figure 2.8 b) [18]. Results for plane strain conditions have also confirmed that critical conditions were not met for damage formation as no damage was observed during this work on the middle plane (ND,RD) of the TMC specimens after the tests. Further observations of local damage through the TD direction in the Gleeble FCS specimen have revealed the extent of damage below the surface (about 300 microns) which closely matched the region of stress triaxiality values ranging from 0.3 to 0.5 in the FE model. Results from TMC tests, although mostly unexploitable in terms of damage development, have, however, revealed the difficulty and complexity of the study of edge cracking in air, which correspond to the real situation during industrial rolling, due to the influence of oxidation on crack development (Figure 4.12).

Results obtained in this work have highlighted the effect of thermal etching for all tests carried out at high temperature on polished surfaces. Although thermal etching has been a useful means to reveal austenite grain boundaries (Figure 4.17) at high temperature,  it has also generated debonding of the interface between inclusions and the surrounding steel matrix (Figure 4.24 b). Such damage nucleation mechanism observed at the surface of the specimens due to the applied temperature before any strain was applied may be explained by McLean [22] who explained that there is a thermal effect on the surface tension of materials. Such damage mechanism has therefore likely influenced the formation of cracks along grain boundaries in Fe-30wt%Ni+S and FCS tested at 1000⁰C due to the presence of inclusions along what has been thought to be grain boundaries (Figure 4.32 and Figure 4.26). However grain boundary damage has also been observed in Fe-30wt%Ni without the presence of inclusions. It therefore appears that grain boundary cracking is an inherent damage mechanism at 1000⁰C for these three materials investigated in this work. These results are different from those published in [11, 12, 18, 54] where the main damage mechanism was due to inclusions in FCS at high temperature, despite similar stress triaxiality conditions. Damage along grain boundaries in FCS has also been reported in other studies at high temperatures in both tensile [37] and compressive [11] modes, even though the fraction of grain boundary damage is higher in the current work in comparison with these published studies. Liu et al. [37] who run tensile tests on FCS at 1000oC at two very different strain rates of 0.1s-1 and 10s-1 concluded that damage along grain boundaries is mostly observed at the lower strain rate with only very limited grain boundary damage at the higher strain rate. According to these published results it is therefore possible to observe grain boundary damage in FCS at 1000oC for the strain rate of 1s-1 used in this work even though it is expected to be more limited than that observed in this work. The difference might be due to the fact that the current work mainly studied damage on the specimen surface while all the previous studies analysed damage after specimen sectioning (e.g. subsurface observation). It is also possible that surface tension effects at high temperature, as reported in [22], might have played a role in favouring the formation of damage along grain boundaries in this work. Additionally, a suggestion for a physical explanation of damage propagation along grain boundaries is provided by Cho [42] who claims that cracks propagate through areas of microstructures where there is concentration of high energy boundaries in hot rolled austenitic steels. Observation of the microstructure in the FCS cut along the mid-plane (ND,TD) of the Gleeble specimen in this work have also revealed some grain boundary cracking (revealed through etching carried out on the (ND,TD) plane) at the sub-surface of the specimen (Figure 4.57). Intra-granular cracking was also observed, in one instance and very locally, further away from the surface in a region where damage had taken place around inclusions (Figure 4.58). Damage/crack mechanisms associated with inclusions found at the subsurface are similar to the results reported in [11, 12, 18, 54]. The proportion of inter-granular cracking in this work, however, is therefore in contradiction with Liu et al.’s suggestion that tests conducted at strain rate higher than 0.1s-1 show less grain boundary damage than that generated by inclusions. Observations made on the same FCS specimen in this work have also confirmed the effect of thermal etching on inclusions damage observed at the very surface of the specimen since debonding of the inclusions was not observed below the surface.

Further tests would be required to study rigorously the effect of strain rate on grain boundary cracking, as strain rate was proven to have a direct effect on damage formation in [108]. Among the wide range of strain rates experienced by FCS during industrial hot rolling (from 0.1 to 10s-1), a single strain rate value of 1s-1 was selected for this work in order to limit the number of tests. This value was selected to study damage formation during the early stages of rolling as strain rates during roughing rolling vary between 0.1 and 5s-1 [14].

Results from Figure 4.30 d and e have clearly shown that the mechanisms for crack formation in FCS at the surface of the Gleeble specimens change with temperature as much fewer cracks are observed at 850oC compared to the test carried out at 1000oC, especially in the transformed region (austenite). This effect might correspond to the strengthening of grain boundaries as the temperature decreases, as suggested through the concept of ECT in [4].  Although some cracks have been observed in FCS deformed at 850oC (Figure 4.18 b and Figure 4.30 b), it is not clear at this stage what damage mechanisms have led to the formation of these cracks and further tests would be needed after revealing the microstructure through etching (and with microgrid).

One result, however, suggests that crack formation in the non-transformed region takes place through trans-granular cracking (Figure 4.30 a and b). Another result in the transformed phase suggests a stronger influence of the inclusions on crack formation at this temperature (Figure 5.1 a). A crack seems, indeed, to link two voids created around inclusions, in a similar way to that observed at room temperature during tensile testing (Figure 5.1 b). Such finding is in line with  Foster et al.’ s results [12] who studied damage coalescence between inclusions during the hot rolling of FCS. However the fact that coalescence was not observed experimentally at 1000oC between voids generated around inclusions seems in contradiction with simulations results reported in the literature [11, 12, 18, 54].

Figure 5.1 Coalescence of damage between inclusions at a) 850⁰C and b) room temperature

Results obtained at room temperature through tensile testing have clearly revealed the strong influence of MnS inclusions on strain localisation and subsequent damage development through, purely, intra-granular cracking in FCS (Figure 4.71 and Figure 4.70). It is therefore clear that damage mechanisms at the surface of the tested specimens change from intergranular to transgranular between high and room temperature.

Although debonding of the interface between inclusions and the steel matrix has been observed at high temperature at the surface of the Gleeble specimens due to thermal etching, sub-surface observations on FCS at 1000oC have revealed a stronger cohesion of the interface with no voids observed around MnS inclusions which were very elongated towards the centre of the specimen. Results at room temperature after tensile testing have revealed that debonding of the interface takes place as an early form of damage after 2.7% local strain in FCS (Figure 4.68), due to the incompatibility of plastic deformation between inclusions and surrounding steel matrix under tension at room temperature. Voids are therefore generated and grow, as for the high temperature tests after voids created through thermal etching, due to plastic deformation of the steel matrix (Figure 4.67 and Figure 4.19 a) to a large extent without crack formation. Stress triaxiality levels ranging from 0.3 to 0.5 under compression tests at high temperature led to local void opening around inclusions, which is similar to Kaye’s results who suggests that void opening around inclusions is expected when stress triaxiality levels are positive [11], [12, 18]. The voids extension found around inclusions in the current work at high temperature is also similar to that found in Liu et al.’s results [37] but with shorter void length since Liu et al.’s tests were conducted in tensile mode (stress triaxiality of 0.33 to 1.5). Voids generated in a tensile specimen are extended along the tensile direction as seen in the tensile test results obtained at room temperature in this work (Figure 4.67). Following void growth at room temperature, unlike observations made at high temperatures, strain localisation then takes place between voids (Figure 4.71) leading eventually to coalescence (Figure 4.69 and Figure 4.70)  as in the classical theory of ductile damage development. The formation of damage which progressively transforms into cracks go through three stages: Nucleation, growth and coalescence [12, 24, 26, 27]

In summary, tests at three temperatures were conducted in the current study with the aim to understand the temperature effect on damage mechanisms in FCS. At 1000⁰C, when FCS is fully transformed into an austenitic steel, grain boundary damage dominates at the surface of the specimens with minor inclusions-induced damage. Inclusions showed minor effect on the formation of major surface cracks unless they are located along grain boundaries. However, inclusions may influence propagation as observed at the sub-surface of the Gleeble specimen on FCS. In contrast, at 850⁰C when FCS is only partially transformed, less obvious damage was observed on the surface of the specimen but more shear bands were generated in the transformed phase. These results may suggest that hot rolling conducted at 850⁰C will produce less cracks compared to hot rolling conducted at 1000⁰C. However, results also showed that at 850⁰C, only the transformed phase is heavily deformed while the non-transformed phase has relatively minor deformation (by looking at the relatively small distortion of the grids in Figure 4.18 b). This means that deformation is much more heterogeneous in the two-phase microstructure of FCS when the steel is rolled at 850⁰C. On the other hand, the effect of inclusions on strain localisation is more important at 850⁰C, especially in the non-transformed phase, and definitely predominant at room temperature. The final tests conducted at room temperature were helpful in observing the development of local deformation and the influence of inclusions in progressive damage formation. Moreover, they showed some common features to those found in FCS tested at 850⁰C. The main similarity observed between the test carried out at room temperature and at 850⁰C, despite the different loading modes, is the formation of shear bands across wide areas of the microstructure (Figure 5.2 c and f) and some transgranular crack formation (Figure 5.2 a,b and d,e). Plastic deformation through the formation of very large shear bands was not as obvious at 1000⁰C. Thus, 850⁰C may be a transition temperature in terms of modes of deformation and damage in the microstructure of FCS. The impact of inclusions on local deformation and damage mechanisms on the surface of FCS decreases as the temperature rises. For instance, at room temperature, the damage mechanism of FCS is dominantly associated with inclusions as shown in Figure 5.3 a. At 850⁰C, inclusions still alter local strain distributions but higher strain localisation is found within the transformed phase as highlighted with yellow arrows in Figure 5.3 b. Finally, instead of inclusions, austenitic grain boundaries are dominating damage formation at 1000⁰C as shown in Figure 5.3 c with, in general, little effect of the inclusions unless they are located along grain boundaries.

Figure 5.2 FCS a) before and b) after deformation with c) observed shear bands at room temperature. FCS d) before and e) after deformation with f) observed shear bands at 850⁰C

Figure 5.3 FCS microstructure deformed at a) room temperature, b) 850⁰C and c) 1000⁰C

Figure 5.4 a summarises on a schematic drawing the damage mechanisms observed experimentally in this work in FCS at 1000oC, which provides physical insight into the early development of damage from the surface, which has never been observed in previous studies, and at the sub-surface in relation to previous studies, with key input from the literature review to provide a physical explanation for the damage mechanism observed at the surface. These results therefore provide much insight into the development of damage in FCS at temperatures and deformation conditions representatives of those leading to edge cracking in industrial rolling. There are in line with results from Farrugia [14] who stated that subsurface inclusions can be a catalyst to damage nucleation leading to corner cracking, with the additional effect of grain boundaries clearly discovered in this work.

Figure 5.4 a) Schematic of damage mechanism observed in this work at 1000oC at the surface and subsurface with references b) [22] c) [42] d) [56] e) [10] f)[54]

## Summary

The novelty of this work relates to the experimental evidence of a significant change in damage mechanisms in FCS with temperature along with a strong surface effect when tests are conducted at high temperatures. Inclusions do play a major role in damage formation at room temperature while for high temperature, namely 1000⁰C, their contribution appears negligible in comparison with damage generated along grain boundaries at the surface. Their influence seems to be, however, more significant away below the surface even though more test would need to be conducted to confirm this conclusion. The new experimental procedure developed for full-field strain measurements at the scale of the microstructure at high temperature seems to confirm this result with a negligible effect of inclusions on strain localisation as opposed to room temperature results where cracks propagate along shear bands generated between inclusions after large deformation.

Chapter 6

# Conclusions and Future Work

## Conclusions

Edge cracking taking place during the industrial rolling of FCS is strongly influenced by both stress triaxiality conditions and microstructure. Previous works showed that stress triaxiality levels generated at the surface of compressed specimens at high temperature could generate the required conditions for damage initiation, representatives to those leading to edge cracking during industrial rolling. This work has therefore made used of these tests to focus the analysis on damage development at the scale of the microstructure in FCS. A new approach has been developed to study, for the first time, the formation of damage in relation to local strain distributions in hot deformed microstructures using a microgrid technique. Results from this work have shown that hot compression carried out on specially designed tapered specimens did generate damage from the surface. However, tests had to be eventually conducted under vacuum to generate useful and quantifiable results. Therefore, most of the tests have been conducted on a Gleeble machine with microgrids located on the external surface of the specimens where stress trixiality levels ranging from 0.3 to 0.5, calculated through FE simulations, have been generated to initiate and propagate damage. Two simulation materials, Fe-30wt%Ni and Fe-30wt%Ni+S, were also used in this work to study the deformation of the austenite phase of FCS at high temperatures, as the stress/strain curves for the three materials were similar at 1000oC, without the issue of phase transformation taking place in FCS upon heating and cooling, which could make the microgrids disappear. Results have also shown that, for the first time, gold microgrids with a pitch ranging from 2.5 microns to 20 microns could withstand temperatures up to 1000oC without any problems during the large compression applied. While etched microgrids were used in previous studies for hot plane strain compression tests, gold microgrids are a much better option as they do not affect microstructure evolution, including damage formation, at the scale of the microstructure. Strain maps and histograms have been produced over large areas of the microstructures with a relatively fine pitch to study the effect of microstructures on strain localisation at both small and large scales. Strain measurements carried out over a large scale have also enable the validation of FE calculations in terms of strain prediction.

Additional tensile tests were also carried out at room temperature in a SEM with local strain measurements obtained using DIC as the technique offers a much better spatial resolution compared to the microgrid technique, although DIC could not be used at high temperature. Results from DIC were however validated using the microgrid technique at a relevant scale as DIC is a non-direct strain measurement technique which computes strain values through an optimisation algorithm for the correlation of images using the natural features of microstructures. These original results at room temperature, despite being obtained under tensile loading, provided further insight into the change of deformation and damage mechanisms with temperature in FCS.

Strain map results have revealed high deformation heterogeneity in all studied microstructures and at all temperatures. High strain localisation was observed along grain boundaries in Fe-30wt%Ni at 1000oC with strain—yy values as high as 80% for 25% applied strain. Results also revealed the unexpected appearance of clear grain boundary cracking on Fe-30wt%Ni but also in FCS. This result is a clearly novelty compared to previously published studies, especially for the relatively high strain rate of 1 s-1 constantly used in this work. Intergranular damage propagation was also observed in FCS at the sub-surface after cutting the specimen along the middle (ND,TD) plane and revealing the microstructure through etching. However, intragranular damage was also observed around inclusions further away from the surface of the specimen. Inclusions at the surface did not seem to influence strain localisation in the microstructure, as revealed by strain measurements carried out on Fe-30wt%Ni+S. However, it is worth pointing out that the spatial distribution of inclusions in the as-cast Fe-30wt%Ni+S differ from that in FCS and further work would be needed to confirm this conclusion. Void formation around inclusions was, however, observed at the surface of the specimen due to thermal etching. Void growth around inclusions at the surface was observed due to plastic deformation of the steel matrix but did not generate any cracks.

A two-pass compression test was attempted to study damage development at the surface but, unfortunately, the microgrid visibility was not good enough after the second pass. However, new damage sites seem to appear after the second pass at grain boundary locations where strain-xx values after the first pass were relatively low (below 25%). This result also demonstrates that damage development, including nucleation and propagation, could be studied in the future by better controlling the newly developed experimental procedure.

Compression tests carried out on FCS at 850oC showed very surprising results as far as the microgrids are concerned. While microgrids with a 2.5 micron pitch partially disappeared, as expected due to partial phase transformation, microgrids with a 20 micron pitch remain entirely visible after the test. This unexpected result has therefore enabled the quantification of strain distributions in the microstructure of FCS at 850oC and offer new opportunities to study the high temperature deformation of microstructures in transformable metals in the future. High local equivalent strain values of about 100% were also measured in the microstructure of FCS for 25% applied strain but much fewer damage sites were observed in comparison with the test at 1000oC. Much more intense and larger shear deformation bands were observed in the transformed phase of the microstructure in comparison with results obtained at 1000oC in FCS. As for the non-transformed phase, clues about a clear effect of the spatial distribution of inclusions on strain localisation and the formation of intragranular cracking were revealed. These latter results are in line with observations made at room temperature after the tensile tests conducted in the SEM. Results also showed high strain localisation in the microstructure of FCS with strain values along the tensile direction as high as 80% locally in the necking region, just before fracture. Strong influence of the inclusions on strain localisation, which was quantified through both DIC and microgrid analyses, and subsequent coalescence and fracture was also revealed.

Results obtained in this work have therefore highlighted and analysed in detail, for the first time, the change in deformation and damage mechanisms operating in FCS with temperature. Apart from the new physical insight gained in the experimental work carried out in this study, strain maps and distributions provide invaluable results to inform and validate microstructural models of the deformation and damage of FCS at high temperature. It is believed that the development of such sound microstructural models will lead to a breakthrough in the understanding and prediction of edge cracking during rolling in the future.

## Future work

Given the broad range of tests conducted in this study, there are various avenues for future research. Tests on the Gleeble machine for FCS at temperatures of about 1000oC with etched microstructure and a coarse microgrid pitch would need to be attempted based on the unexpected, but unfortunately late in the project, results obtained in this work. Multi-pass tests should also be conducted in a controlled manner to analyse damage development, including nucleation and propagation, in relation to strain distributions in the microstructure as the two-pass test conducted in this work proved the feasibility of such experimental procedure. Specimens should be cut along mid-planes after each tests to systematically study sub-surface damage propagation. More tests should be conducted over a wider range of strain rates and temperatures as results in this work and from published studies have clearly shown the strong influence of these two variables on local deformation and damage in the microstructure of FCS. Should the proposed experimental procedure for FCS not be successful at temperatures as high as 1000oC, better simulation materials should be produced, especially in terms of the distribution and location of inclusions in the microstructure, by conducting a casting process under more controlled conditions, especially under vacuum. The microgrid pitch size should be reduced to resolve strain distributions within inclusions. This could be achieved by using a better SEM such as a FEG-SEM. As for DIC, additional features could be generated within inclusions at room temperature to enable better image correlation. Finally, microstructural modelling should be conducted in conjunction with the experimental results obtained in this work and through x-ray tomography, for three-dimensional measurements, to understand and predict damage development in FCS under thermos-mechanical conditions representative to those leading to edge cracking in industrial rolling.

# References

1.	World Steel In Figures 2015. 2015, Worldsteel association.

2.	https://www.lme.com/. Accessed May 2015

3.	H.K.D.H. Bhadeshia, R.W.K. Honeycombe, Steels: microstructure and properties. 3rd ed. 2006, Amsterdam: Butterworth-Heinemann.

4.	G.E. Dieter, Mechanical Metallurgy. SI Metric ed. 2001.

5.	B. Hwang, H.S. Lee, Y.G. Kim, S. Lee, Analysis and prevention of side cracking phenomenon occurring during hot rolling of thick low-carbon steel plates. Materials Science & Engineering, 2005. A 402: p. 177-187.

6.	S. Kalpakjian, S.R. Schmid, Manufacturing Processes for Engineering Materials. 5 ed. 2007: Prentice Hall.

7.	C. Moore, The commercial machinability and metallurgy of low carbon free cutting steel. 1968, University of Sheffield.

8.	E.P. Degarmo,  J.T. Black, R.A. Kohser, Materials and Processes in Manufacturing. 9th ed. 2003.

9.	M.C. Shaw, P.A. Smith, E.G. Loewen, N.H. Cook, The Influence of Lead on Metal-Cutting Forces and Temperatures. Transactions of the ASME, 1957. 79: p. 1143-1154.

10.	A.D. Foster, J. Lin, D.C.J. Farrugia, T.A. Dean, A Test for Evaluating the Effects of Stress-States on Damage Evolution with Specific Application to the Hot Rolling of Free-Cutting Steels. International Journal of Damage Mechanics 2011. 20: p. 113-129.

11.	M. Kaye, Advanced damage modelling of free machining steels. 2012, Imperial College.

12.	A.D. Foster, J. Lin, D.C.J. Farrugia, T.A. Dean, Investigation into damage nucleation and growth for a free-cutting steel under hot-rolling conditions. The Journal of Strain Analysis for Engineering Design, 2007. 42: p. 227.

13.	A.D. Foster, modelling of damage evolution under complex strain path and stress-states in hot deformation. 2007, Birmingham University.

14.	D.C.J. Farrugia, High temperature ductile damage during rolling of free cutting steels. Ironmaking & Steelmaking, 2010.

15.	D.C.J. Farrugia, Prediction and avoidance of high temperature damage in long product hot rolling. Journal of Materials Processing Technology, 2006. 177(1-3): p. 486-492.

16.	W.D. Callister, D.G.Rethwisch, Materials science and engineering : an introduction. 7th ed. 2007, John Wiley.

17.	H. Chandler, Metallurgy for the Non-Metallurgist. 1998: Materials Park.

18.	D. Farrugia, Z. Husain, V. Santisteban, J. Llanos, J. Bianchi, P. Vescovo, J.pera, J. Rodriguez-Ibabe, C. Revilla, J. Fredriksson, J. Demurger, R. Forestier, B. Kieber, PACROLP: the prediction and avoidance of cracking in long product hot rolling. 2009. p. 23-25.

19.	B. Masek, H. Stankova, L. Kruger, L.W. Meyer, Comparison of intensity of high temperature surface damage for 20MoCrS4 steel with varying parameters of dynamical heating. Materials Science and Technology, 2006. 22: p. 1444-1448.

20.	Y. Kim, H. Kim, S.Y. Shin, K. Rhee, S.B. Ahn, D.L. Lee, N.J. Kim, S. Lee, Formation Mechanisms of Cracks Formed During Hot Rolling of Free-Machining Steel Billets. Metallurgical and Materials Transactions A, 2012. 43A: p. 882-892.

21.	C. Garcia de Andres, F.G. Caballero, C. Capdevila, D. San Martin, Revealing austenite grain boundaries by thermal etching: advantages and disadvantages. Materials Characterization, 2003. 49: p. 121-127.

22.	D. McLean, Grain Boundaries in Metals. 1957, Clarendon Press.

23.	J. Cho, J.A. Szpunar, The effect of Grain Boundary Charactetr Distribution (GBCD) on Edge Cracking during Hot rolling of austenitic stainless steel. Materials science Forum, 2002. 408-412: p. 1365-1370.

24.	J. Lin, Y. Liu, T.A. Dean, A review on damage mechanisms, models and calibration methods under various deformation conditions. International Journal of DAMAGE MECHANICS, 2005. 14: p. 299-319.

25.	E. Maire, C. Bordreuil, L. Babout, J.C. Boyer, Damage initiation and growth in metals: Comparison between modelling and tomography experiments. Journal of the Mechanics and Physics of Solids, 2005. 53: p. 2411-2434.

26.	N. Schlu¨ter, F. Grimpe, W. Bleck, W. Dahl, Modelling of the damage in ductile steels. Computational Materials Science, 1996. 7: p. 27-33.

27.	H. Tinet, H. Klocker, J.L. Coze, Damage analysis during hot deformation of a resulfurised stainless steel. Acta Materialia, 2004. 52: p. 3825-3842.

28.	F.W. Brust, B.N. Leis, A new model for characterizing primary creep damage. International journal of fracture, 1992. 54: p. 45-63.

29.	M.F. Ashby, B.F. Dyson, Creep damage mechanics and micromechanisms. 1984, Pergamon.

30.	C.E. Pearson, Journal of the Institute of Metals, 1934. 54: p. 111.

31.	B.H. Cheong, Modelling of microstructural and damage evolution in superplastic forming. 2002, The University of Birmingham.

32.	V.N. Perevezentsev, V.V. Rybin, V.N. Chuvil'deev, The theory of structural superplasticity - II. Accumulation of defects on the intergranular and interphase boundaries. Accommodation of the grain-boundary sliding. The upper bound of the superplastic strain rate. Acta Metallurgica et Materialia, 1992. 40(895-905).

33.	J. Lin, A.D. Foster, Y. Liu, D.C.  Farrugia, T.A. Dean, On micro-damage in hot metal working Part 2: Constitutive modelling. Engineering Transactions, 2007. 55(1): p. 1-18.

34.	Y. Liu, A.D. Foster, J. Lin, D.C.J. Farrugia, T. A. Dean, On micro-damage in hot metal working Part 1: Experimental investigation. Journal of Engineering Transactions, 2006. 54(4): p. 271-287.

35.	S.L. Semiatin, V. Seetharaman, A.K. Ghosh, E.B. Shell, M.P. Simon, P.N. Fagin, Cavitation during hot tension testing of Ti–6Al–4V. Materials Science and Engineering, 1998. A256: p. 92–110.

36.	J. Ochoa, Hot workability of sulphur containing free-cutting steels. 2002, The University of Sheffield.

37.	Y. Liu, J. Lin, T.A. Dean, D.C.J. Farrugia, A numerical and experimental study of cavitation in a hot tensile axisymmetric testpiece. The Journal of Strain Analysis for Engineering Design, 2005. 40: p. 571-586.

38.	D. Krajcinovic, S. Mastilovic, Some fundamental issues of damage mechanics. Mechanics of materials, 1995. 21: p. 217-230.

39.	K. Hellan, Introduction to fracture mechanics. 1984, Norway.

40.	J.A. Szpunar, D.C. Hinz, Correlation between the Texture and Plastic Anisotropy in Rolled Brass. The journal of the materials 1990. 42: p. 40.

41.	P. Blandford, J.A. Szpunar, D. Daniel, J.J. Jonas, Textural Inhomogeneity and its Influence on the Prediction of Plastic Anisotropy. Textures and Microstructures, 1991. 14-18: p. 525-530.

42.	J.Y. Cho, H.T. Jeong, J.A. Szpunar, Effect of Through Thickness Inhomogeneity of Texture on Edge Cracking during Planetary Hot Rolling of Austenitic Stainless Steel, in Proceedings of the Twelfth International Conference in Textures of Materials (ICOTOM-12). 1999. p. 1254-1259.

43.	K.A. Bywater, T. Gladman, Influence of composition and microstructure on hot workability of austenitic stainless steels. Met. Technol., 1976. 3: p. 358.

44.	X. Duan, T. Sheppard, Influence of forming parameters on static recrystallization behaviour during hot rolling aluminium alloy 5083. Modelling and Simulation in Materials Science and Engineering, 2002. 34(4): p. 363-380.

45.	H.B. Xie, Z.Y. Jiang, W.Y.D. Yuen, Analysis of friction and surface roughness effects on edge crack evolution of thin strip during cold rolling. Tribology International, 2011. 44: p. 971-979.

46.	P.F. Thomason, Ductile Fracture of Metals. 1990. Pergamon Press.

47.	P. F. Thomson, N.M. Burman, Edge Cracking in hot-rolled Al-Mg Alloys. Materials Science and Engineering, 1980. 45: p. 95-107.

48.	J.A. Schey, Prevention of Edge Cracking in Rolling by Means of Edge Restraint. Journal of the Institute of Metals, 1966. 94: p. 193-200.

49.	S. Jun, Effect Of Stress Triaxiality On Micro-Mechanisms of Void Coalesence and Micro-Fracture Ductility of Materials. Engineering Fracture Mechanics, 1991. 39: p. 799-805.

50.	A.C. Mackenzie, J.W. Hancock, D.K. Brown, On the influence of state of stress on ductile failure initiation in high strength steels. Engineering Fracture Mechanics, 1977. 9: p. 167-188.

51.	Y. Bao, T. Wierzbicki, On fracture locus in the equivalent strain and stress triaxiality space. International Journal of Mechanical Sciences 2004. 46.

52.	X. Zhang, Y. Zhang, Y. Li, J. Liu, Cracking initiation mechanism of 316LN stainless steel in the process of the hot deformation. Materials Science & Engineering, 2013. 559: p. 301-306.

53.	A. V. Kuklev, V.V. Sosnin, A. M. Longinov, I. V. Barantseva, A. V. Ziborov, V. V. Zyryanov, S. A. Kulagin, M. S. Kuznetsov, G. I. Kotel’nikov, Reasons for the formation and growth of edge cracks on hot-rolled plates of steel 10KhSNDA. Metallurgist, 2008. 52(5-6): p. 289-292.

54.	C. Puncreobutr, P.D. Lee, M. Kaye, D. Balint, D. Farrugia, T. Connolley, J. Lin, Quantifying damage accumulation during the hot deformation of free cutting steels using ultra-fast synchrotron tomography, in IOP Conference Series: Materials Science and Engineering. 2012.

55.	J. Besson, C. Berdin, Local approach to fracture. 2004, Ecole des Mines de Paris.

56.	J.M. Rodriguez-Ibabe, M.C. Revilla, N. Gonzalez, D.C.J. Farrugia, Z. Husain, G. Claxton, D. Wilcox, M. Whitwood, E. McGee, B. Cheong, M. Llanos, V. Santisteban, J.H. Bianchi, F. Macci, F.D. Vici, P.O. Bouchard, M. Bernacki, E. Roux, PACROLP-II: The prediction and avoidance of cracking in long product hot rolling. Phase II. 2012.

57.	C. Luo, Modeling the behavior of inclusions in plastic deformation of steels. 2001, University in Stockholm.

58.	C. Luo, U. Stahlberg, A mesomechanical approach for studying the material behavior close to non-metallic inclusions in steel hot rolling, in 2nd European Rolling conference. 2000: Sweden.

59.	J.P. Bandstra, D.A. Koss, A. Geltmacher, P. Matic, R.K. Everett Modeling void coalescence during ductile fracture of a steel. Materials Science and Engineering A 2004. 366: p. 269–281.

60.	Y.Q. Wu, H.J. Shi, K.S. Zhang, H.Y. Yeh, Numerical investigation of grain boundary effects on elevated-temperature deformation and fracture. International Journal of Solids and Structures 2006. 43: p. 4546–4577.

61.	S.A. Asgari, P.D. Hodgson, C. Yang, B.F. Rolfe Modelling of advanced high strength steels with the realistic microstructure-strength relationships. Computational Materials Science, 2009. 45(4): p. 860–866.

62.	M.S. Thompson, H. Schell, J. Lienau, G.N. Duda, Digital image correlation: A technique for determining local mechanical conditions within early bone callus. Medical Engineering & Physics, 2007. 29: p. 820-823.

63.	T.J. Keating, P.R. Wolf, F.L. Scarpace, An Improved Method of Digital Image Correlation. Photogrammetric Engineering and Remote Sensing, 1975. 41(8): p. 993-1002.

64.	A. Davidkova, M.K. Jain, R.H. Petrova, D.S. Wilkinson, R.K. Mishra, Strain localization and damage development during bending of Al–Mg alloy Sheets. Materials Science and Engineering A, 2012. 550: p. 395-407.

65.	H. Ghadbeigi, C. Pinna, S. Celotto, Quantitative Strain Analysis of the Large Deformation at the Scale of Microstructure: Comparison between Digital Image Correlation and Microgrid Techniques. Experimental Mechanics, 2012. 52: p. 1483-1492.

66.	M.S. Loveday, G.J. Mahon, B. Roabuck, A.J. Lacey, E.J. Palmiere, C.M. Sellars, M.R. van der Winden, Measurement of flow stress in hot plane strain. 2006, University of Sheffield.

67.	S. Almaguer, C.M. Sellars, W.M. Rainfort, Study of the Static Recrystallisation of an Fe-%30Ni Alloy and Comparison with Plain Carbon Steels. Recrystallization and Grain Growth, 2001. 2: p. 831-836.

68.	B.M.B Grant, H.J. Stone, P.J. Withers, M. Preuss, High-temperature strain field measurement using digital image correlation. The Journal of Strain Analysis for Engineering Design, 2009. 44: p. 263-271.

69.	P.F. Thomson, N.M. Burman, Edge cracking in Hot-rolled Al-Mg Alloys. Materials Science & Engineering, 1980. 45: p. 95-107.

70.	B. Dodd, P. Boddington, The causes of edge cracking in cold rolling. Journal of mechanical working technology, 1980. 3: p. 239-252.

71.	M.H. Han, S. Lee, N.J. Kim, K.J. Lee, T. Chung, G. Byun, Analysis and prevention of edge cracking phenomenon during hot rolling of non-oriented electrical steel sheets. Materials Science & Engineering: A, 1999. 264: p. 47-59.

72.	G.Cusminsky, F. Ellis, An inverstigation into the influence of edge shape on cracking during rolling. Journal of the Institute of Metals, 1967. 95: p. 33-37.

73.	P.D Nicolaou, S.L. Semiatin, An experimental and theoretical investigation of the influence of stress state on cavitation during hot working. Acta Materialia, 2003. 51: p. 613-623.

74.	A.M. Othman, J. Lin, D.R. Hayhurst, B.F. Dyson, Comparison of creep rupture lifetimes of single and double notched tensile bars. Acta Metallurgica et Materialia, 1993. 41: p. 17-24.

75.	A.L. Gurson, Continuum Theory of Ductile Rupture by Void Nucleation and Growth: Part I-Yield Criteria and Flow Rules for Porous Ductile Media. Journal of Engineering Materials and Technology 1977. 99: p. 2-15.

76.	H. Just, A. Behrens, Investigations on the use of damage indicating criteria in FE simulations of cold and semi-hot bulk forging operations, in ASME International Mechanical Engineering Congress and RD&D Expo. 2004.

77.	L.M. Kachanov, Rupture time under creep conditions. Izvestia Akademii Nauk SSSR, 1958. 8: p. 26-31.

78.	A. Nicholson, D. Smith, P. Shaw, Hot workability testing at united steel companies. 1968: The Iron & Steel Institute.

79.	T. J. Baker, J.A. Charles, Deformation of MnS Inclusions in Steel. Journal of The Iron and Steel Institute, 1972. 210: p. 680-690.

80.	M.A. Sutton, J.J. Orteu, H. Schreier, Image correlation for shape, motion and deformation measurements. 1950: Springer.

81.	B. Pan, D. Wu, Z. Wang, Y. Xia, High-temperature digital image correlation method for full-field deformation measurement at 1200 ◦C. Measurement Science and Technology, 2011. 22.

82.	H. Ghadbeigi, C. Pinna, S. Celotto, J.R. Yates, Local plastic strain evolution in a high strength dual-phase steel. Materials Science and Engineering A, 2010. 527: p. 5026-5032.

83.	N.J. Karanjgaokar, C.S. Oh, I. Chasiotis, Microscale Experiments at Elevated Temperatures Evaluated with Digital Image Correlation. Experimental Mechanics, 2011. 51: p. 609-618.

84.	E.A. Torres, F. Montoro, R.D. Righetto, A.J. Ramirez, Development of high temperature strain instrumentation for in situ SEM evaluation of ductility dip cracking. Journal of microscopy, 2014(254): p. 147-165.

85.	L. Allais, M. Bornert, T. Bretheau, D. Caldemaison, Experimental characterization of the local strain filed in a heterogeneous elastoplastic material. Acta Metallurgica et Materialia, 1994. 42(11): p. 3865-3880.

86.	C. Pinna, J.H. Beynon, C.M. Sellars, M. Bornert, Experimental investigation and micromechanical modelling of hot deformation of duplex stainless steels. Mathematical modelling in metal processing and and manufacturing, 2000.

87.	G. Martin, D. Caldemaison, M. Bornert, C. Pinna, Y. Bréchet, M. Véron, J.D. Mithieux, T. Pardoen, Characterization of the High Temperature Strain Partitioning in Duplex Steels. Experimental Mechanics, 2013. 53: p. 205-215.

88.	A. Soula, D. Locq, D. Boivin, Y. Renollet, P. Caron, Y. Bre´chet, Quantitative evaluation of high temperature deformation mechanisms: a specific microgrid extensometry technique coupled with EBSD analysis. Journal of Materials Science, 2010. 45: p. 5649–5659.

89.	ABAQUS 6.11 documentation. Dassault systemes 2011.

90.	N. Brink, Edge cracking of hot rolled steels: Laboratory simulation and microstructural analysis. 2011, Tata Steel, The University of Sheffield, University of Eindhoven.

91.	P. Munther, J.G. Lenard, Tribology during Hot, Flat Rolling of Steels. CIRP Annals - Manufacturing Technology, 1995. 44(1): p. 213-216.

92.	J.F. Lin, T.K. Huang, C.T. Hsu, Evaluation of lubricants for cold strip rolling. Wear, 1991. 147(1): p. 79-91.

93.	J.S. Hinton, Testing on the IMMPETUS Thermo-mechanical Compression (TMC) Test machine. 2009, University of Sheffield.

94.	L.E.H. Castillo, Determination of micro-scale strain distribution in hot-worked steel microstructures. 2005, University of Sheffield.

95.	J.C. Nabity, Nanometer Pattern Generation System. 2004.

96.	G. Gutierrez, Gridanalysis, University of Sheffield. 2005.

97.	LAVision, DaVis Strain Master Software. 2005.

98.	Surfer, in Surface Mapping System, G.S. Inc, Editor.: Colorado.

99.	R. Kiessling, N. Lange, Non-metallic inclusions in steel. 1978: The metals society.

100.	SigmaScan, Systat Software Inc.

101.	Chalon, Modelling of the microstructural deformation of duplex stainless steel during plane strain compression. 2004, University of Sheffield.

102.	M.A. Mohtadi-Bonab, M. Eskandari, J.A. Szpunar, Texture, local misorientation, grain boundary and recrystallization fraction in pipeline steels related to hydrogen induced cracking. Materials Science & Engineering A, 2015. 620: p. 97-106.

103.	M. Kamaya, Assessment of local deformation using EBSD: Quantification of local damage at grain boundaries. Materials Characterization, 2012. 66: p. 56-67.

104.	C. Pinna, Y. Lan, Local Strain Measurement in Hot Deformed Microstructures. Applied Mechanics and Materials, 2007. 7-8: p. 167-172.

105.	L.E. Hernandez-Castillo, J.H. Beynon, C. Pinna, S. van der Zwagg, Micro-scale strain distribution in hot-worked duplex stainless steel. Steel Research International, 2005. 76(2-3): p. 137-141.

106.	C. Boldetti, C. Pinna, I.C. Howard, G. Gutierrez, Measurement of deformation gradient in hot rolling of AA3004. Experimental Mechanics, 2005. 45(6): p. 517-525.

107.	E. Kardoulaki, J. Lin, D. Balint, D. Farrugia, Triaxiality Effect on Material Damage Evolution in Hot Rolling. Key Engineering Materials, 2014. 622-623: p. 1041-1048.

108.	W.J. Kim, H.K. Kim, W.Y. Kim, S.W. Han, Temperature and strain rate effect incorporated failure criteria for sheet forming of magnesium alloys. Materials Science and Engineering, 2008. 488: p. 468-474.

# Appendix

## Data

### TMC data correction

Collected data from TMC machine, namely time, sample temperature, measured load, displacement and velocity are used to plot useful graph. A typical load- displacement curve that shown in Figure 8.1 is plotted based on the raw data collected from TMC machine.

Figure 8.1 Load against displacement graph of raw data from TMC

The data obtained from the TMC machine requires a series of corrections in order to produce a more reliable stress-strain curve [3].

The list of corrections which was done on the data is shown below:

#### Origin correction

The graph was shifted by 0.025 to the right, so that the plotted graph starts from the origin (no displacement when no force is applied).

Figure 8.2 Load against displacement graph with origin correction

#### Compliance correction

The slope of the curve from Figure 6.3.2b at 0.40278mm is:

72.04-00.403-0=178.85kN/mm

A compliance correction is then calculated:

Compliance corrected height=origin corrected height-loadslope

and applied to all the data points as shown in Figure 8.2 to produce a graph as shown in Figure 8.3.

Figure 8.3 Load against displacement graph with compliance correction

#### Breadth spreading correction

Due to the compressive forces, the sample material spreads along the breadth direction so in order to perform a correction, a spread coefficient is introduced from the deformed sample measurements:

Spread coefficient, Cb=bfbo-11-(hfho)0.5

By substituting Cb into the following equation; a corrected breadth value is obtained:

Breadth at intermediate time, b= bo1+Cb-Cb(hho)0.18

The corrected breadth values are used in the following corrections.

#### Friction correction

In order for the friction correction, a zo, which relates the position of tool width to the friction condition, is introduced:

zo=h2μIn12μ		Where friction coefficient, μ is equal to 0.4

The values of zo shows different friction conditions, and hence, the value of shear flow stress, k is calculated differently depending on friction conditions.

| 2zo>w (sliding friction) | p2k=1bw2h2μ2 + b-whμ expμwh-1-2hμb |
| --- | --- |
| w>2zo>0 (partial sticking friction) | p2k=hbw12μ-1+w2-zoμw+ w2-zo2hw+1μb2zo2w-zo-2hzoμw+h2μ-h+h2wμ2-2h2wμ +1hbzo2-4zo33w-w212 |
| 0>2zo (Sticking friction) | p2k=1+w4h-w212hb |

After the shear flow stress k is found, the equivalent stress σ is calculated as shown in following section.

#### Stress and strain value calculated

a) Equivalent strain is calculated as below:

e= 23e22+e2e3+e32		Where e2 = Log(bbo), 	 e3 = Log(hho)

b) After the equivalent strain is calculated and tabulated, the strain correction factor f is introduced in order to calculate the value of equivalent stress. The value of f is dependent on the strain value of e2 and e3 as shown below:

| For e3 ≥ 0 and e2 ≤0 , f = 1.155 | Otherwise, f = -ee3 |
| --- | --- |

With the value of f obtained, equivalent stress σ=2kf is calculated and tabulated. A Stress- strain curve is then plotted as shown in Figure 8.4.

Figure 8.4 Stress against strain graph with strain rate

### Stress/ strain curves obtained from Gleeble machine

Several stress strain curves were obtained from Gleeble machine and they are plotted as shown in Figure 8.5 (1000⁰C) and Figure 8.6 (850⁰C) .

Figure 8.5 Stress strain curves of FCS, Fe-30wt%Ni+S and Fe-30wt%Ni

Figure 8.6 Stress strain curves of FCS at 850⁰C

## Deformed specimens

Figure 8.7 a shows un-deformed specimen with welding of insert in the middle. PSC test must start with a sample trial to ensure the machine works fine, Figure 8.7 b shows TMC machine fail to operate as expected while Figure 8.7 c shows a successful compressed test specimen.

Figure 8.7 a) Inserts welded into the PSC holder b) fail test specimen c) deformed specimen

## Heat treatments

Early stage of polishing and etching is not in the best condition, so the picture produced is in least quality. However, reasonable images to examine the condition of heat treatment for Fe-30wt%Ni. Figure 8.8 shows microstructure of Fe-30wt%Ni after heat treatment at 1200⁰C for corresponding period of time. The results shows that heat treatment of 10mins is able to generate equiaxed grains for study.

Figure 8.8 Microstructure of Fe-30wt%Ni after heat treated for a) 10mins b) 15mins c) 20mins

## Grinding and polishing

Grinding and polishing skill is part of the challenging process and yet, it is essential part for microstructure observation. Figure 8.9 a shows poorly polished Fe-30wt%Ni microstructure after etching. The heavily scratched surface as shown in Figure 8.9 a are due to the poor grinding process while the dots that appeared on the surface of Fe-30wt%Ni shown in Figure 8.9 b could be due to poor etch conditions. Finally, Figure 8.9 c shows the best polished condition for Fe-30wt%Ni.

Figure 8.9 Fe-30wt%Ni surface with a) poor polishing and etching b) improved polishing but poor etching c) well-polished and right etching condition

## Etching conditions

Figure 11.3a, b & c show outcomes of different etching conditions. Wiping specimen’s surface with solution wetted cotton gives the worst result (Figure 8.10 c): there is no visible grain boundaries and with the most amounts of dots appeared. Pour solution on top of specimen’s surface reveal the grain boundaries but indicates over etching as shown in Figure 8.10 b. Finally, dipping the specimen in the acid solution for 45 second reveals grain boundaries and minimised the amount of black dots as shown in Figure 8.10 a. Therefore, dip the specimen in the acid solution for 45 second is the best etching condition found.

Figure 8.10 Microstructure of Fe-30wt%Ni after a) dip in solution for 45s b) pour solution on top of specimen surface c) wipe specimen’s surface with solution wetted cotton

### Chemical etching of Fe-30wt%Ni+S

Etching condition and solution for Fe-30wt%Ni was used to etch Fe-30wt%Ni+S. However, such etching solution was not suitable for Fe-30wt%Ni+S due to the appearance of non-metallic inclusions. Acid reacts rapidly with inclusions rather than grain boundaries as shown in Figure 8.11.

Figure 8.11 Chemically etched Fe-30wt%Ni+S

## Microgrid

There are challenges during the production of microgrid. One of the challenges is the quality of deposited resin on which it will detached from the surface during the microgrid printing as shown in Figure 8.12 a. Such problem can be due to the poor resin solution, unclean surface or poor heating process. On the other hand, during printing of microgrids through the electron beam control in SEM, perfectly square grids can become rectangular as shown in Figure 8.12 b. This is due to the error in voltage control setting in x and y axis between the NPGS and SEM. Finally, errors such as electron beam size, printing time, printing speed and as well as magnification control can lead to resin removal for entire area (Figure 8.12 c) rather than grid pattern. Such challenge can be overcame only through multiple trials and errors to obtain optimum printing conditons.

Figure 8.12 a) Detached resin from the surface b) un-even microgrid c) resin removal from the surface

Other than that, another great impact factors to the outcome of microgrids are the printing speed/ printing time of the electron beam and resin thickness. For instance, electron beam cannot burn through a thick resin and left with microdots instead of microgrids as shown in Figure 8.13 a. Unevenly spread resin thickness can cause the microgrid to be printed partially as shown in Figure 8.13 b. Finally, the gold thickness shall be controlled through deposition time so that it will not be too thick enough to trap resin within as shown in Figure 8.13 c.

Figure 8.13 a) Microdots b) partially distributed microgrids c) resin trapped under gold layer

## Microgrid after test

Gold microgrid was test to its limit up to 1200⁰C. Encouraging result obtained despite its imperfection as shown in Figure 8.14. Figure 8.15 a and b shows photomicrograph of PSC tested microgrid at 1000⁰C. Due to poor welding and sealing of samples, oxidation caused microgrids to lose its visibility but the microstructure of Fe-30wt%Ni can still be observed as shown in Figure 8.15 b.

Figure 8.14 Microgird on Fe-30wt%Ni after test at 1200⁰C a) secondary electron signal imaging b) backscattered electron signal imaging

Figure 8.15 Fe-30wt%Ni after test at 1000⁰C a) test 1 b) test 2

On the other hand, 2.5 micron pitched microgrid deposited onto Fe-30wt%Ni+S that undergoes PSC tests at 1000⁰C also fail to survive due to the poor welding and oxidation issue. Figure 8.16 a and b shows oxidized microstructure of Fe-30wt%Ni+S on which materials were ridded off the surface (Figure 8.16 b).

Figure 8.16 Fe-30wt%Ni+S after test at 1000⁰C a) test 1 b) test 2